## Slide 1: Heat Transport
NE 591

## Slide 2: Last Time
Mining -> Processing -> Conversion -> Enrichment -> Powder -> Compaction/Sintering -> Rod/Assembly
U3O8 must be converted to UF6 for enrichment, which is then converted to UO2 powder for pellet manufacture
For different fuel types, enriched UF6 follows a different path

## Slide 3: Last Time
General heat transport
Heat is produced in the fuel, transports through the cladding and gap, and into the coolant
The geometry of our problem
The initial condition of T
The boundary conditions of T
Is each parameter is a function of T
  Thermal conductivity, heat capacity
Function of space/time?
  Heat generation, dependent upon flux

## Slide 4: The most accurate solution is numerical, in 3D, requires modeling the entire core, and is multi-physics
Solution is 3D and changes in time
All the properties are functions of temperature
The boundary conditions comes from information about the coolant flow
The heat generation rate comes from information about the neutronics in the reactor
No analytical solution is possible

## Slide 5: In order to solve, make assumptions!
#1: steady state ->
#2: axisymmetric ->
#3: constant in z
#4: constant thermal conductivity

## Slide 6: Directly Solving for Temperature Profile
Boundary conditions: r0 = 0, r1=R, T’(0) = 0, T(R) = Ts
r0
r1

## Slide 7: Linear Heat Rate
  Where Qav is the radially averaged heat generation rate, in units of per-length, i.e. W/cm
Substitute LHR into previous equation on T0-Ts

## Slide 8: Heat transport through the gap
The heat flux gives the rate, per unit area, at which heat flows in a given direction
The heat flux from the fuel is the LHR/pellet circumference
Heat flux from the fuel is the same as heat flux into the gap
Gap thickness = Rg-Rf = tg
Cladding thickness = Rc-Rg = tc
R0=0
R1=Rf
R2=Rg
R3=Rc

## Slide 9: Heat transport through the gap
Set heat flux fuel/gap equal
Gap conductance is defined as:
Gap conductance depends on the gas filling the gap
  For pure He, kgap=16x10-6 * T0.79 (W/cm-K)
  For pure Xe, kgap=0.7x10-6 * T0.79 (W/cm-K)
  Simple mixing rule: kgap = kHe1-y x kXey
=

## Slide 10: Heat transport through the cladding
Heat flux through the cladding
Set equal your heat fluxes
My nomenclature is often also seen where Tgap = TCI, Tclad = TCO

## Slide 11: Heat transfer to the coolant
Heat is transported from the cladding to the coolant via convection
Tcool is the coolant temperature, hcool is the convective heat transfer coefficient between cladding wall and coolant
Adding gap + cladding + coolant:
+

## Slide 12: Summary of analytical solutions