## Slide 1: Fuel Chemistry
NE 591

## Slide 2: Last Time
Basic materials science overview
  Crystal structures
  Point defects, dislocations, grain boundaries, etc.
Began fuel chemistry
  UO2 stoichiometry

## Slide 3: Incorporation of Fission Products
As fission products form, the valance state of the uranium can change
Valance of soluble fission products is M3+ (typical)
The uranium valance state changes to compensate
  Oxygen liberated by fission
  Fission products produced with M3+ valance state incorporated in fuel lattice
  Uranium oxidizes from U4+ to U5+ or U6+ to maintain local electrical neutrality

## Slide 4: Oxygen potential
The oxygen potential is a measure of how free the oxygen is to escape/move around
Oxygen potential is defined as or, equivalently
With = Chemical potential of oxygen in solution
= Gibbs free energy of gaseous oxygen at temperature T and a standard pressure (1 atm)
It is possible to determine the stoichiometry from the oxygen potential

## Slide 5: Oxygen potential
The oxygen potential changes during irradiation, indicating change in the O/M ratio
Oxygen potential changes during irradiation due to
  Liberation of oxygen by fission
  Generation of fission products
  Conversion of uranium to plutonium
  Reaction of oxygen with U, Pu, fission products, and cladding
Oxygen potential across pellet radius observed to be constant at the approximate value of Mo/MoO2 reaction (from calculations)
Oxygen potential is low near the cladding, because the oxygen enters the cladding

## Slide 6: Fuel Stoichiometry/Properties
The stoichiometry of the fuel directly impacts the fuel performance
Stoichiometry impacts
  Melting temperature
  Thermal conductivity
  Processes dependent on diffusion
    Grain growth
    Fission gas release
    Creep
  Chemical state and behavior of fission products
  Chemical reactions at inner cladding surface
Thermal conductivity is highest for stoichiometric UO2

## Slide 7: Fuel Stoichiometry/Properties
The lattice constant of the material decreases with increasing stoichiometry
The vacancy formation energy also changes with stoichiometry

## Slide 8: Fuel Stoichiometry/Properties
The solution energy of Xe, Cs, and Sr in UO2 depends on stoichiometry as well
The coefficient defining Xe diffusion also changes with stoichiometry
Though stoichiometry matters, most fuel performance codes ignore it
Fission product | UO1.97 | UO2 | UO2.03
Xe | 3.88 eV | 3.88 ev | 2.61 eV
Cs | 1.7 eV | -0.04 eV | -3.29 eV
Sr | -3.71 eV | -6.03 eV | -9.55 eV

## Slide 9: Fuel Chemistry Summary
UO2 has a cubic flourite structure that is very stable
The charges are balanced with a U4+ valance state
However, the ratio of oxygen to uranium can change. We call this the stoichiometry and abreviate it as O/M ratio
The O/M ratio changes during reactor operation, but it is complicated
The O/M ratio impacts many properties of the fuel

## Slide 10: Grain Growth

## Slide 11: Grain Growth in UO2
Materials are typically composed of various regions where the crystal lattice is oriented differently
When two grains meet, there is a plane of atoms that do not follow the crystal lattice called a grain boundary
Grain boundaries add energy to the material that is a function of their structure
A grain boundary’s energy is determined by its:
  Inclination – the orientation of the 2D grain boundary plane (2 degrees of freedom)
  misorientation – the rotation required to align one grain with the other (3 degrees of freedom)

## Slide 12: Texture
The orientation of all the grains in a material is called the texture
Electron back scatter diffraction map for cubic crystal structure
Orientation distribution function

## Slide 13: Grain size
In a polycrystal, there is also a distribution of grain sizes
The average grain size of the fuel has a significant impact on its behavior
Typical LWR fuel as an initial average grain size of about 10 microns
The average grain size impacts
  Fission gas release
  Swelling
  Thermal conductivity
  Creep

## Slide 14: Grain boundary diffusion
Diffusion often occurs faster along grain boundaries than in the perfect crystal
Grain boundaries have more space than the perfect lattice
So, atoms diffuse faster along grain boundaries than through the perfect lattice
This means that grain boundary, or intergranular, diffusion increasingly dominates volume, or intragranular, diffusion as the temperature is reduced.
Grain boundary vacancy diffusion has a large impact on creep

## Slide 15: Grain boundary segregation
Impurity atoms (such as fission gas) and other defects move to grain boundaries
Due to grain boundaries having more open space, impurity atoms have a lower energy when they are on grain boundaries.
This is called grain boundary segregation

## Slide 16: Dislocation interaction with grain boundaries
Grain boundaries impede dislocation motion
The number of dislocations within a grain impact how easily dislocations can traverse grain boundaries and travel from grain to grain.
So, by changing grain size one can influence dislocation movement and yield strength.
This is called the Hall-Petch effect

## Slide 17: Grain boundaries and cracks
Materials often crack along grain boundaries
Grain boundaries can be weaker than the perfect lattice
Thus, fracture will often occur along grain boundaries (intergranular fracture)

## Slide 18: Grain size change
A single crystal has a lower energy state than a polycrystal, due to the grain boundary energy
So, grain boundaries migrate to reduce the energy
vGB = MGB (Pd – Pr)
  MGB is the grain boundary mobility
  Pd is the driving force (pressure) for grain growth
  Pr is the pressure resisting grain growth

## Slide 19: Grain growth
Due to grain boundary migration, the average grain size goes up with time
As grain boundaries migrate, some grains grow and some shrink
Shrinking grains eventually disappear
The average grain volume
Therefore, as Ngrains decreases due to grain disappearance, the average grain volume goes up

## Slide 20: Grain boundary mobility
The grain boundary mobility is a function of temperature and GrB type
The grain boundary mobility is determined according to
  m4/(J s)
  kb = 8.6173e-5 eV/K is the Boltzmann constant
Both the pre-factor M0 and the activation energy Q change as a function of the grain boundary misorientation
We often use an average grain boundary for a material, taken from polycrystal measurements-> UO2: M0 (m4 /J-s) = 4.6e-09, Q (eV) = 2.77
What is the mobility of UO2 at 1600 K?
  MGB = 4.6e-9*exp(-2.77/(1600*8.6173303e-5)= 8.7e-18 m4/J-s

## Slide 21: Grain growth
There are various driving forces for grain growth
The most common driving force is the reduction of grain boundary energy
  , where γGB is the GB energy and R is the radius of curvature
  It is often called the curvature driving force, because it drives grain boundaries to be straight
  It also causes larger grains to grow at the expense of smaller ones
Other driving forces include
  Temperature gradients
  Elastic energy gradients
  Dislocation energy gradients
  Magnetic free energy density gradients
Velocity of a spherical grain:

## Slide 22: Grain growth
Grain boundary motion is inhibited by pores, precipitates, solute atoms, etc.
Solute atoms (whether in interstitial sites or vacancies) can decrease the grain boundary mobility.
  This is called Solute Drag
  Even a small concentration of impurities can decrease the mobility by 3 to 4 orders of magnitude
Particles and pores resist grain boundary motion

## Slide 23: Irradiation can accelerate grain growth, but it is only significant with small grains and low temperature

## Slide 24: Maximum grain size
Consider a material with an average grain size D
The change in D can be written as
  k = 2 MGB γGB is a rate constant that can be determined from experiments
  Dm is the grain size at which the driving force equals the resistive pressure
For UO2:
Dm is a function of temperature microns

## Slide 25: Fuel Densification
Remember that fresh fuel pellets are not fabricated to be 100% dense, more like 95-99% dense
Early in life, fuel pellets shrink and the initial porosity is largely eliminated
In some ways, densification is a continuation of the sintering process
However, irradiation accelerates the process
Small pores close due to effects of fission spikes and vacancy diffusion
Large pores stable (in absence of large hydrostatic stress)
Pellets with higher initial density, densify less

## Slide 26: Densification
The driving force for densification is the change in free energy from the decrease in surface area of pores and lowering of the surface free energy
An empirical relation to describe densitifcation has been built as a function of
  β - Burnup (in FIMA)
  Δρ0 – Total densification that can occur ~ 0.01
  βD – Burnup at which densification stops ~5 MWD/kgU, ~0.005 FIMA
  CD = 7.235 − 0.0086 (T − 25) for T < 750 C and CD = 1 for T ≥ 750 C

## Slide 27: Empirical models
Many models of reactor fuel behavior are fits to experimental data
They are typically correlated to burnup
Burnup is a measure of how much fissioning has taken place. Typical units are:
  MWD/kgU
  FIMA
It can be calculated from the volumetric fission rate
Units of this equation are FIMA
To convert from FIMA to MWD/kgU, multiply by 950
after Garzarolli in [Rudling et al, 2007]

## Slide 28: Summary
The average grain size in UO2 impacts
  Fission gas release
  Swelling
  Thermal conductivity
  Creep
The material wants to reduce its energy by having large grains grow at the expense of small grains
Grain growth eventually stops due to other defects reducing the grain boundary migration
Fuel densification is driven by reduction in surface area of pores
Empirical models describe densification as a function of burnup