## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2024

## Slide 2: Exam 2
Average: 90.7
Stdev: 8.6
No curve this time
If you have any questions or comments, observed discrepancies, etc., let me know

## Slide 3: MOOSE Project Notes
For part 2, I want everyone to use contact and gap heat transfer
You can compare your results from part 1 and the analytical solution as an initial stage of verification
Some of you may have done this, I have not worked through all input files yet
Make sure your executable has contact compiled, and you have a thermal contact block
The rest I leave for you to figure out

## Slide 4: Last Time
The average grain size in UO2 impacts fuel behavior and performance
The material wants to reduce its energy by having large grains grow at the expense of small grains
Fuel densification is driven by reduction in surface area of pores – continuation of sintering process
Started fuel chemistry

## Slide 5: Fuel Stoichiometry/Properties
The lattice constant of the material decreases with increasing stoichiometry
The vacancy formation energy also changes with stoichiometry

## Slide 6: Fuel Stoichiometry/Properties
The solution energy of Xe, Cs, and Sr in UO2 depends on stoichiometry as well
The coefficient defining Xe diffusion also changes with stoichiometry
Though stoichiometry matters, most fuel performance codes ignore it
Fission product | UO1.97 | UO2 | UO2.03
Xe | 3.88 eV | 3.88 ev | 2.61 eV
Cs | 1.7 eV | -0.04 eV | -3.29 eV
Sr | -3.71 eV | -6.03 eV | -9.55 eV

## Slide 7: Fuel Chemistry Summary
UO2 has a cubic fluorite structure that is very stable
The charges are balanced with a U4+ valence state
However, the ratio of oxygen to uranium can change. We call this the stoichiometry and abbreviate it as O/M ratio
The O/M ratio changes during reactor operation, but it is complicated
The O/M ratio impacts many properties of the fuel

## Slide 8: Fission products

## Slide 9: Fission Product Generation
Fission releases around 200 MeV
  The fission fragments have 169 MeV of kinetic energy
  2 to 3 neutrons with an average energy of 2 MeV
  7 MeV of prompt gamma ray photons
  The remaining energy is released by beta decay
Every fission product that is produced is now in the crystal lattice of the fuel, changing the chemistry/microstructure

## Slide 10: There are various types of fission products that form
Noble gases (Xe, Kr)
Essentially insoluble in the fuel matrix
Form either intragranular (within grain) voids or bubbles or intergranular (grain boundary) bubbles
Volatiles (Br, Rb, Te, I and Cs)
Exist as gases at high temperatures of the pellet interior
Also exist as solids at the cooler pellet exterior
Metals (Mo, Ru, Pd, and Tc)
Form metallic precipitates
Insoluble oxides (Zr, Ba and Sr)
Form insoluble oxides in the fluorite lattice
Soluble oxides (Y, La and the rare earths)
Dissolved in the cation sublattice

## Slide 11: All fission products impact the behavior of the fuel

## Slide 12: Fission Product Evolution
Not only are the absolute proportion of fission products accumulating with time, but the relative proportions are changing with respect to one another
There are continuous transitions between the groups as the critical concentration conditions for new phase development are surpassed because of increased burnup
Since fission releases two oxygen but only one metal atom, and not all metal atoms will react to bond the oxygen, the O/M ratio of the fuel slowly increases during burnup

## Slide 13: Oxide Formation
With burnup, the liberated oxygen will associate with U, Pu, and La but may not be in sufficient supply to combine with Pd and other less oxidizing elements
If the Gibbs energy of formation of the given fission product lies below the fuel oxygen potential, the element will be capable of forming an oxide (Ce, Sr, Ba)
If the reaction line is above the oxygen potential in the fuel, the fission product will exist as an element in the fuel (in a separate metallic phase) (Ru, Pd, Tc)

## Slide 14: Soluble/Insoluble Fission Products
When a 4+ valence fission product (e.g.,Zr4+) enters the lattice, there is no change in the electrical neutrality
If the charge of the fission-product cation is lower than U+4, the site occupancy of the lattice is altered to achieve electrical neutrality
The alkaline earth cations Ba+ and Sr2+ have large ionic radii and form a separate oxide phase
Fission products that have limited solubility in UO2 will segregate to the grain boundaries and voids

## Slide 15: Fission Product Segregation/Precipitation
Fission products can be segregated because of their migration to specific locations such as intragranular segregations, grain boundaries, or pellet surfaces
Metallic inclusions are commonly observed in ceramographs from irradiated samples
They are formed by isotopes of Mo, Tc, Ru, Rh, Pd, Ag, Cd, In, Sn, Sb, and Te
These inclusions are found at the surface of the grain boundaries and are associated, in general, with grain boundaries and intragranular bubbles
Some of the components of these precipitates can be oxidized or reduced forming other compounds that can be released from the fuel matrix
Cs, Ru, Te, and Ba have been consistently found at the cracks in the pellet and on the clad inner surface
The white inclusions are metallic precipitates, which are composed of Mo, Tc, Rh, Ru, and Pd, form a quinary alloy in an hcp structure
A “gray oxide phase” perovskite structure containing different combinations of Ba, Cs, Zr, Mo, and U can also form

## Slide 16: Volatile/Gaseous Fission Products
Xe release occurs at the central region of the pellet where the highest temperatures were achieved during irradiation
Volatile FPs are released from the fuel matrix similar to that of the noble gases
Volatile fission products in the gap can react among themselves, resulting in a changing chemical speciation
The kinetics of formation/decomposition of CsI and Zr iodides are possible factors in the mechanism of SCC

## Slide 17: FP Interaction with Zr Cladding
Fission fragments will deposit on the inner surface of the cladding
Some of these species can diffuse into the cladding, while others can attack the cladding thereby initiating cracks that can later progress with the formation of through-wall cracks
Oxygen will diffuse into the cladding and contribute to its oxidation state
Measurements have shown deposits of Sr, Cs, Pu, and Am
The corrosion behavior of zirconium by Te has been reported
The chemical reaction between some corrosive fission products and the cladding can lead to PCI
Fission products such as Cs, Cd, or I can attack the cladding inducing crack initiation, which then progress through the cladding by intragranular and transgranular cracking modes

## Slide 18: Fission Gas Release

## Slide 19: Fission Gas Release
Fission gases (Xe, Kr) are released in a process composed of three stages in UO2
Stage 1: Gas atoms are produced throughout the fuel due to fission and diffuse towards grain boundaries
Small intragranular bubbles form within the grains, but never get larger than a few nm radius due to resolution from energized particles
Gas atoms that don’t get trapped within the intragranular bubbles migrate to grain boundaries
Atoms forming a vacancy cluster

## Slide 20: Fission Gas Release
Stage 2: Gas bubbles nucleate on grain boundaries, growing and interconnecting
Stage 3: Gas travels through interconnected bubbles to a free surface

## Slide 21: Fission Gas Release
Fission gas release also occurs due to mechanisms that don’t depend on diffusion
Release can occur to particle recoil and knockout at low temperature
It can occur due to fracture during rapid transients

## Slide 22: Fission Gas Release
Released fission gas enters the gap and plenum, causing various problems
Xe and Kr have very low thermal conductivities, reducing the gap conductance
The plenum pressure increases
The volatile fission gases corrode the cladding
They are also radioactive and hazardous, causing problems when the cladding is breached
Fission gas release experiments:
  Post irradiation annealing
    Fuel is irradiated at low temperature; Fuel is then placed into a furnace and heated; Gas atom release is then measured
  In-pile release
    Gas release is measured during reactor operation; It is much more difficult than post-irradiation annealing; Total amount released is measured by puncturing cladding after irradiation; Release with time can be estimated using a pressure transducer inside an instrumented fuel rod

## Slide 23: Fission Gas Release
Fission gas release models attempt to predict the rate at which gas is released from the fuel
To model fission gas release, ideally, we must model all three stages of gas release
  Diffusion of gas atoms to grain boundaries
  Growth and interconnection of grain boundary bubbles
  Transport of gas atoms through interconnected bubbles to free surfaces
The earliest models only considered Stage 1
Most models now consider stage 1 and 2
There are no models that consider all three stages, but some are under development

## Slide 24: Fission Gas Release
Fission gas release models attempt to predict the rate at which gas is released from the fuel
To model fission gas release, ideally, we must model all three stages of gas release
  Diffusion of gas atoms to grain boundaries
  Growth and interconnection of grain boundary bubbles
  Transport of gas atoms through interconnected bubbles to free surfaces
The earliest models only considered Stage 1
Most models now consider stage 1 and 2
There are no models that consider all three stages, but some are under development

## Slide 25: Booth Model
The Booth model is the earliest model of fission gas release and only considers stage 1
A grain is considered as a simple sphere
Gas atoms are released at the grain boundary
The model solves the diffusion equation in 1D spherical coordinates
Assumptions
  cg(r, t)
  All grains are spheres of radius a
  D is constant throughout the grain
  Gas is produced uniformly throughout the grain
  Gas is released once it reaches the grain boundary
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = 0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 26: Modeling post-irradiation annealing
The initial gas concentration is cg0
No gas is produced
Solving this equation tells us the value of cg at any radius or time
However, we want to know the fraction of gas atoms that have made it to the grain boundary
We use the flux at the grain boundary
Grain boundary
Gas atoms
Release
ICs and BCs
cg(r, 0) = cg0
cg,r(0, t) = 0
cg(a, t) = 0 (release)

## Slide 27: Solving the Booth Model
This equation is solved using a Laplace transform after nondimensionalization
Will not go through the derivation (shown in Olander)
τ = D x t / a2
τ < π-2
τ ≥ π-2
Grain boundary
Gas atoms
Release

## Slide 28: Booth Example
For a diffusion coefficient for Xe of D = 8e-15 cm2/s, what fraction of the fission gas trapped in an post-irradiation annealed fuel pellet has escaped after one hour? It has an average grain size of 10 microns
  D = 8e-15 cm2/s
  a = 10e-4 cm
  t = 3600 s
Which f? τ = D x t/a2 = 2.88E-4 < p-2 = 0.101
  f = 6*sqrt(8e-15*3600/(pi*(10e-4)^2)) – 3*8e-15*3600/(10e-4)^2 = 0.0181

## Slide 29: Different expressions for fission gas release
Given the data from the previous example, can plot both
  t < p-2
  t > p-2