NE 763 Exam 4

Please provide your responses to the following questions. Point values indicated the expected depth of response.

- What are some considerations when optimizing the composition for F/M steels? (10 pts)

- Why do ferritic steels swell considerably less than austenitic steels? (10 pts)

- What is the ductile to brittle transition temperature? Discuss irradiation embrittlement in F/M alloys. (10 pts)

- Why are FeCrAl alloys of interest? What are the considerations for balancing compositions of these alloys? (8 pts)

- What role do the oxide particles play in ODS steels? (6 pts)

- What are some advantages and disadvantages of Ni alloys? (8 pts)

- What are benefits and drawbacks of U-Si fuel compared to U-Al fuel? Describe the differences in U3Si and U3Si2 swelling. (12 pts)

- The gamma phase of U-Mo is not the thermodynamically stable phase at research reactor temperatures. Why is this phase the dominant phase in-reactor? (7 pts)

- What effect does the solidus/liquidus gap have on the fabrication of U-Mo fuels? (6 pts)

- Discuss the evolution of fission gas bubbles in U-Mo fuel as a function of burnup. (10 pts)

- Why is the interaction layer of interest in U-Mo fuels? What mitigation strategies have been deployed to limit the amount of interaction layer? (7 pts)

- Why is Al ideally suited for the research reactor environment when it is unable to be used in LWRs? (6 pts)