## Slide 1
Angelica M. Lopez Morales
Multiscale modeling of fission gas behavior in U3Si2 under LWR conditions
NE 591-Technical Paper Project
T. Barani et al., Journal of Nuclear Materials, 2019. 522: p. 97-110

## Slide 2
Introduction
The goal of this study was to proposed multiscale model of fission gas swelling and release in U3Si2 under LWR conditions for application in engineering fuel analysis
The model includes components for intra-granular and inter-granular behavior of fission gases
Intra-granular: Describes the evolution during irradiation of the average size and number density of intra-granular fission gas bubbles coupled to gas diffusion to grain boundaries.
Inter-granular: Include precipitation, growth, and coalescence of bubbles contributing to fuel swelling, and the eventual thermal fission gas release (FGR).
Challenge: Experimentally derived values for important modeling parameters, such as the lattice diffusion coefficient of gas atoms and the rate of irradiation-induced re-solution of gas atoms from intra-granular bubbles, are unavailable for U3Si2 under LWR condition.
Density Functional Theory (DFT) and Binary Collision Approximation (BCA) calculations were used to estimate these variables

## Slide 3
Density functional theory calculations
v: attempt frequency
a: jump distance
Z: number of sites available for the Xe atom or vacancy to jump to
Ga: activation free energy given by the migration enthalpy and the defect formation and binding energies and entropies
The resulting activation energies and preexponential factors were approximated based on experience from other materials such as UO2
Intra-granular re-solution calculation
The total re-solution rate at which atoms are knocked back into the fuel was calculated by,
: fission rate density
Rb: bubble radius
αo: re-solution parameter
n: number of atoms in a bubble
𝜌: is the bubble concentration distribution function
Gas atoms being knocked out of a gas bubble due to a collision with the fission fragments.
Homogeneous Model
Experimental Procedure

## Slide 4
Intra-granular fission gas behavior model
N: total concentration of bubbles
ɸ= c2/N represents the fraction of dimers over the total number of bubbles
m: total concentration of gas in bubbles
G: production rate of gas atoms
ν: nucleation rate of fission gas dimers →
αn represents the probability per second that an atom is re-solved from a cluster containing n atoms
D is the single gas atom diffusion coefficient in the fuel matrix, Rn is the cluster size, and c1 is the concentration of atoms in the matrix
: probability per second that a single atom is trapped by a cluster containing n atoms
D is the diffusion coefficient of single gas atoms in the fuel matrix, Rsg is the radius of a gas atom, and fn is the nucleation factor.
α0 is a coefficient, which can in principle depend on the cluster size
Experimental Procedure
Considering that process occurs faster than the growth process,

## Slide 5
Intra-granular swelling
Experimental Procedure
Inter-granular swelling
V is the bubble volume
rgr is the grain radius
Ngf is bubble number density
Bubble growth is compensated by gas release in order to maintain the constant coverage condition.
Agf: bubble projected area on the grain face
Thermal FGR is modeled based on a principle of grain boundary saturation

## Slide 6
Irradiation experiment simulation
Irradiation conditions for AI-7-1 experiment
FGR exhibits an incubation behavior, with no release being observed until the grain-boundary bubble coverage attains a saturation level.
Change of the swelling rate can be observed at the onset of FGR.
FGR comparison is not fully consistent, as the calculation refers to the centerline (hottest) portion of the specimen only. As expected, FGR is thus over-estimated.
Results

## Slide 7
Critique
7
The IID mechanism established that the migration energy of defects in ceramics () may change with the charge state of the migrating defect resulting in an overall lowered diffusion barrier.
S and B different charge states
Bourgoin, J. C., et al. (1973). "Ionization enhanced diffusion." The Journal of Chemical Physics 59(8): 4042-404
In the calculation of the diffusivity of the Xe and vacancies in U3Si2 the authors only considered a vacancy diffusion mechanism.
In the article, only the fastest diffusion rate for Xe and uranium vacancies was analyzed.
The authors neglected RED which can drastically influence the diffusivity of the atoms under irradiation.
The authors failed to acknowledge and to discuss other processes that influenced diffusion in ionic irradiated crystal such as the Ionization Induced Diffusion Mechanism.
There are others diffusion mechanism that might play an important role.

## Slide 8
Critique
8
Possible changes in the stichometry of the fuel are not included in the model proposed by the authors
The O/M ratio might change due to:
Oxygen liberation by fission
Reaction of oxygen fission products and cladding
Fission products produced with M3+ valance state incorporated in fuel lattice
The vacancy formation energy, Xe diffusion and FGR can highly be impacted by the stichometry of the fuel.
The model proposed by the authors made estimation for the intra-granular re-solution rate however the inter-granular re-solution calculation was totally neglected.

## Slide 9
Questions ?
Thank You !

## Slide 10
Backup Slides

## Slide 11
Lower number density and a higher radius of intra-granular bubbles compared to UO2 under operational LWR conditions.
This appears consistent with the higher diffusivities of gas atoms and vacancies in U3Si2 compared to UO2.
The decrease in the bubble density is due to the progressive bubble coalescence during growth. Correspondingly, the bubble radius increases.
Results
Intra-granular bubbles
Inter-granular bubbles

## Slide 12
Sensitivity analysis
The Pearson coefficient indicates how strong the correlation of a certain parameter is with respect to the chosen figure of merit.
The normalized sensitivity coefficient provides a measure of the relative variation of the figure of merit with respect to the variation of a specific parameter.
Results
Low impact
Low impact

## Slide 13
Results

## Slide 14
Results

## Slide 15
Density functional theory calculations of defects and fission gas properties
The authors only considered the fastest diffusion rate of Xe and uranium vacancies. For both of these species, the highest diffusivity is obtained for vacancy mechanisms along the c axis.
v: attempt frequency (s-1 ),
a: jump distance (m)
Z: number of sites available for the Xe atom or vacancy to jump to,
Ga: activation free energy given by the migration enthalpy and the defect formation and binding energies and entropies (eV)
Xe diffusion mechanism in U3Si2 involving a Xe atom in a uranium vacancy trap site and a second uranium vacancy assisting diffusion in the c direction.
The resulting activation energies and preexponential factors were approximated based on experience from other materials such as UO2

## Slide 16
Intra-granular fission gas behavior model
N: total concentration of bubbles
ɸ= c2/N represents the fraction of dimers over the total number of bubbles
m: total concentration of gas in bubbles
G: production rate of gas atoms
ν: nucleation rate of fission gas dimers →
αn represents the probability per second that an atom is re-solved from a cluster containing n atoms
D is the single gas atom diffusion coefficient in the fuel matrix, Rn is the cluster size, and c1 is the concentration of atoms in the matrix
: probability per second that a single atom is trapped by a cluster containing n atoms
D is the diffusion coefficient of single gas atoms in the fuel matrix, Rsg is the radius of a gas atom, and fn is the nucleation factor.
α0 is a coefficient, which can in principle depend on the cluster size
Experimental Procedure
Considering that homogeneous nucleation is consistently considered as a process of formation of dimers rather than at the average bubble size

## Slide 17
ω is the van der Waals atomic volume for xenon
𝛀 is the vacancy volume
d/dt is variation rate of the number of atoms per bubble
d/dt is vacancy absorption/emission rate at the bubble
is the number of vacancies per intra-granular bubble
is the intra-granular vacancy diffusion coefficient
𝜌 is the radius of simulated cell
ξ is a dimensionless factor calculated
is the equilibrium pressure of a gas bubble
is the U3Si2/gas specific surface energy
is the hydrostatic stress
p is the pressure in the gas bubble
ɳ is the ratio between and niv.
ψ is the ratio between the radii of the bubble and of the cell
Intra-granular fission gas behavior model
Experimental Procedure

## Slide 18
Inter-granular model
The absorption rate of gas at the grain-boundary bubbles is assumed to equal the arrival rate of gas at the grain boundaries.
All grain-boundary bubbles are considered to have, at any instant, equal size and equal lenticular shape of circular projection.
Re-solution of grain-boundary bubbles is neglected.
The fractional fuel volume change due to grain-boundary fission gas swelling can be estimated as:
V is the bubble volume
rgr is the grain radius
Ngf is bubble number density
Bubble growth is compensated by gas release in order to maintain the constant coverage condition.
Agf: bubble projected area on the grain face
Experimental Procedure
Thermal FGR is modeled based on a principle of grain boundary saturation

## Slide 19
Concentration Rate = Generation Rate- Loss Rate
Eq. 1
Eq. 2
Ko is the production rate of point defects that are free to migrate (dpa/sec)
Cv ,Ci, concentrations of vacancies and interstitials
Cs sinks concentration
Cvo thermal concentration of vacancies
Kiv, reaction rate constant for recombination
Kvs, and Kis reaction rate for vacancy-sink annihilation, and interstitial-sink annihilation, respectively
represent the diffusion into or out of the local volume
Radiation Enhanced Diffusion (RED)
Interstitial-Vacancy Recombination
Annihilation of point defects at sinks