## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2026

## Slide 2: MOOSE Notes
When you login: enter “groups” in the command line
Verify that ne533s26 is listed – this should be fixed… but I want you to verify
Ensure that you have set conda up!
(base) [bwbeeler@login01 ~]$
conda activate /usr/local/usrapps/ne533s26/bwbeeler/moose
cd /share/ne533s26/$USER
#Make your 'input.file'
mpirun -np 2 /usr/local/usrapps/ne533s26/beeler_moose/beeler_moose-opt -i input.file

## Slide 3: MOOSE Project
Three-part project
Will upload input and output files to Moodle
Will upload a written Part 1 report, max of 10 pages (including figures)
This is an individual project, but some collaboration is encouraged
Write up with deliverables from Part 1, choice of materials, mesh, details therein, etc.
Part 1 is due March 3

## Slide 4: MOOSE Project Part 1
Fuel pellet dimensions listed
This is a 1-D problem, but I want your geometry to be set up in 2-D RZ
Assume reasonable values for material properties
Outer cladding temperature is constant: 600 K
Solve temperature profile for:
  Steady-state: Q = 350 W/cm^3
  Compare against analytical solution
Use both a constant k and a temperature-dependent k
Perform a mesh convergence study
Use transient solver
Explore two mesh options:
  explicitly meshing the gap
  without meshing the gap
Fuel
Gap
Cladding
0.5 cm
0.005 cm
0.1 cm
1 cm

## Slide 5: Last Time
Defined strain as a matrix of deformations
Tensile test stress/strain curves
  Youngs modulus, yield strength, ultimate tensile strength, fracture strength
Matrix of elastic constants relating strains to stresses
  only two unique constants for isotropic materials
Strain hardening
  permanent deformation, leading to increased yield strength
  dislocation pileup, increase in number of barriers
We developed analytical solutions for the stress in a pressurized cylinder with a thin wall

## Slide 6: Develop constitutive relations for thick-walled
We assume small strains, so the strain is defined with respect to displacement: u
We assume isotropic material response:

## Slide 7: Stress within a pressurized cylinder that has thick walls (radius/thickness<20)
The cylinder as an inner radius Ri and an outer Radius Ro
We assume there is no shear stress, so σrz = 0
We will begin with the r equation
Now we need our constitutive law
We combine these equations to get

## Slide 8: Develop equations for the stress within a pressurized cylinder with thick walls
We need one more relationship from the definition of the strain
From the previous slide, we have
If we combine these, we get
Again, from the previous slide
We end up with

## Slide 9: We now have an ODE so we can solve to get the stress
Our boundary conditions are σrr(Ri) = -p and σrr(Ro) = 0
After integrating twice, we get
From σrr, we can get σθθ from
From the end condition, we determine σzz
(a)
(b)
(c)

## Slide 10: Determine if a fuel rod will exceed its yield stress
A fuel rod has an initial pressure of 5 MPa that increases to 9 MPa during operation. Will it exceed its yield stress?
  Ri = 0.52, Ro = 0.58 cm, σy = 381 MPa
Which stress is the largest?
  σθθ
At what position r will the hoop stress be the largest?
  r = Ri = 0.52 cm
What is the stress at p = 5 MPa?
  σθθ = 5*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 46.0 MPa
What is the stress at p = 9 Mpa?
  σθθ = 9*((0.58/0.52)^2 + 1)/((0.58/0.52)^2 – 1) = 82.7 Mpa
Again, we don’t even get close to yielding

## Slide 11: We’ve now solved this same problem assuming thin and thick-walled cylinders

## Slide 12: THERMO-Mechanics

## Slide 13: Thermal Expansion
As the temperature increases, atoms have larger vibrations, causing the material to expand
This expansion doesn’t raise the energy of the material when unrestrained
This expansion can be treated as a strain, but as one that doesn’t cause stress

## Slide 14: Thermal Expansion
In isotropic materials, thermal expansion happens equally in all directions and is linear with temperature
In this equation
  T is the current temperature
  T0 is the temperature the original size was measured
  α is the linear thermal expansion coefficient
  I is the identity tensor

## Slide 15: Thermal Expansion
Though thermal expansion doesn’t directly cause stress, it can still lead to thermal stress

## Slide 16: What is the stress in a thin constrained rod of length L when it is heated to ΔT?
The rod has a Young’s modulus of E and an expansion coefficient of α

## Slide 17: The large temperature gradient within a fuel pellet results in large thermal stresses

## Slide 18: Consider the constitutive relations plus T
We assume small strains, so the strain is defined as
We assume isotropic material response, so

## Slide 19: Consider a cylinder with thermal expansion but not pressure
Similar to the equations we worked through before
Solving this ODE:

## Slide 20: What is the hoop stress in the cladding?

## Slide 21: Where is hoop stress equal to zero?

## Slide 22: The linear temperature gradient across the cladding causes axial thermal stresses

## Slide 23: Same approach to the thermal stress in a fuel pellet
The thermal stress is due to the temperature gradient

## Slide 24: Solve this stress ODE
The boundary conditions are:
Once we solve it, we obtain
Then we can solve the hoop stress
The axial stress is more complicated to obtain, but you end up with

## Slide 25: The fuel temperature gradient causes large thermal stresses

## Slide 26: Example

## Slide 27: How far do fuel cracks extend?
E = 200 GPa, ν = 0.345, α = 11.0e-6 1/K, σfr = 130 MPa, ΔT = 550 K
Solve for η
  – σfr / σ* = 1 – 3 η2
  3 η2 = 1 + σfr / σ*
  η = ( (1 + σfr / σ*)/3 )½
σ* = 11.0e-6*200*550/(4*(1 – 0.345) ) = 461.8 MPa
η = sqrt( (1 + 130/461.8)/3 ) = 0.65

## Slide 28: thermal expansion

## Slide 29: The gap changes as a function of time
Both the pellet and the cladding swell
But, as the gap decreases, the temperature changes, which again makes the gap change
The solution using the analytical equations is iterative, due to the dependence of the gap size and temperature

## Slide 30: Example

## Slide 31: This calculation is repeated until the gap width stops changing significantly
The change in the gap does NOT affect the coolant or outer cladding temperatures, just the gap and fuel temperatures
Does fuel centerline temp go up or down with correction?
Iteration | δgap (cm) | Ts (K) | T0 (K)
0 | 0.003 | 701 | 1232
1 | 0.00066 | 644 | 1174
2 | 0.00097 | 652 | 1182
3 | 0.00094 | 651 | 1181
4 | 0.00094 | 651 | 1181