## Slide 1: Cladding Oxidation
NE 591

## Slide 2: Last time
Growth and creep are the major mechanisms for dimensional instability in zirconium alloy cladding
Growth results from the clustering of interstitials on prismatic planes
Creep occurs in three stages: (1)creep down from water pressure; (2)creep out from fuel column; (3)fuel column axial stress
Under irradiation, zirconium experiences irradiation induced hardening due to interstitial loops on the prismatic planes
Channels form that don’t have loops, resulting in localized deformation
Other phenomena:
  Fatigue; SCC; PCMI; PCCI

## Slide 3: Zirconium Oxidation
Corrosion of zirconium is one of the largest concerns for LWR fuel operation
Zirconium interacts with water to make zirconia and hydrogen
Both the oxide layer and the hydrogen adversely impact cladding performance
Zr metal
ZrO2

## Slide 4: Corrosion
Corrosion is the degradation of a material and its properties under the action of the surrounding environment by chemical and/or electrochemical reaction
Corrosion reactions require the following:
  Oxidant
  Electric current
A corrosion reaction is composed of an oxidation reaction and a reduction reaction
During corrosion at a particular spot on the surface of the object made of iron, oxidation takes place and that spot behaves as an anode
The electrons released at this anodic spot move through the metal and go to another spot on the metal and reduce oxygen at that spot in presence of H+, which behaves as a cathode

## Slide 5: Corrosion
Corrosion reaction rates are determined by thermodynamics and kinetics
Thermodynamics tell us whether a material may corrode
  Measure voltage difference between anodic and cathodic sites
Kinetics tell us how quickly a material will corrode
  Measure net current between anodic and cathodic sites

## Slide 6: Formation of Oxide Layer After Oxide Formation
Oxidation reaction:
Reduction reaction:
H20
Zr
H20
Zr
ZrO2
O-2
e-
Dissociation of water at oxide/water interface
Absorption of oxygen into oxide layer
Diffusion of oxygen through oxide layer
Reaction of oxygen with zirconium
Diffusion of electrons through oxide layer
Reduction of hydrogen

## Slide 7: Corrosion rate limited by diffusion
Because the rate limiting steps are diffusion, we can model the oxidation rate using diffusion
Assumptions:
  Transport of O species is rate-limiting
  Transport of charged species by diffusion only
  Homogeneous oxide layer
  No sources/sinks of ions in oxide
  All oxygen is used to create oxide
  No loss of oxide

## Slide 8: Observed kinetics are slower than parabolic
Parabolic kinetics
  Diffusion of species across the oxide
Sub-parabolic kinetics
  Development of cracks in oxide
  Additional ions in oxide
  Non-uniform electric field in oxide layer
Once a nonhomogeneous electric field arises, the corrosion rate decreases to the sub-parabolic rate due to inhibition of transport of charged species.

## Slide 9: Corrosion
Corrosion is measured by sample weight gain
Oxidation of alloys is measured experimentally using the weight gain in mg/dm2
Oxide forms by incorporating oxygen in the metal structure causing an increase in weight
Dividing by the surface enables comparison between samples
Approximation weight gain – oxide thickness for Zr:

## Slide 10: Pilling-Bedworth ratio : PBR
The ratio of oxide thickness to metal thickness is called the Pilling-Bedworth ratio (PBR)
PBR < 1: the oxide coating layer is too thin, likely broken and provides no protective effect (for example magnesium)
PBR > 2: the oxide coating chips off and provides no protective effect (example iron)
1 < PBR < 2: the oxide coating is passivating and provides a protecting effect against further surface oxidation
Zr metal
ZrO2

## Slide 11: Example
A corrosion coupon of ZIRLO measures 2.8 cm x 2.8 cm x 600 µm and has an initial mass of 3 g. After corrosion for 200 days, its final mass is 3.0721 g. What is the estimated oxide thickness?
First, we need to convert the units
  S = 0.28*0.28 dm2
  dM = 300 mg – 307.21 mg
Then we calculate the weight gain per area
  W = dM/S = (307.21-300)/0.28^2 = 91.96 mg/dm2
Last estimate the thickness
  d = W/14.7 = 91.96/14.7 = 6.3 microns thick after 200 days

## Slide 12: Corrosion Rate
Average weight gain of a sample follows linear kinetics
The oxide reaches transition at different times in different points, but the average is linear
Critical oxide thickness for transition is defined as
Critical time for transition is defined as
After transition, oxide thickness is

## Slide 13: Example
Estimate the oxide thickness on a ZIRLO sample at 650 K after 200 days exposed to water.
First, we have to determine if the oxide has gone through transition
  t* = 6.62e-7*exp(11949/650 k) = 63.76 days
  So, the sample is past transition, so we need to use the linear fit
Next, we calculate the oxide thickness at transition
  δ* = 5.1*exp(-550/650) = 2.19 microns
Now, we can compute the final oxide thickness
  KL = 7.48e6*exp(-12500/650) = 0.0333
  δ = 2.19 + 0.0333*(200 – 63.76) = 6.73 microns

## Slide 14: Other factors affecting corrosion
Irradiation: Production of radicals through radiolysis; Radiation damage to the metal; Radiation damage to oxide
Water chemistry: Coolant additions are added to control neutronics, corrosion, and hydrogen pick-up
Temperature:
  Corrosion rate increases
  with temperature

## Slide 15: Impact of Corrosion
The oxide layer has a low thermal conductivity, restricting heat transport
  For Zircaloy, k = 22 W/(mK)
  For ZrO2, k = 1.7 – 2.7 W/(mK)
The oxide layer is much more brittle than the zircaloy
  Zircaloy metal is removed as brittle oxide is added to the material
Oxidation produces hydrogen that can enter the cladding and form brittle hydrides

## Slide 16: Corrosion Summary
Corrosion is the environmental degradation of materials
Cladding oxidizes, forming ZrO2
The limiting step for oxidation is the oxygen transport through the oxide layer
  It begins being controlled by diffusion
  Then, a protective layer forms that slows oxidation
  Once transition occurs, it loses its protectiveness and speeds up again
Oxidation hurts cladding performance by
  Restricting heat transport
  Converting zircaloy into a brittle oxide

## Slide 17: Hydride Formation
Corrosion of zirconium so damaging in large part due to hydride formation
Some of the hydrogen atoms produced by oxidation enter the cladding and form a hydride phase
The fraction of the produced hydrogen that enters the cladding is defined by the pickup fraction:
Hydrogen is produced twice as fast as oxygen
  JH = 2 f JO
Corrosion reaction:
Hydrogen pick-up
Zr metal
ZrO2

## Slide 18: Given a thickness of oxide, how can we predict the hydrogen pickup?
A cladding with an initial thickness of 600 microns that initially has 40 wt. ppm H undergoes corrosion to a total oxide thickness of 80 microns. What is the overall hydrogen content in wt. ppm if the hydrogen pickup fraction is 15%?
First, we must determine the weight of H that has entered the cladding
  δZrO2 is 5.68 g/cm3, of which 32/(91+32)= 0.26 = 26% is O, thus 1.47 g/cm3 of O
  A 1 micron oxide layer corresponds to a weight gain of 14.7 mg/dm2 (see previous lecture), and thus with an 80 micron layer, weight gain = 14.7*80 = 1176 mg/dm2
  This mass corresponds to 1.176 NA/16 atoms of oxygen = 4.42 x 1022 atoms/dm2
  f = 15%, so the ingress of hydrogen will be 0.15*2*4.42e22 = 1.33e22 atoms of hydrogen/dm2, or 0.022 g of H.
Now, we determine the fraction in wt. ppm in a 10 cm square cross section w/ PBR = 1.56
  The uncorroded thickness is 600 – 80/PBR = 600 – 80/1.56=549 microns
  The volume of zirconium is 549 x 10-4 (cm)*10*10 =5.49 cm3
  rZr = 6.5 g/cm3, so the total mass of Zr is 6.5*5.49 =35.7 g.
Thus the hydrogen concentration is 0.022/35.7 =6.18e-4= 618 wt. ppm, which, added to the original 40 wt. ppm, is 658 wt. ppm

## Slide 19: We can estimate the hydrogen content in the cladding from the oxide thickness δ and the pickup fraction f

## Slide 20: Hydrogen Diffusion
The diffusion coefficient of H in Zr is
The characteristic time required for hydrogen to diffuse through the entire cladding is
What is the characteristic time for cladding at 355 C (average cladding temperature) that is 0.06 cm thick?
  DHZr = 7x10-3*exp(-0.47/( kB*(355+273.15))) = 1.19e-6 cm2/s,
  t = 0.06^2/(4*1.19e-6) cm2/s =756.3 s =12 min,
  So, the hydrogen atoms have plenty of time to move through the entire clad

## Slide 21: Hydriding
Hydride concentrations are not uniform, because they respond to temperature and stress gradients
Hydrogen tends to move toward lower temperature (Soret effect)
It also moves to areas with tensile stress
Hydrogen has a low solubility in zirconium, so even small hydrogen concentrations result in hydrides

## Slide 22: Effect of Hydrides
The hydride rim is caused by the Soret effect and the temperature dependence of the solubility
The hydride rim and blisters can cause a loss of ductility, leading to earlier failure
Hydride rims are layers of uniform depth, that can reach 50–60 microns, and cover a wide area on the tube azimuthal and axial directions
Blisters have an elliptic shape, are more localized on the tube external surface and are deeper, usually covering half of the cladding thickness.

## Slide 23: Blister failure examples
23
40 μm Blister Broken at 25 °C
M014
53 μm Blister Broken at 300 °C M025
93 μm Blister Broken at 25 °C
M020
83 μm Blister Broken at 300 °C M023
90 degree failure at RT
But in small blisters => shear instability
At 300 C, 45 degree shear

## Slide 24: Circumferential vs Radial Hydrides
Under reactor conditions, hydride platelets precipitate circumferentially
In used fuel after drying, the hydrides can reprecipitate with a radial orientation
The hydrides reform in a radial direction due to the tensile hoop stress
Radial hydrides provide easy crack paths and significantly decrease the ductility of the cladding

## Slide 25: Hydrides Summary
Hydrogen released by oxidation enters the cladding
It quickly diffuses throughout the cladding, but prefers low temperature
Due to low solubility (that is a function of temperature), hydrides form
Hydrides are brittle, and so reduce the ductility of the cladding
Radial hydrides can form in used fuel after drying, and reduce the ductility much more than circumferential hydrides