## Slide 1: NE 763: Advanced Reactor Materials
Fall 2026
Dr. Benjamin Beeler

## Slide 2: Last Time
Metallic fuel performance modeling
  needs to fully encompass mechanical behavior, chemical interactions, fission gas behavior, and temperature profile
  Porosity models inform temperature profiles which inform redistribution/phases (cycle)
  Validate against limited data: cladding strain, gas release, cladding T
Metal fuel fabrication/reprocessing
  historically via injection casting
  pyroprocessing with molten salts, depositing U/MA/TRU on cathodes
  can refabricate via injection casting for closure of fuel cycle

## Slide 3: Last Time
MOX fuels
  higher powers and higher temperatures
  similar geometry to metallic fuels, but with higher smear density, pellet fuel
MOX restructuring
  high T and steep T gradient lead to four distinct zones in MOX fuel
  central void, columnar grains, large equiaxed grains, as-fab microstructure
  void+columnar grains result of pore migration up the T gradient

## Slide 4: Redistribution of Pu
The movement of pores leads to a redistribution of plutonium, resulting in a spike in Pu concentration surrounding the central void
Similar behavior has been observed for americium
This transuranic concentration increase is accompanied with a decrease in U concentration
This redistribution increases the local fission rate and centerline temperature, while generating lower melting point phases

## Slide 5: Redistribution of Pu
This phenomenon is currently understood as an evaporation-condensation process
The fuel at the edge of the pore closest to the centerline becomes gaseous inside the pore and deposits itself on the cooler region of the pore closest to the cladding
UO2 is the more volatile of the U/Pu heavy metal species present in the fuel matrix
The high oxygen potential can lead to a high partial pressure of UO3 within the self-contained pores
Enriched regions of PuO2 are left behind and deposited at the leading edge of the central void as the porosity accumulates in the fuel center
Some experiments on O/M ratio seems to point towards higher O potential leading to more redistribution
While this is the working theory, it is not clear if this explanation can also account for the necessary pore velocities
No experimentally proven substitution has been put forth as a replacement theory to the observed features

## Slide 6: Pu-rich Agglomerates
Regions of high Pu concentration can also form in the MOX fuel matrix due to incomplete mixing during fabrication
Clusters of dispersed porosity form in high Pu concentration regions because of the high fission rate
Thermal conductivity of the spots is also lower than the surrounding matrix, thus the PAs are both hotter and undergo a greater number of fission events in a very small region
Burnup in these regions may be 2-3 times greater than that of the pellet as a whole
The morphology of porosity in the agglomerates depends on the temperature, with smaller bubbles in cold regions and large bubbles in hot regions
Porosity formed due to PAs are visually distinct from fission gas bubbles or pre-existing porosity

## Slide 7: Pu-rich Agglomerates
The presence of the high burnup structure (HBS) has been observed within the PA regions
The HBS is basically a fine grained, cauliflower-like structure
In MOX fuels, the HBS structure appears in fuels following burnups between 60 and 80 GWd/tM at temperatures below approximately 1100C
PA's reach these local burnups at pellet burnups far below this threshold

## Slide 8: Oxygen Redistribution
The as-fabricated oxide pellets used as fuel in fast reactors are always hypostoichiometric with an initial O/M typically in the range 1.93–2.00
Oxygen is redistributed radially, migrating down the thermal gradient, thus bringing the composition close to stoichiometry near the periphery, whereas the O/M ratio becomes very low in the hottest area
Oxygen transport is likely a combination of vapor and solid diffusion

## Slide 9: O/M Ratio
Fission releases two oxygen atoms, which cannot be fully bound by the fission products, this increases the O potential in the fuel as dissolved O
The O potential increases until the point where Mo starts to oxidize, leaving the metallic inclusions
The O/M ratio increases until Mo starts to oxidize, then maintains at approximately 2.0 or thereabouts
Ratio of Mo/Ru in metal precipitates
Oxygen potential vs T at different burnups

## Slide 10: Solid Fission Products
Fission products in oxide fuels can be grouped into 4/5 categories
Fission gases and volatile species
Metallic precipitates
Oxide precipitates
Soluble oxides
LWR fuel vs Pu-containing MOX fuel, we see a higher concentration Ru, Rh, Pd, and a lower concentration of Zr and Mo
Target higher burnups, so we have a very high inventory of fission products

## Slide 11: Metallic Inclusions
Mo, Tc, Ru, Rh, and Pd form prominent phases in irradiated nuclear fuels commonly referred to as “white inclusions,” “noble metal,” or “five-metal” precipitates
The particles exist as a solid solution taking on the hexagonal close packed (hcp) structure
The particle size, frequency, and composition exist over a wide range, depending on the burnup and position found within the pellet

## Slide 12: Metallic Inclusions
In the columnar grain region of the fuel, the particles are commonly 5-10 mm in diameter, collecting primarily on the grain boundaries
Particles tend to be much smaller (2 mm and below) in the equiaxed and as-sintered regions, but occur more frequently intragranularly
The particles form as a result of fission product phase agglomeration, as opposed to nucleation and growth process
Columnar Grain Region
Equiaxed Grain Region

## Slide 13: Oxide Phases
Oxides containing Sr, Zr, or the rare earth (RE) elements form solid solutions with either UO2, PuO2, or both at low concentrations
Barium is only soluble to 1.6 at% in MOX fuels and thus precipitates a separate oxide phase at higher concentrations
The separate oxide phase, commonly referred to as the “grey phase,” form ABO3 perovskite structures, in which A=(Ba1-x-y, Srx, Csy, x,y ≪1) and B=(U, Pu, Zr, Mo, RE)
The particles are primarily Ba rich, followed by Zr, U, Pu, Mo, Sr, and trace amounts of the remaining products
Due to the sheer number of constituents, the structures are largely unknown
Grey phase is typically found in the equiaxed or outermost regions of the columnar grains commonly intermixed with other constituent oxides

## Slide 14: Joint Oxyde Gaine
The volatiles class of fission products produced during reactor operation are of particular interest to fuel-cladding interactions
Cs, Te, and I all evaporate at low operating temperatures and migrate to the coolest part of the fuel where they react with fuel or cladding constituents
Mo has a tendency to combine with Cs and O to become volatile and migrate toward cooler fuel regions
This has been termed Joint Oxyde Gaine (JOG)
JOG is an oxide buildup formed on the fuel surface between the pellet and cladding
After gap closure, there remains a minimal residual gap
Primarily Cs2MoO4 or Cs2(U, Pu)O4, the JOG structure is irregular and dense, found in regions where the peak fuel temperature is lowest

## Slide 15: Joint Oxide Gain
The volatile constituents of the JOG structure evaporate from the fuel pellet at high temperatures and condense to become solid at the cooler top or bottom of the fuel
It is believed that the existence of JOG aids in thermal transport of the fuel, as the oxide structures have higher thermal conductivity than a fuel-cladding gap filled with fission gases

## Slide 16: Joint Oxide Gain
JOG acts as a mechanical buffer, limiting the amount of PCMI, or stresses in the cladding
JOG reduces fuel swelling, by allowing fission products to leave the fuel into a preferable chemical state
Fission products in the JOG play a predominant role on FCCI and on the resulting strong cladding corrosion

## Slide 17: MOX FCCI
While T is too low in LWRs with MOX to initiate FCCI, in SFRs with MOX, the cladding inner surface temperature can reach sufficiently high temperatures under normal operating conditions to initiate detrimental oxidation and chemical attack
FCCI manifests itself in three primary modes: matrix attack, intergranular attack, or combined, which demonstrates the properties of both matrix and intergranular attack
Matrix FCCI attack corresponds to the localized oxidation of the cladding material, with primarily oxidation of the Cr in the stainless steel

## Slide 18: MOX FCCI
Intergranular attack modes occur due to the depletion of Cr in grain boundaries due to the formation of Cr23C6 carbides allowing penetration of corrosive species
Oxygen and volatile fission products (Cs, Te, I, etc.) are the primary culprits of FCCI initiation in oxide fuel systems
In MOX fuels, the oxygen potential of the system is the greatest difference from LWR UO2
The preferential formation of noble metals rather than oxide formers leads to an excess of available oxygen in the system

## Slide 19: MOX FCCI
Under normal operation, stainless steel cladding forms a chromia (Cr2O3) layer that acts to protect the cladding from corrosion
Cs is generally unreactive with stainless steel claddings, but reacts with the protective oxide layer to create Cs-chromates (Cs2CrO4 or Cs2Cr2O7) when excess oxygen is present
The decay of the protective oxide layer causes deeper penetration of the FCCI into the cladding
Iodine is primarily bound to Cs in the form of CsI, and can lead to an enhancement in oxidation in hyperstoichiometric fuels
Tellurium is highly active when combined with Cs to create Cs2Te, which can dissolve cladding constituents in the presence of high oxygen potential
The O/M ratio of the fuel before and during irradiation are significant factors, and FCCI can potentially be limited by operating with a hypostoichiometric initial fuel composition

## Slide 20: MOX Summary
Phenomena of interest: Restructuring, O and Pu redistribution, Pu agglomerates, fission product chemistries, JOG formation, and FCCI
O/M ratio is one of the most significant factors in determining the nature of actinide redistribution, fission product precipitate chemistries, and FCCI formation
The effects of fission product precipitates and Pu agglomerates on fuel thermal behavior is highly localized with little discernible influence on the overall fuel burnup behavior

## Slide 21: Sodium coolant

## Slide 22: Liquid Metal Coolants
Liquid metals (LM), such as sodium (Na), lead (Pb), and lead–bismuth (Pb–Bi) eutectic, are considered as potential coolants for the fast spectrum nuclear reactors of the next generation
The main advantages of Na coolant in comparison with Pb are the lower melting temperature, density, and dynamic viscosity and the higher thermal and electrical conductivities

## Slide 23: Sodium
Sodium is a solid at room temperature; melting point is 98 C; boiling point is 881 C
Therefore, sodium is in the liquid phase at FR operating temperatures without pressurization
For this reason, it is not necessary to adopt the pressurized design employed in light water reactors for SFRs (SFRs operate near atmospheric pressure)
Sodium is a great heat transfer medium due to high thermal conductivity, high heat capacity, and large liquid range
Allows for high power density core and low coolant fraction
Na has insignificant neutron moderation, making it suitable for the coolant for the FBR
The weakness of sodium as a coolant is its reactivity with oxygen and/or water

## Slide 24: Structural Material Selection for Na
It is necessary to take the environment into consideration by estimating the mechanical properties and thermal characteristics
Environments specific to the SFR components include: (a) contact with the coolant, (b) high temperature at which the creep effects must be taken into account, and (c) neutron irradiation
The dissolution of elements contained in the material, such as iron, chromium, and nickel, in sodium and the reverse phenomenon (deposition) occur on the material surface due to the difference in chemical potential
The behavior is fundamentally controlled by the solubility of the material elements in sodium and by the diffusion rate of the materials

## Slide 25: Structural Materials in SFRs
Austenitic and ferritic/martensitic steels are two key alloy classes for SFR structural materials
Most research has been done on SS-304 and SS-316, but advanced alloy behavior (HT9, T91, ODS steels, etc.) is being studied

## Slide 26: Solubilities and Compatibility
Among the elements in austenitic stainless steel, the solubility of nickel is greatest
Therefore, the phase transformation of austenite to ferrite through nickel dissolution is observed on the surface in long-term immersion in sodium
Solubility can be greatly impacted by impurities

## Slide 27: Sodium Corrosion
There are two known mechanisms of sodium corrosion
  Type I: corrosion produced by the dissolution of alloy elements to sodium
  Type II: corrosion produced through chemical reaction with the impurities in sodium
Type I corrosion is dependent on the solubility in sodium of the elemental composition in the material, temperature, and the rate of solution
K is the solution rate constant, Cs is the solubility limit in sodium, and Ci is the actual concentration in sodium