## Slide 1: NE 763: Advanced Reactor Materials
Advanced Cladding: Supplement
Dr. Benjamin Beeler
Notes: Supplement to Lectures 18-20. Three insert blocks: (1) one slide on fabrication and joining, to follow the ODS material in Lec 19; (2) an 11-slide block on radiation-resistant austenitic steels, which fits between the 'need for advanced cladding' slides and F/M steels in Lec 18, or as its own lecture; (3) two slides on CALPHAD and machine-learning design of HEAs for the HEA material in Lec 19-20. Numbered sources are on the final three slides.

## Slide 2: Fabrication and Joining
ODS tube fabrication
  Milled powder (+Y₂O₃, TiH₂) → hot extrusion (~1100 °C) → cold pilgering with ~1200 °C intermediate anneals
  Ferritic ODS: grains elongate along the rolling direction with ⟨110⟩ texture → anisotropic properties; one Fe-14Cr tube resisted recrystallization even at 1350 °C
  9Cr martensitic ODS can reset its grain structure through the α↔γ transformation
Joining
  Fusion welding agglomerates the yttria and adds porosity and coarse grains → weak weld zone
  Solid-state methods instead: pressure resistance welding (PRW), resistance upset welding
  PRW MA957/HT-9 joints: ~90° bends, no burst at RT or 400 °C; joints failed at ≥575 °C
  Upset welds (9Cr, 14Cr ODS): dynamic recrystallization; oxide size and fraction change only slightly
Additive manufacturing
  L-PBF cools at 10⁴–10⁷ K/s vs. 10²–10⁴ K/s for DED → less time for oxides to coarsen
  Slower cooling agglomerates oxides; routes include GARS powder and in situ oxide formation
Sources: [1] tube route; [2] PRW; [3] upset welding; [4], [5] additive manufacturing
Notes: Point: the properties in the ODS lecture exist only if fabrication preserves the nanoscale oxides. Tube route and texture: Salliot et al. 2024 (CEA Fe-14Cr ODS; the 1350 C no-recrystallization result is from that one study, not a general rule). For 9Cr martensitic ODS, the alpha-gamma phase transformation offers a way to reset the elongated grains. Joining: fusion welding causes flocculation and agglomeration of the yttria, so end-plug closures use solid-state methods. INL PRW work (Jerred et al. 2010) joined MA957 to HT-9 and noted failures at 575 C and above. Upset welding (Doyen et al. 2019): dynamic recrystallization changes grain morphology, but precipitates change little. AM: cooling rates quoted from a 2025 review; L-PBF is the most promising because of faster cooling.

## Slide 3: Radiation-resistant austenitics
Notes: Positioning: Lec 18 opened with why 304/316 fail (void swelling). This block covers the other response: fixing the austenitics instead of replacing them with F/M steels.

## Slide 4: Why Revisit Austenitic Steels?
Advantages
  FCC: no ductile-to-brittle transition
  Good creep strength at cladding temperatures (up to ~650 °C)
  Large fuel-pin database: EBR-II, FFTF, Phénix, BN-600, FBTR
  Still selected: Alloy D9 clads India's 500 MWe PFBR
Limitations
  Void swelling after an incubation dose, then ~1%/dpa
  Swelling-driven dimensional change caps burnup
  Ni transmutation → He at grain boundaries at high T
  Radiation-induced phase instability erodes the alloy design
Key question: how far can composition and processing push the swelling incubation dose?
Sources: [6]–[11]
Notes: Cladding temperatures up to ~650 C: Griffiths 2021 review. Reactor experience: FFTF/EBR-II (316, D9), Phénix (15-15Ti), BN-600 (ChS-68 and predecessors), FBTR (D9 test subassembly for PFBR). The limits column previews the rest of the block.

## Slide 5: Ti-Modified 15Cr–15Ni Steels
Common recipe: more Ni than 316, Ti additions (with B, P or Si in some grades), and ~20% cold work
Alloy | Program | What stands out
Type 316 (CW) | US: FFTF, EBR-II | Baseline; swelling became the burnup limit
D9 | US | Ti-modified 316; swelled less than 316 in FFTF
D9I | India | Improved D9 for PFBR clad and wrapper
DIN 1.4970 | Germany | Ti-stabilized; TiC dispersions tested against He embrittlement
15-15Ti | France | Phénix cladding 1982–1998, up to 130 dpa
ChS-68 | Russia | BN-600 cladding, 20% CW; successor to EI-847
JPCA | Japan | Japanese member of the same Ti-modified class
Sources: [8] alloy family; [9] ChS-68; [10] D9 in FBTR; [11] FFTF; [17] DIN 1.4970
Notes: Liu et al. (2024) list ChS-68, D9, D9I, DIN 1.4970 and JPCA as alloys similar to 15-15Ti. Exact compositions differ by program; I have not put a composition table here because I did not verify each grade's specification. Add from your own references if you want one.

## Slide 6: Swelling Kinetics
Transient (incubation), then steady state near 1%/dpa
  Steady ~1%/dpa seen above ~425 °C; not observed below 380 °C
Steady-state rate is hard to change
  15-15Ti still reaches ~1%/dpa at 400 dpa (ions, 580 °C)
So alloy design targets the incubation dose, not the slope
Dose and dose rate can't be fully separated
  Lower rates can swell more at the same dose
Sources: [6] incubation and 1%/dpa; [8] 15-15Ti to 400 dpa; [16] dose rate. Figure is schematic.
Notes: The figure is a schematic, not data. Chung (NUREG/CR-6897, 2006) gives the 1%/dpa rule of thumb, observed above about 425 C, with no evidence of it below 380 C. Liu et al. (2024) ion-irradiated 20% CW 15-15Ti at 580 C to 400 dpa; the steady-state rate stayed near 1%/dpa. Dose-rate nuance: Chung says dose and dose-rate effects cannot be separated. Allen et al. (1999) found no statistically significant effect for 2-3x dose-rate differences in 12% CW 316, though the lower-rate samples swelled somewhat more. So present the dose-rate effect as real but debated in magnitude.

## Slide 7: Cold Work
Cold work introduces a high dislocation density that absorbs point defects
  Delays void nucleation → extends the incubation period
~20% cold work is the standard condition for 15-15Ti and ChS-68 cladding
  Also raises strength
Limitation
  Under irradiation the network evolves toward a dose-dependent steady state and recovers at high temperature
  Cold work delays swelling; it does not prevent it
Cold work buys dose, not immunity.
Sources: [6] cold work extends incubation; [8], [9] 20% CW practice
Notes: The 'Limit' card summarizes the widely reported evolution of the dislocation network toward a steady state under irradiation. It is textbook material rather than something tied to one reference here; cite your preferred review (for example Garner's) if students ask.

## Slide 8: Composition Effects
Element | Effect on swelling
Ni | Swelling minimum near 30–50% Ni in Fe-15Cr-Ni (~100 dpa); but more Ni means more He [7]
Si | Suppresses swelling with little effect on other properties [7]
P | Non-monotonic: below ~0.02 wt% often increases swelling; higher levels reduce it [12]
Ti | Forms stable precipitates that trap point defects, extending incubation [13]
B | Possible contributor to ChS-68's extra ~10 dpa transient over EI-847 [9]
Catch: Ni and Si only help while they stay in solution. Irradiation pulls them out of the matrix (next slides).
Sources: [7], [9], [12], [13]
Notes: Ni: Griffiths (2021) shows the swelling minimum in the 30-50% Ni range for Fe-15Cr-Ni ternaries near 100 dpa, depending on temperature; this is why cladding steels raise Ni above 316 levels. Phosphorus: Garner and Mitchell (1992) is a good example of a non-monotonic solute effect. Boron in ChS-68: Porollo et al. (2009) say boron 'potentially' contributes, so present it as a hypothesis.

## Slide 9: Ti Carbide Precipitates
Fine intragranular TiC adds sink surface for point defects
  Longer incubation
Traps He in the matrix
  Dispersed TiC suppressed He embrittlement in DIN 1.4970
  Benefit depended on the right thermomechanical pre-treatment
HT-UPS scales up the idea
  Ti + Nb + V with B and P for stable nanoscale MC carbides
Same strategy as ODS steels
  ODS: stable Y–Ti–O nanoclusters in a ferritic matrix
  Here: stable MC carbides in an austenitic matrix
  Both work only while the nanofeatures stay fine under irradiation
Sources: [8] TiC in 15-15Ti; [13] Ti and incubation; [17] TiC vs. He; [18] HT-UPS
Notes: Kesternich, Matta and Rothaut (1984): after suitable pre-treatment, DIN 1.4970 with dispersed TiC outperformed 316 in strength, ductility and resistance to He embrittlement in He-implanted creep tests. The ODS link is a teaching bridge: the same 'stable nanoscale feature' principle works across matrices.

## Slide 10: Radiation-Induced Phase Instability
Temperature window: in BN-600, ChS-68's peak swelling (430–460 °C) was where G-phase dominated (~0.5 vol% at 84 dpa)
The compositional levers from the previous slides erode with dose
Nuance: segregation to void surfaces has been correlated with reduced void swelling, so RIS is not only harmful
1. RIS
Ni and Si enrich at sinks; Cr depletes
2. Precipitation
γ′ (Ni₃Si), G-phase and M₂₃(C,Si)₆ form
3. Depletion
Matrix loses the Ni and Si that resisted swelling
4. Swelling
ChS-68: onset coincided with G-phase formation
Sources: [9] ChS-68 and G-phase; [14] RIS; [15] γ′ and M₂₃(C,Si)₆
Notes: RIS in Fe-Cr-Ni: Cr depletes and Ni enriches at grain boundaries, more so as bulk Ni rises (Allen, Cole, Was, Kenik 2002). Si, an undersized solute, also enriches at sinks. The 1978 J. Nucl. Mater. paper's title states the link: swelling as a consequence of gamma-prime and M23(C,Si)6 formation in 316. Porollo, Konobeev and Garner (2009) found swelling onset coincided with G-phase formation in ChS-68. They attributed ChS-68's advantage over EI-847 mainly to more stable faulted loops, possibly helped by boron.

## Slide 11: In-Reactor Performance
Alloy | Where | Dose | Result
316 vs. D9 | FFTF (US) | — | D9 swelled less than 316 in fuel pins
D9 | FBTR (India) | 40–62 dpa | Beat 316; supports PFBR target of 85 dpa
15-15Ti | Phénix, 1982–98 | ≤130 dpa | Deformation still acceptable
ChS-68, 20% CW | BN-600 (Russia) | 56–84 dpa | ~10 dpa longer transient than EI-847
15-15Ti | Ions, 580 °C | to 400 dpa | Steady swelling stays ~1%/dpa
Future SFR assemblies may reach 200 dpa, beyond the austenitic record. That is one reason F/M and ODS steels are favored for high-burnup cores.
Sources: [8] Phénix, ions, 200 dpa goal; [9] BN-600; [10] FBTR; [11] FFTF
Notes: FFTF (1986 conference paper): 316 swelling was temperature-independent above about 490 C, and D9 outperformed 316 on swelling. FBTR (Karthik et al. 2022): D9 test subassembly with 37 MOX pins, 112 GWd/t peak burnup, 40-62 dpa. PFBR's initial target is 100 GWd/t, about 85 dpa. Ion data (Liu et al. 2024) are not a substitute for neutron data but show that the steady-state rate does not drop at very high dose.

## Slide 12: Helium Effects
Ni helps against swelling but produces He
  Ni-rich alloys generate He by transmutation, most strongly in thermal or mixed spectra (see Ni alloys)
Effects
  He promotes void swelling at high temperature
  He bubbles on grain boundaries reduce creep ductility
Mitigation
  Dispersed TiC holds He in the matrix; it suppressed He embrittlement in DIN 1.4970 creep tests
Design tension: the Ni lever for swelling has a helium cost
Sources: [7] He and swelling; [17] TiC and He embrittlement
Notes: This connects the Ni-alloy slides in Lec 20 (Ni transmutation, He generation) to the austenitic cladding story: the Ni lever from the composition slide has a helium cost. Griffiths (2021) notes that He promotes void swelling at high temperature and forms dense bubble populations at low temperature.

## Slide 13: Next-Generation Austenitics
HT-UPS (ORNL): precipitate design
  Ti + Nb + V with B and P → stable nanoscale MC carbides; from 1970s–80s breeder and fusion programs
  Creep resistance comparable to Alloy 617 (R&D 100 award, 1990)
Alloy 709: SFR structures, not cladding
  Fe–20Cr–25Ni–1.5Mo with Nb and N; RT yield/UTS 270/640 MPa vs. 205/515 MPa for 316H
  ASME Section III, Division 5 design data for 100,000 h completed in 2024
Alumina-forming austenitic (AFA) steels: Pb and LBE coolants
  Al forms a protective Al₂O₃ scale (ORNL, 2006)
  In liquid Pb at 550 °C, 316L and 15-15Ti struggled to form protective oxides; low-Ni AFA resisted, high-Ni AFA dissolved
Sources: [18] HT-UPS, AFA; [19] AFA in Pb; [20] Alloy 709 properties; [21] code qualification
Notes: HT-UPS: Maziasz (2018, JOM) reviews ORNL's precipitate-engineered austenitics; HT-UPS came from fast breeder and fusion work and won an R&D 100 award in 1990. Alloy 709: composition and properties from Sham and McMurtrey (INL, 2021); the 100,000-hour Class A design data were completed in 2024, with 300,000 and 500,000-hour work ongoing (Wang et al. 2025). It is a vessel and internals material for SFRs, not cladding. AFA in Pb: Ejenstam and Szakalos (2015), one-year exposure at 550 C with very low oxygen; lowering Ni avoided dissolution attack.

## Slide 14: Austenitic vs. F/M Summary
 | Advanced austenitic (15-15Ti, D9) | Ferritic-martensitic (HT-9, T91)
Structure | FCC: no DBTT | BCC: DBTT rises under low-T irradiation
Swelling | Incubation, then ~1%/dpa | Low swelling
High-T strength | Strong creep resistance | Weaker; ODS dispersions compensate
Helium | High Ni → more He, GB embrittlement | Less Ni → less He
Service record | ≤130 dpa (15-15Ti in Phénix) | Favored for higher-dose cores
Best fit | Moderate dose, higher temperature | High dose, long residence
Sources: [7], [8]; F/M column summarizes the F/M and ODS lectures
Notes: Good exam prompt: given a coolant, peak cladding temperature and target dose, choose between a Ti-modified austenitic and an F/M or ODS steel, and justify with swelling incubation, DBTT and creep.

## Slide 15: HEA design: CALPHAD and ML
Notes: Insert after the HEA introduction in Lec 19-20.

## Slide 16: CALPHAD Screening of HEAs
Senkov et al. screened >130,000 alloy systems
  Kept only alloys whose binaries were fully assessed; >95% excluded
  Single-phase solid solutions got rarer with more elements: 16% (3 elements) → 1.2% (6)
  Configurational entropy grows as ln N; element pairs grow as N(N−1)/2, and one intermetallic-forming pair is enough
Nuclear example: low-cross-section refractory HEAs
  Screen: VEC ≤ 4.8, neutron cross-section < 2.4 b, BCC stable above 800 °C
  Result: Al₉.₅Mo₄.₇Nb₂₀.₂Ti₄.₆Zr₆₁.₀, single-phase BCC as cast, 0.77 b
  Not yet tested: ductility, oxidation, irradiation
CALPHAD predicts equilibrium. Irradiation drives segregation and precipitation away from it, the same lesson as austenitic phase instability.
Sources: [22] Senkov et al.; [23] Li et al.
Notes: Senkov, Miller, Miracle and Woodward (Nat. Commun. 2015) ran 134,547 phase-diagram calculations for 3- to 6-component systems. They kept only those where every binary had a complete database description (f_AB = 1). The fraction of single-phase solid-solution alloys fell from 16% (3-component) to 1.2% (6-component), against the original HEA entropy argument. Li et al. (Intermetallics 2026) combined a random-forest strength model with CALPHAD constraints to design Zr-rich refractory alloys with low neutron absorption. Al acted as a 'compatibilizer' suppressing the Zr-Nb miscibility gap. The authors note irradiation behavior still needs evaluation.

## Slide 17: Machine Learning for HEA Design
Phase classification
  ANN, CNN, SVM trained on 601 alloys with 13 descriptors (δ, ΔHmix, Sid, Δχ, VEC…): ~94–99% test accuracy by phase class [24]
Property model → CALPHAD
  Random forest on 392 points (74 systems), R² = 0.89 for BCC alloys; Mo and Al top strengtheners; output fed a CALPHAD screen [23]
Closed-loop active learning
  ML + DFT + thermodynamics + experiments: 17 alloys made, 2 Invar HEAs with CTE ≈ 2×10⁻⁶ K⁻¹ at 300 K [25]
Machine-learned interatomic potentials
  Cascades in MoNbTaVW: more surviving defects than W but fewer interstitial clusters, attributed to subcascade splitting [26]
Gap: training data are mostly as-cast, unirradiated alloys. Radiation-tolerance ML still depends on simulation plus targeted ion-irradiation checks.
Sources: [23]–[26]
Notes: Four roles for ML. (1) Zhou et al. 2019 (npj Comput. Mater.): classifiers for solid solution, intermetallic and amorphous phases; high accuracy, but a 601-alloy dataset is small and biased toward published alloys. (2) Li et al. 2026: ML supplies a property model that CALPHAD cannot, and CALPHAD supplies phase stability that the ML cannot. (3) Rao et al. 2022 (Science): not a nuclear alloy, but the clearest example of a closed discovery loop. (4) Liu, Byggmästar et al. 2025 (J. Nucl. Mater.): machine-learned potentials make DFT-quality cascade simulations in 5-component alloys practical. The 'Gap' statement is my synthesis for discussion, not a quote from these papers.

## Slide 18: References (1/3)
[1] F. Salliot et al. (2024) Dislocation hardening in a new manufacturing route of ferritic ODS Fe-14Cr cladding tube. Materials 17, 1146
[2] N. Jerred et al. (2010) Pressure resistance welding of high temperature metallic materials. INL report
[3] O. Doyen et al. (2019) Ferritic and martensitic ODS steel resistance upset welding of fuel claddings. J. Nucl. Mater. 518, 326
[4] Research progress on laser additive manufacturing of oxide dispersion-strengthened alloys: a review. Materials (2025)
[5] Laser powder bed fusion AM of ODS steel using gas atomized reaction synthesis powder. Materials & Design 216 (2022)
[6] H.M. Chung (2006) Assessment of void swelling in austenitic stainless steel core internals. NUREG/CR-6897
[7] M. Griffiths (2021) Effect of neutron irradiation on the mechanical properties, swelling and creep of austenitic stainless steels. Materials 14, 2622
[8] Liu et al. (2024) Cavity swelling of 15-15Ti steel at high doses by ion irradiation. Materials 17, 925
[9] S.I. Porollo, Yu.V. Konobeev, F.A. Garner (2009) Swelling and microstructure of austenitic stainless steel ChS-68 CW after high dose neutron irradiation. J. Nucl. Mater. 393, 61
Notes: Click a reference to open the source.

## Slide 19: References (2/3)
[10] V. Karthik et al. (2022) Irradiation behaviour of alloy D9 clad and wrapper in FBTR. J. Nucl. Mater. 565, 153711
[11] Swelling of 316 stainless steel and D9 cladding in FFTF (1986). Conference paper, OSTI 6047164
[12] F.A. Garner, M.A. Mitchell (1992) The complex role of phosphorus in the neutron-induced swelling of titanium-modified austenitic stainless steels. J. Nucl. Mater. 187, 223
[13] T. Yoshiie, Q. Xu (2021) Effects of alloying elements Mn, Mo, Ti, Si, P and C on the incubation period of void swelling in austenitic stainless steels. Tungsten 3, 3
[14] T.R. Allen, J.I. Cole, G.S. Was, E.A. Kenik (2002) Radiation-induced segregation and the relationship to physical properties in irradiated austenitic alloys. ANL
[15] Swelling as a consequence of gamma prime (γ′) and M₂₃(C,Si)₆ formation in neutron irradiated 316 stainless steel. J. Nucl. Mater. (1978)
[16] T.R. Allen et al. (1999) The effect of low dose rate irradiation on the swelling of 12% cold-worked 316 stainless steel. OSTI 10981
[17] W. Kesternich, M.K. Matta, J. Rothaut (1984) Influence of TiC precipitation in austenitic stainless steel on strength, ductility and helium embrittlement. J. Nucl. Mater. 122, 130
[18] P.J. Maziasz (2018) Development of creep-resistant and oxidation-resistant austenitic stainless steels for high temperature applications. JOM 70, 66
Notes: Click a reference to open the source.

## Slide 20: References (3/3)
[19] J. Ejenstam, P. Szakálos (2015) Long term corrosion resistance of alumina forming austenitic stainless steels in liquid lead. J. Nucl. Mater. 461, 164
[20] T.-L. Sham, M.D. McMurtrey (2021) Alloy 709 advanced austenitic stainless steel. INL
[21] Y. Wang et al. (2025) Code qualification of Alloy 709 for high temperature reactor applications. ORNL
[22] O.N. Senkov, J.D. Miller, D.B. Miracle, C. Woodward (2015) Accelerated exploration of multi-principal element alloys with solid solution phases. Nat. Commun. 6, 6529
[23] D. Li et al. (2026) Machine learning and Calphad guided exploration of low-neutron-cross-section refractory multi-principal element alloys. Intermetallics 198
[24] Z. Zhou et al. (2019) Machine learning guided appraisal and exploration of phase design for high entropy alloys. npj Comput. Mater. 5, 128
[25] Z. Rao et al. (2022) Machine learning–enabled high-entropy alloy discovery. Science
[26] J. Liu, J. Byggmästar et al. (2025) Utilizing a machine-learned potential to explore enhanced radiation tolerance in the MoNbTaVW high-entropy alloy. J. Nucl. Mater.
Notes: Click a reference to open the source.