## Slide 1: NE 763: Advanced Reactor Materials
Fall 2026
Dr. Benjamin Beeler

## Slide 2: Today
Space nuclear reactors, from a materials point of view
  two very different missions, two very different materials problems
Nuclear thermal propulsion (NTP)
  Rover/NERVA: core layout, fuel element evolution, coatings
  hydrogen corrosion and midband corrosion
  CERMET fuels, moderators, and the move to HALEU
Space fission power
  SNAP, SP-100, Kilopower/KRUSTY, Fission Surface Power
  hydride fuels, refractory alloys, heat pipes, alkali metal compatibility
Cross-cutting: what is actually blocking deployment

## Slide 3: Why Nuclear in Space
Propulsion
  chemical rockets are limited by the chemical energy in the propellant: ~450 s Isp for LH2/LOX
  fission decouples the energy source from the working fluid – you can heat whatever you want
  Isp ∝ √(T_chamber / M), so pick hydrogen (M = 2) and push T as high as the materials allow
  NTP design points are ~875–950 s at ~2700–2950 K chamber temperature
Surface / in-space power
  solar flux falls as 1/r² – Mars sees ~43% of Earth’s, and the outer planets are impractical
  lunar night is ~14 Earth days; batteries at the 40–100 kWe scale are not a viable mass
  fission gives continuous power independent of sun angle, dust, and latitude
  targets: 1–10 kWe (Kilopower class) up to 40–100 kWe (Fission Surface Power)

## Slide 4: Design Drivers Unique to Space
Mass is the currency
  every kg of shield, reflector, or structure is a kg of payload you did not deliver
  drives you hot (better conversion efficiency, smaller radiators) and compact (fast or epithermal cores)
No maintenance, no refueling, no coolant makeup
  10–15 year unattended life for power systems; a single leak is mission-ending
Launch and reentry safety
  the core must stay subcritical if it is dropped into water or wet sand, and survive reentry intact
Thermal cycling
  NTP: ambient to ~2700 K in seconds, repeated tens of times
  power systems: one startup, then hold temperature for a decade

## Slide 5: A Brief History
1955–1973 – Rover/NERVA
  13 research reactors and 6 nuclear engines built and tested in Nevada
1955–1973 – SNAP
  SNAP-10A launched April 1965; still the only U.S. reactor flown
1960s–70s – GE-710 and ANL cermet programs
1970s–80s – Soviet BUK/RORSAT and TOPAZ
  more than 30 reactors flown
1983–1994 – SP-100
  UN / Li / Nb-1Zr, 100 kWe, never flown
1987–1993 – SNTP (Timberwind), particle bed
2015–2018 – Kilopower / KRUSTY
  first U.S. space reactor criticality since the 1960s
2021–2025 – DRACO (cancelled May 2025)
2022–present – Fission Surface Power

## Slide 6: Space fission power

## Slide 7: A Different Duty Cycle
Nuclear thermal propulsion
  hours of operation, total
  2700–3000 K
  flowing hydrogen
  tens of thermal cycles
  burnup is negligible – swelling and fission gas do not matter
  failure mode: corrosion and coating cracking
Space fission power
  10–15 years continuous
  800–1400 K
  liquid metal, static or pumped
  one startup, then hold
  burnup, swelling, and creep are first-order
  failure mode: mass transfer, creep rupture, hydrogen loss

## Slide 8: The SNAP Program
Systems for Nuclear Auxiliary Power, 1955–1973
  compact U–ZrH cores, NaK coolant, SiGe thermoelectric conversion
SNAP-10A – launched 3 April 1965
  reached ~590 We, operated 43 days
  shut down by a spacecraft voltage regulator failure, not by the reactor
  still the only U.S. fission reactor ever flown
SNAP-8 Experimental Reactor – the ground test article
  600 kWt, 211 fuel elements, 93.15% enriched, 6.56 kg ²³⁵U, 10,000 h design life
  NaK inlet 1100 °F / outlet 1300 °F, BeO internal and Be external reflector

## Slide 9: SNAP Fuel: U–ZrH
Fuel and moderator in a single material: Zr–10 wt% U, hydrided to ~6×10²² H atoms/cm³
The hydrogen gives a strong prompt negative temperature coefficient
  heat the fuel, the hydrogen spectrum hardens, reactivity drops – the core self-regulates
  this is why such a small, simple core is stable enough to fly unattended
Every materials problem with this fuel comes from the same hydrogen
  dissociation and loss at temperature
  redistribution down thermal gradients, shifting local moderation and local power
  hydride phase changes produce volume change and cracking
The upper temperature limit of the fuel is set by hydrogen retention, not by melting

## Slide 10: Hydrogen Permeation Barriers
If hydrogen leaves the fuel you lose moderation, then reactivity, then the core
SNAP-8 used Hastelloy-N cladding with a ceramic diffusion barrier on the inner surface
  barrier designated AI-8763D, infused with Sm₂O₃ as a burnable poison at 3.34 mg/in of cladding
The barrier does double duty – it blocks hydrogen and carries the burnable absorber
Barrier integrity is the life-limiting item
  a crack or a thin spot is a local hydrogen leak, and the damage is not recoverable
  you cannot inspect or repair it once the system is launched
The same problem is back today for ZrH and YH moderators in terrestrial microreactors

## Slide 11: SP-100
1983–1994 joint DOE / NASA / DARPA program; 2.5 MWt producing 100 kWe
UN fuel pins, PWC-11 cladding (Nb–1Zr–0.1C), lithium coolant
  PWC-11 also used for the vessel, internals, and primary heat transport
Reactor outlet 1300–1350 K; heat rejection at 800–850 K
SiGe/GaP thermoelectric conversion at ~4% efficiency
  no moving parts, at the cost of a very large radiator
12 BeO reflector elements for control; 4 in-core B₄C safety rods
Shield: LiH for neutrons, W for gammas, Be for thermal control, in a Ti shell
Cancelled without flight – the fuel and refractory alloy database is what survived

## Slide 12: UN Fuel
Attractive for exactly the reasons oxide is not
  high uranium density (~13.5 g U/cm³), high thermal conductivity, high melting point
  thermal conductivity increases with temperature – the opposite of UO₂
The drawbacks are chemical and economic
  dissociates rather than melting congruently; wants a nitrogen overpressure at high temperature
  oxygen- and moisture-sensitive – fabrication and handling must be inert throughout
  ¹⁴N(n,p)¹⁴C production argues for ¹⁵N enrichment, which is expensive
Swelling and fission gas release drive the pin design: plenum volume, smear density, gap
The same fuel is the reference for cermet NTP and for several terrestrial microreactors

## Slide 13: Refractory Alloys: the Real Obstacle
Nb–1Zr, PWC-11, Mo–Re, Ta–10W, W–Re–Mo – the only structural options above ~1300 K
Zr and Hf additions exist to scavenge oxygen
  that is the entire reason Nb–1Zr survives in lithium
Oxygen contamination during fabrication is the dominant failure mode
  welding and processing must be in vacuum or ultra-high-purity inert gas
  Nb–1Zr shows intergranular attack once initial oxygen exceeds ~3375 ppm
Recrystallization during service raises DBTT and embrittles the component
  irradiation hardening compounds it – Mo and W are marginal to begin with
The loss of U.S. industrial capability in these alloys since SP-100 is frequently cited as a program risk

## Slide 14: Kilopower and KRUSTY
LANL/NASA; the Kilopower family was designed for 1–10 kWe over 12–15 years
KRUSTY was the 1 kWe demonstration unit, tested at NNSS from November 2017 to March 2018
Core: cast U–8 wt% Mo, 93% enriched, ~32 kg
  a single annulus – 4 cm ID, 11 cm OD, 25 cm tall
8 Haynes 230 sodium heat pipes in slots machined into the fuel, ~15 cc Na each
BeO reflector plates; stainless steel and B₄C shielding
2 live Stirling convertors plus 6 thermally identical mock-ups
20 March 2018: 28 h full-power run, ~5 kWt, peak core ~800–850 °C
  deliberately abused – convertor shutdown, thermal cycling, loss of heat removal – and it self-regulated

## Slide 15: KRUSTY Fuel: U–8Mo
Monolithic cast metal fuel – not pins, not pellets, a single piece
Mo stabilizes the high-temperature γ-U phase
  suppresses the anisotropic irradiation growth of α-U that plagues unalloyed uranium
Very high thermal conductivity – the core is close to isothermal and responds as one body
Control is the fuel itself: thermal expansion increases leakage, which drops power
  no operator action, no control system in the loop
What a 28 h test does not tell you, for a 12 year mission:
  fission gas swelling at these temperatures over a decade
  creep of the fuel around the heat pipe slots, and gap conductance evolution
  fuel / heat pipe interdiffusion, and γ-U–Mo phase stability under irradiation at ~800 °C

## Slide 16: Heat Pipes
A heat pipe moves heat with no pump and no moving parts – exactly what you want when you cannot maintain it
Envelope + wick + working fluid; the fluid sets the useful temperature range
  Na: ~800–1100 K (Kilopower class)
  K: intermediate
  Li: 1400–1700 K (SP-100 class and above)
Envelope pairing follows the fluid
  Haynes 230 or stainless for Na; Nb–1Zr or Mo for K and Li
Failure modes are chemical, not mechanical – the pipe does not burst, it fouls
Redundancy is the design answer: lose a pipe and the core redistributes heat to its neighbors

## Slide 17: Alkali Metal Compatibility
Pure alkali metals are compatible with most refractory alloys. Impure ones are not
The mechanism is impurity transport
  O and C diffuse out of the condenser wall into the fluid
  they concentrate at the evaporator, then precipitate or form low-melting eutectics
Purity targets are severe
  <0.1 ppm oxygen in sodium, by vacuum distillation
  Ti and Zr getters, plus oxygen-scavenging alloy additions
Demonstrated lifetimes
  Mo / Na: 45,039 h at 1391 K, no failure
  Mo / Li: 25,216 h at 1700 K, failed by grain-boundary Ni attack
  Nb–1Zr / K: 10,000 h at 1150 °C, essentially no attack
>10⁵ h (~12 yr) is considered achievable with the same procedures
These lifetimes are set by cleanliness during manufacturing
  a process control problem as much as a materials problem

## Slide 18: Power Conversion and Shielding
Conversion
  thermoelectric (SiGe): no moving parts, ~4% efficient – SNAP-10A, SP-100
  Stirling: much higher efficiency with moving parts – Kilopower; hot-end alloy and regenerator are the materials issues
  closed Brayton: NASA’s preferred route at 100 kWe; needs high-temperature turbine alloys and a gas boundary
Efficiency buys radiator area, and radiator area is mass
Shielding
  LiH for neutrons – highest hydrogen density per unit mass
  W or depleted U for gammas
  shadow shield only – 4π shielding is unaffordable, so everything off-axis sees full fluence
LiH brings its own problems
  hydrogen retention and a low temperature limit – the same hydride issue, again

## Slide 19: Fission Surface Power Today
Phase 1 (2022): three 12-month design contracts at a 40 kWe target
  Lockheed Martin, Westinghouse, and IX (Intuitive Machines / X-energy)
  6000 kg mass limit, 120 Vdc, 5 rem/yr at 1 km
August 2025 RFI raised the target to 100 kWe with closed Brayton conversion
  heavy-class lander, up to 15 t
January 2026: NASA/DOE memorandum of understanding; reactor targeted for readiness by Q1 FY2030
  the releases are deliberately ambiguous about “built by then” versus “operating on the Moon by then”
Russia and China have announced lunar surface reactors in the 2033–2035 timeframe
Fuel form and enrichment are not public for all three U.S. teams

## Slide 20: Cross-Cutting Materials Challenges
Temperature – everything wants to run hotter: higher Isp, better efficiency, smaller radiators
Time – NTP needs hours, power systems need a decade; the same material fails differently in each
Environment – hot hydrogen, liquid alkali metals, and vacuum each attack something different
Irradiation – fast spectrum, and almost no relevant irradiation data on any of these materials
Fabrication – refractory alloys, carbides, and cermets are hard to make and harder to make reproducibly
Qualification – terrestrial fuel is qualified by years of irradiation; no space program has that schedule
Note that none of these are new materials
  it is the same short list from the 1960s, still not qualified

## Slide 21: Nuclear thermal propulsion

## Slide 22: NTP Fundamentals
Solid-core NTP: hydrogen flows through channels in a fueled solid and out a nozzle
Performance is set by chamber temperature divided by exhaust molecular weight
  Isp ≈ (1/g₀)√[ 2γ/(γ–1) · RᵤT_c / M ]
Chemical combustion is stuck at M ≈ 18–22 for LH2/LOX; NTP runs pure H2 at M = 2
  even at a lower chamber temperature, NTP roughly doubles Isp
There is no combustion, so the peak temperature is not set by chemistry – it is set by the fuel
The entire engine reduces to one materials question:
  how hot can a fueled solid get, in flowing hydrogen, without losing its uranium?

## Slide 23: Why Hydrogen, and Why It Hurts
Hydrogen is the best propellant and the worst chemical environment you could pick
Strongly reducing
  reduces oxides – UO₂ survives only if it is fully encapsulated
Reacts with carbon to form volatile hydrocarbons
  CH₄ and C₂H₂ formation dominates mass loss from ~1500–2900 K
  above ~2900 K, vaporization of U–Zr–C takes over as the dominant loss mechanism
Dissociates to atomic H at temperature
  permeates metals, and strips hydrogen out of hydride moderators
Mass flow is enormous, so corrosion products are swept away continuously
  no protective scale ever forms – attack does not self-limit

## Slide 24: Rover/NERVA Overview
Kiwi (1959–64)
  non-flight “won’t fly” test reactors; proved the concept and found the failure modes
Phoebus (1965–68)
  power scaling; Phoebus-2A reached 4100 MWt in July 1968
Pewee (1968)
  small, very high power density test bed; set the fuel and exhaust temperature records
NRX / XE (1964–69)
  engine-configuration tests; NRX-A6 ran 62 min continuously, XE′ demonstrated 28 restarts
Nuclear Furnace NF-1 (1972)
  fuel element test reactor; ~109 min accumulated at full power, ~5 MWt/L
Cancelled in 1973
  for budget and mission reasons, not because of a technical failure

## Slide 25: The NERVA Core
Hexagonal prismatic fuel elements in a tightly packed hexagonal array
Structural tie tubes interspersed among the fuel elements
  roughly 2 fuel elements per tie tube – the SNRE design used 564 elements and 241 tie tubes
Beryllium radial reflector with rotating control drums (absorber on one face)
Hydrogen path is a cascade of cooling duties before the core:
  tank → turbopump → nozzle and reflector cooling → tie tubes → core → nozzle
  everything structural sits upstream of the hot end and stays cold
Aluminum/steel pressure vessel, internal shield, regeneratively cooled nozzle

## Slide 26: Fuel Element Geometry
Hexagonal prism, ~0.75 in across the flats, 52 in (1.32 m) long in heritage designs
  later SNRE-class designs shortened the element to 0.89 m (35 in)
19 axial coolant channels per element
Channels and the element exterior are coated by CVD – NbC early, ZrC later
  uniform coating of a 1.3 m long, ~2.5 mm diameter hole is a nontrivial process problem
Uranium loading ~0.25–0.60 g U/cm³ depending on engine class
Peak demonstrated power density ~5 MWt/L (~5000 MWt/m³)
  for comparison, an LWR core runs about 0.1 MWt/L

## Slide 27: Tie Tubes and the ZrH Moderator
Tie tubes carry the mechanical load and hold the core in compression
They also carry a sleeve of ZrH moderator with a coaxial Inconel tube for regenerative cooling
  moderation raises reactivity, which lets you cut uranium loading – or reach LEU at all
Two-pass flow: hydrogen cools the tie tubes, then returns to the core inlet
  recovering that heat instead of dumping it raises Isp
The materials constraint is severe
  ZrH begins losing hydrogen above ~700 K
  so a ~700 K component has to survive while sitting inside a ~2700 K core
ZrH tie tubes were demonstrated in Pewee

## Slide 28: Fuel Generation 1: Beaded Graphite
Original Kiwi/NERVA fuel: UO₂ or UC₂ particles dispersed in an extruded graphite matrix
  later versions coated the particles in pyrolytic carbon to retain fission products
Graphite is attractive – it moderates, it is cheap, machinable, and strong at temperature
Graphite is also the problem
  carbon + hot H2 → CH₄ / C₂H₂, so any exposed matrix is consumed
  the graphite matrix CTE does not match the carbide coating, so the coating cracks on heatup
Uranium loss shows up twice: as reactivity and performance loss, and as effluent contamination

## Slide 29: Fuel Generation 2: Composite
(U,Zr)C dispersed in a graphite matrix – the “composite” fuel
The two jobs are now separated
  the carbide phase carries the uranium and resists hydrogen
  the graphite provides moderation, thermal conductivity, and machinability
Critically, the CTE moves in the right direction
  composite fuel: 6–6.5 μm/m·K, versus 7.1 μm/m·K for NbC coating
  much less coating cracking, therefore much less corrosion
Higher temperature capability and better fission product retention than beaded fuel
This is the fuel form that NF-1 tested most successfully

## Slide 30: Fuel Generation 3: Carbides
Solid-solution (U,Zr)C with no free graphite – the highest temperature capability tested
Composition control is the whole game
  target C/M ratios of 0.88–0.95 – substoichiometric carbon suppresses free carbon
  ternary (U,Zr,Nb)C melts ~100–700 K above binary carbides that have a separate carbon phase
Elements were designed for fuel temperatures up to ~3200 K
The cost is fabricability and toughness
  very brittle, poor thermal shock resistance, hard to form into long thin-web elements
Never fully qualified before the program ended in 1973

## Slide 31: Coatings
The coating is the only thing between hot hydrogen and the fuel
NbC first
  CVD applied, but the CTE mismatch with graphite fuel cracked it during heatup
ZrC later
  better fission product retention at high temperature, better CTE match to composite fuel
  typical particle architecture: two pyrocarbon layers plus an outer ZrC layer
Coating failure is local and self-accelerating
  a crack exposes matrix → hydrogen excavates a cavity → the cavity grows and unloads more coating
So coating integrity, not fuel melting, sets the practical temperature limit

## Slide 32: Hydrogen Corrosion Mechanisms
Chemical attack, ~1500–2900 K
  carbon constituents react with H2 to form CH₄ and C₂H₂
  rate set by H2 partial pressure, temperature, and exposed carbon area
  dominant loss mechanism over most of the element length
  no protective product forms – flow sweeps everything away
Vaporization, above ~2900 K
  vaporization of U–Zr–C takes over
  shifts in the U/Zr/C ratio liberate free carbon, which then reacts chemically
Irradiation makes both worse
  radiation damage lowers thermal conductivity
  steeper gradients → higher stresses → more cracks → deeper hydrogen penetration

## Slide 33: Midband Corrosion
Corrosion in Rover/NERVA elements was not uniform along the length – it peaked in the middle
The usual explanation is mechanical, with a chemical consequence
  cold inlet end: gas is hot enough to flow but kinetics are too slow to matter
  hot exit end: the coating is above its brittle range and accommodates strain
  midband: the coating is still brittle but the gas is already hot – cracks open and stay open
So the root cause is CTE mismatch and thermal stress; the damage is hydrogen attack through the crack
The fix was not a better coating – it was a fuel with a CTE closer to the coating
  i.e., the move from beaded graphite to composite fuel

## Slide 34: What Rover/NERVA Actually Demonstrated
United States
  13 research reactors, 6 nuclear engines
  Phoebus-2A: 4100 MWt (July 1968)
  Pewee: 2750 K peak fuel temperature, ~2550 K peak exhaust, ~5200 MWt/m³ peak power density
  NRX-A6: 62 min continuous
  XE′: 28 restarts
  NF-1: ~109 min accumulated at full power
Soviet Union
  ~1550 fuel assemblies tested over 19 years
  7 full-core tests and ~160 transient tests at IGR (1962–1978)
  reported H2 exit temperatures of 2800–3300 K
  uranium loss inferred at 0.5–1.0% from reactivity loss measurements
Note what is missing from both lists
  no long-duration, high-burnup fuel performance data

## Slide 35: CERMET Fuels: History
The parallel development line: put the fuel in a refractory metal matrix instead of carbon
GE-710 (1962–68) and the ANL Nuclear Rocket program: W–UO₂ and Mo–UO₂ cermets
  1–2 μm tungsten powder sintered to ~95% of theoretical density
  gadolinia-stabilized ANL fuel retained UO₂ at 2770 K for 45 h and 180 thermal cycles
Advantages over graphite-based fuel
  no carbon, so no methane pathway; high thermal conductivity; ductile matrix; excellent FP retention
Disadvantages
  W is 19.3 g/cm³ – mass is a real penalty, and enriched ¹⁸⁴W is needed to limit parasitic absorption
  powder metallurgy fabrication is difficult and expensive at element scale

## Slide 36: CERMET Fuels: Current Reference
NASA’s reference NTP fuel is UN particles at 40–70 vol% in a Mo–30W matrix
Why UN instead of UO₂
  higher uranium density, much higher thermal conductivity, higher melting point
Why Mo–30W instead of W
  lower density and lower absorption while still refractory
  the solid solution resists grain growth far better than pure Mo
The particles are coated (e.g., W) to block UN–matrix interaction and fission product release
The open issue is UN itself
  UN dissociates rather than melting congruently and wants a nitrogen overpressure
  you cannot provide that inside a flowing hydrogen channel

## Slide 37: CERMET Fabrication
Powder metallurgy: blend, consolidate, densify
Current routes are hot isostatic pressing and spark plasma sintering
  SPS densifies fast at lower temperature, which limits matrix grain growth and particle interaction
Volume loading is the central tradeoff
  more fuel gives more uranium but a weaker, less well-connected matrix
Ceramic particle additions strongly suppress matrix grain growth
  demonstrated with YSZ surrogate particles in Mo–30W
Historical stabilizers (Gd₂O₃, Y₂O₃) were used to slow UO₂ loss from oxide cermets
Reproducibility at element scale, not feasibility, is the current problem

## Slide 38: Hot Hydrogen Testing
Mo–30W with YSZ surrogate particles, flowing H2, 1920–2500 °C, 80 min exposures
  minimal mass loss, minor to no cracking, good retention of the internal particles
  the solid solution outperformed pure Mo, especially at the top of the temperature range
Encouraging – but understand what these tests are not
  surrogate particles: no real UN chemistry, no actinide transport
  no fission: no fission products, no fission gas, no radiation damage
  minutes to hours, against a mission duty cycle of tens of cycles and hours at temperature
There is no modern integral irradiation data on any candidate NTP fuel

## Slide 39: Moderators for NTP
A HALEU core needs moderation, and moderation means putting hydrogen inside a very hot core
ZrH – demonstrated in Pewee tie tubes, but dissociates above ~700 K
YH is the leading alternative
  at 900 °C, YH holds ~1.6× the hydrogen of ZrH at 1 atm equilibrium; ~2.6× at 1100 °C
  at the same temperature and H/M ratio, YH equilibrium H2 pressure is orders of magnitude lower
Both need cladding and a permeation barrier – hydrogen loss is reactivity loss
Data gaps are significant
  mechanical properties above 700 °C are largely missing; irradiation data stop around 2 dpa
  desorption kinetics and hydrogen redistribution in a gradient are essentially uncharacterized

## Slide 40: Reflectors, Control, and Structure
Radial reflector: Be or BeO
  best reflection per unit mass available, which is why it is used despite everything else
  limited to below ~1000 K, brittle, and the dust is a serious industrial hygiene problem
Control: drums in the reflector with an absorber (B₄C) on one face, rotated to change leakage
  no room for control rods in the core – the core is all fuel
Tie tubes: Inconel, coaxial, doing structural and thermal duty simultaneously
Cladding and structural candidates for the hot end: Ta, Ta–10W, W–30Re–30Mo
  W–30Re–30Mo has low oxygen permeability and high strength, but thermal cycling stresses the bond

## Slide 41: From HEU to HALEU
Rover/NERVA was HEU. Modern programs are pushed toward <20% enrichment
The neutronic consequences cascade straight into materials
  less ²³⁵U per unit volume → you need more moderation, or a physically larger core
  more moderation → hydride in the core → a hydrogen retention problem at temperature
  more ²³⁸U → more parasitic absorption and a harder core design
A larger core is heavier, and mass is the thing you were optimizing
The critical point for this course:
  the entire historical fuel, corrosion, and coating database is HEU
  there is no experimental performance data for a HALEU NTP fuel system

## Slide 42: DRACO
DARPA program, NASA formally joined January 2023; goal was an in-space NTP flight demonstration
HALEU (~20%) fuel, processed by BWXT; early reactor design work at General Atomics
Lockheed Martin and BWX Advanced Technologies selected July 2023 to design, build, and demonstrate
  launch planned for 2027, target Isp >800 s
Launch placed on indefinite hold January 2025; program cancelled 30 May 2025
  DARPA’s stated reason was falling launch costs weakening the cost-benefit case
  not a materials failure, and not a test failure
Worth discussing: whether an unqualified fuel could have met that schedule regardless

## Slide 43: NTP Materials Gaps
No qualified fuel
  neither cermet nor carbide has an irradiated, hot-hydrogen-tested performance basis
No integral test capability
  no current facility tests fueled elements in flowing hydrogen, at temperature, under fission
Coating and cladding lifetime under thermal cycling is largely uncharacterized
HALEU moderator materials (YH) lack high-temperature mechanical and irradiation data
Property data for (U,Zr)C, UN, and Mo–W above 2000 K are sparse, and often trace to single 1960s studies
No validated fuel performance code exists for NTP conditions
  compare with what we just covered for metallic and oxide fast reactor fuels

## Slide 44: Summary
Space nuclear is two materials problems, not one
  NTP: hot, short, hydrogen. Power: warm, long, liquid metal
NTP fuel evolved beaded graphite → composite → carbide → cermet; none of them is qualified
Hydrogen corrosion, CTE-driven coating cracking, and midband corrosion are the classic NTP failure modes
HALEU pushes moderator into the core, which makes hydride hydrogen retention a first-order problem
Power systems are limited by refractory alloy fabrication, alkali metal purity, and unattended lifetime
KRUSTY showed that a complete system works. It did not show that it works for twelve years
The gap between “demonstrated” and “qualified” is the entire remaining program

## Slide 45: Sources: Nuclear Thermal Propulsion
Nuclear Thermal Propulsion Reactor Materials, IntechOpen (2020)
  fuel forms, coatings, hydrogen corrosion, and the Rover/NERVA and Soviet test records
Space Nuclear Propulsion for Human Mars Exploration, National Academies (2021)
Borowski & Sefcik, NTP engine and fuel element design, NASA NTRS 20160014802
Hot hydrogen testing of Mo30W matrix surrogate cermets, J. Nucl. Mater. (2024)
Yttrium hydride neutron moderators in microreactors, review (2026)
DRACO program timeline and cancellation – secondary summary
Rover/NERVA test data quoted here trace to the two reviews above, not to the original test reports

## Slide 46: Sources: Space Fission Power
Poston et al., KRUSTY Reactor Design, Nuclear Technology 206 (2020)
KRUSTY design detail, LANL LA-UR-15-26603 (OSTI)
Kilopower program summary and KRUSTY test results – secondary summary
SNAP-8 Experimental Reactor description, INL Virtual Test Bed
SNAP-10A flight summary – secondary summary
SP-100 Nuclear Space Power Systems, NASA TM-101403 (1988)
Alkali Metal Heat Pipe Life Issues, NASA NTRS 20040082321
NASA Fission Surface Power, Phase 1 project documentation (NTRS, 2022)
NASA/DOE lunar surface reactor announcement (January 2026)