Exam 3: NE533: Nuclear Fuel Performance

Show all work. Label question number in your response. Pay attention to units. Point values correspond to expected depth of response.

- (10 pts) Determine the total change in the fuel volume given: th=10x10-6, fission rate = 8x1013 fiss/cm3-s, Tf=1500 K, Tref=300 K, 0=0.015, BD=5 MWD/kgU, (UO2) =10.97 g/cc, t=300 days.

- (8 pts) What is the total creep in a RXA zirconium cladding given a von Mises stress of 60 MPa, a temperature of 600 K, a LHR of 250 W/cm, and a time of 200 days? A0 = 3.14 × 1024; G = 4.2519 × 1010 − 2.2185 × 107T; n = 5; Q = 2.7 × 105, C0=1.654E-24; C1=0.85; C2=1

- (8 pts) Two fuel pellets are irradiated for 250 days at 1400 K at a fission rate of 2x1013 fiss/cm3-s. One fuel sample has a grain size of 5 microns, and the other has a grain size of 40 microns. What fraction of fission gas is released in each?

- (4 pts) What is the typical charge state of U in UO2? What can cause it to change?

- (5 pts) How does the oxygen concentration change across the fuel pellet? How does Mo impact this?

- (3 pts) Name three properties that vary as a function of stoichiometry in UO2.

- (10 pts) What are the five types of fission products that form in the fuel? List a role each plays in fuel performance.

- (8 pts) List and describe the three stages of fission gas release.

- (5 pts) What is creep? What is one mechanism of creep (name and physical description)?

- (8 pts) What is the high burnup structure? Why does it form? What are some performance aspects of this structure?

- (6 pts) Describe the irradiation growth of hcp Zr due to point defects.

- (8 pts) Describe how creep impacts the Zr cladding over time in a fuel rod.

- (12 pts) What are the four conditions that must be met for SCC? Briefly describe how each is met in PCI.

- (5 pts) What role does iodine play in the corrosion of Zr cladding?