## Slide 1: NE 763: Advanced Reactor Materials
Fall 2026
Dr. Benjamin Beeler

## Slide 2: Why qualification matters

## Slide 3: What Does "Qualified" Mean?
Fuel qualification (NRC framing, NUREG-2246)
  High confidence that the fuel will be fabricated in accordance with its specification
  High confidence that the fuel will perform as described in the applicable licensing safety case
Structural materials qualification
  Material is accepted by a design code (e.g., ASME Section III) with design allowables for the intended temperature and time
  Code acceptance is then endorsed (with or without conditions) by the regulator
Qualification is always tied to an envelope: temperature, burnup/dose, environment, transients
  Operate outside the envelope, and the material is no longer "qualified"

## Slide 4: Why This Matters for Advanced Reactors
Existing fuel guidance (NUREG-0800, Section 4.2) was developed for Zr-clad UO2 in LWRs
Advanced reactors change nearly everything the guidance was built on
  neutron spectrum (fast vs. thermal)
  fuel form (metallic, TRISO, nitride, carbide, liquid salt)
  temperatures, coolants, neighboring materials
  burnup targets and core lifetimes
Many of the phenomena that dominate LWR fuel limits simply do not apply, and new ones do
Every new fuel or alloy must build its own qualification basis, often from sparse legacy data

## Slide 5: The Traditional Approach
Fabrication
development
Out-of-pile
characterization
Integral
irradiation tests
Post-irradiation
examination
Transient / safety
testing
Licensing
unexpected failure → redesign and repeat
Relies heavily on empirical data from a series of sequential integral tests
Historically has taken 20 years or longer to build a qualification database
Particularly slow for non-LWR fuels with high burnup and multi-year lifetimes
Notes: 20+ year figure: NRC ADAMS ML21287A646, "Accelerated Fuel Qualification White Paper." Diagram is a simplified generic sequence, not taken from a specific source.

## Slide 6: Why Is It So Slow?
Burnup accumulates on the timescale of the test reactor, not the experimenter
  multi-year irradiations are needed to reach high burnup at prototypic fission rates
Test reactor space is limited, and irradiated specimens need cooling before PIE
PIE in hot cells is slow and expensive
Sequential design: a failure late in the program sends you back to the beginning
Test fuel must be representative of production fuel
  changing the fabrication process can invalidate prior irradiation data
Largely empirical understanding transfers poorly to new designs

## Slide 7: Fuel qualification framework

## Slide 8: NUREG-2246 Framework
Issued by the NRC in March 2022 (draft for comment June 2021)
Provides a fuel qualification assessment framework that would satisfy regulatory requirements
Top-down approach: high-level regulatory requirements are supported by lower-level, objective goals
  methodical, and provides some assurance of completeness when a fuel is claimed to be qualified
Applicable to operating licenses, design certifications, combined licenses, manufacturing licenses, and standard design approvals
Technology-inclusive: intended to apply across solid fuel forms
  non-solid fuels (e.g., MSR fuel salt) may require additional or alternative criteria
Notes: NUREG-2246 final: ML22063A131 (includes public comment resolution). ACRS letter on the draft: ML21319A350.

## Slide 9: Framework Structure
Fuel is qualified for its intended use
G1: Fabrication
fuel manufactured per its specification
G2: Performance
fuel performs as described in the safety case
Key manufacturing
parameters identified
Process and quality
controls
Design limits for normal
operation and AOOs
Radionuclide retention
requirements
Evaluation models
and supporting data
Notes: The two top-level criteria (fabricated per specification; performs per safety case) are from NUREG-2246. G2 sub-goal names (e.g., G2.1 design limits during normal operation and AOOs, G2.2.1 radionuclide retention requirements) are paraphrased from the report; sub-boxes are a simplified summary, not the full goal tree. Check Appendix A of NUREG-2246 for the complete list before presenting the tree in detail.

## Slide 10: What the Framework Emphasizes
Key fuel manufacturing parameters
  which as-fabricated attributes actually control performance, and how they are controlled
A fuel performance envelope
  the conditions the fuel must survive; this is what defines testing requirements
Evaluation models
  models used to predict fuel behavior within the envelope, and their validation
Assessment of the experimental data
  data used to develop and validate models and empirical safety criteria must be adequate in quality and coverage

## Slide 11: Evaluation Models and PIRT
An evaluation model links the test data to the licensing safety case
The PIRT (Phenomena Identification and Ranking Table) process is one acceptable method to identify the phenomena a model must capture
  used for Cr-coated Zr cladding guidance (ATF-ISG-2020-01)
  see Regulatory Guide 1.203 for the PIRT and evaluation model development process
The framework allows a graded approach
  simplified, conservative models can be used to reduce data requirements
  the trade-off: more conservatism means less operating margin

## Slide 12: Lead Test Specimens
Lead test specimens (or lead test assemblies) are irradiated ahead of the rest of the fuel
Used successfully in operating reactors, and discussed in NUREG-0800, Section 4.2
NUREG-2246 considers lead test specimen programs as a way to shorten qualification timelines
  begin operation within an already-supported envelope
  extend burnup or operating limits as lead specimens demonstrate performance
Implication: fuel qualification does not have to be complete before first operation, but the operating envelope is limited until data exist

## Slide 13: Accelerated fuel qualification

## Slide 14: The AFQ Concept
Proposed approach to transform and accelerate fuel development and qualification (Terrani et al., 2020)
Use advanced modeling and simulation at the outset
  inform constituent and system selection
  enable integral fuel performance analyses
Modeling identifies and prioritizes the most important fuel performance parameters and phenomena
These are then characterized with targeted separate-effects tests, both out-of-pile and in-pile
Integral tests shift from discovery toward confirmation
Notes: K.A. Terrani, N.A. Capps, M.J. Kerr, C.A. Back, A.T. Nelson, B.D. Wirth, S.L. Hayes, C.R. Stanek, "Accelerating nuclear fuel development and qualification: Modeling and simulation integrated with separate-effects testing," J. Nucl. Mater. 539 (2020) 152267. doi:10.1016/j.jnucmat.2020.152267

## Slide 15: Conventional vs. AFQ
Conventional
Accelerated (AFQ)
Fabricate
Integral irradiation
PIE
Empirical correlations
Qualified envelope
Modeling & simulation
Separate-effects
tests (out-of-pile)
Separate-effects
tests (in-pile)
Integral confirmation
Notes: Schematic simplified from the concept in Terrani et al. (2020); not a reproduction of their figure. Talking point: models prioritize phenomena, and separate-effects test data feed back to refine the models.

## Slide 16: Separate-Effects Testing
Isolate one phenomenon at a time under controlled conditions
  thermal conductivity, creep, swelling, fission gas release, chemical interaction
Out-of-pile: property measurements, diffusion couples, furnace tests, ion irradiation
In-pile: small specimens, controlled temperature, instrumented where possible
Miniature fuel specimens reduce irradiation volume, cost, and PIE burden
  e.g., Petrie et al., J. Nucl. Mater. 526 (2019) 151783
Accelerated-burnup capsule designs
  e.g., Beausoleil et al., Nucl. Technol. (2019)
Data are only useful if they feed parameters in a mechanistic model
Notes: Specimen and capsule references are as cited in the NRC ADAMS AFQ white paper (ML21287A646). I did not verify their full content. Ion irradiation listed as an out-of-pile separate-effects tool is general knowledge; see the non-prototypicality slide.

## Slide 17: The Catch: Non-Prototypical Conditions
Accelerated tests intentionally depart from reactor conditions
  higher fission rates, altered burnup accumulation, small geometries, ions instead of neutrons
Some quantities scale differently than others
  e.g., in the FAST accelerated approach, fuel burnup is accelerated but dose to the cladding is not
An intimate connection to mechanistic modeling is required to account for these non-prototypicalities
Consequence: AFQ moves the burden from test duration to model credibility
  models must be validated, and the regulator must accept the argument
Notes: FAST cladding-dose point is from the NRC ADAMS AFQ white paper (ML21287A646). I believe FAST stands for Fission Accelerated Steady-state Test at INL/ATR, but this was not verified; check before stating the acronym.

## Slide 18: Limits of AFQ
Models can only capture phenomena someone thought to include
  PIRT completeness is a judgment, and unknown-unknowns are the historical cause of fuel failures
Separate-effects data may miss coupled behavior
  e.g., interactions between swelling, temperature, chemistry, and mechanical contact
Integral tests are reduced, not eliminated
Fabrication still must be reproducible and representative
Discussion question: which phenomena in the fuels from this course would be hardest to predict without integral data?
Notes: This slide is instructor synthesis, not drawn from a single source.

## Slide 19: Case studies

## Slide 20: The AGR Fuel Program: Motivation
DOE Advanced Gas Reactor Fuel Development and Qualification Program, started in 2002
The most recent large-scale fuel qualification campaign in the US
Why it was needed
  the last US LEU TRISO irradiation (HRB-21, early 1990s) substantially exceeded expected particle failure and fission product release
  modular HTGRs aim to meet EPA Protective Action Guides at the exclusion area boundary, requiring fuel integrity far better than prior US TRISO
Program goals
  provide a fuel qualification dataset to support HTGR licensing
  establish a domestic commercial TRISO fuel vendor
Notes: HRB-21 and requirements context: AGR-1 objectives report https://inldigitallibrary.inl.gov/sites/sti/sti/3397099.pdf . Start year 2002: Technical Program Plan https://inldigitallibrary.inl.gov/sites/sti/sti/Sort_61424.pdf . EPA PAG design goal: OSTI 1369357 https://www.osti.gov/biblio/1369357 . Goals (qualification data, domestic vendor): Demkowicz 2017 overview https://art.inl.gov/trisofuels/AGR%20TRISO%20Fuels%20Program%20Review%20July%201819%202017/03_Demkowicz_AGR_Overview%20v3.pdf

## Slide 21: TRISO and Functional Containment
TRISO fuel is at the heart of the safety case for modular HTGRs
Key component of the "functional containment" licensing strategy
  radionuclides retained within multiple barriers, with emphasis on retention at their source in the fuel
Qualification therefore requires demonstrating
  high-quality, low-defect fabrication
  robust performance during irradiation and high-temperature transients
  low fission product release
With no VHTR design available at program start, fuel requirements were drawn from GT-MHR pre-conceptual design documentation
Notes: Functional containment and three requirements: Demkowicz AGR overview slides (2015 DOE and 2017 INL program review). GT-MHR basis: AGR-1 objectives report https://inldigitallibrary.inl.gov/sites/sti/sti/3397099.pdf

## Slide 22: AGR Program Elements
Fuel qualification dataset
Fuel
fabrication
Fuel
irradiation
PIE and
safety testing
Fuel performance
modeling
Fission product
transport & source term
Participants: INL, ORNL, BWXT, General Atomics
Irradiations in INL's Advanced Test Reactor; coating process developed to replicate German particles with superior irradiation and accident performance
Notes: Elements and participants: Demkowicz AGR overview, DOE 2015 https://www.energy.gov/sites/default/files/2015/10/f27/Demkowicz%20%20AGR%20overview.pdf . German particle replication goal: Technical Program Plan https://inldigitallibrary.inl.gov/sites/sti/sti/Sort_61424.pdf

## Slide 23: AGR Irradiation Campaigns
AGR-1
Lab-scale fuel (2-in. coater)
Early performance test; shakedown of the test train design
AGR-2
Scaled-up fuel
Engineering-scale particles and compacts
AGR-3/4
Designed-to-fail fuel
Fission product retention and transport in core materials
AGR-5/6/7
Qualification test fuel
Normal and accident conditions; margin to failure
Each campaign: fabrication → ATR irradiation → PIE → high-temperature safety testing
Notes: AGR-1 lab-scale 2-in. coater and scale-up to 6-in. production-scale coater; AGR-3/4 fission product transport; AGR-5/6 qualification test fuel and margin to failure: Technical Program Plan https://inldigitallibrary.inl.gov/sites/sti/sti/Sort_61424.pdf . AGR-1 shakedown and "engineering scale particles and compacts" wording: DOE 2015 overview slides. VERIFY before lecture: the mapping of "engineering-scale" to AGR-2 (inferred from slide ordering), the "designed-to-fail" label for AGR-3/4 (plan refers to DTF fuel), and the specific role of AGR-7 (grouped with 5/6 here).

## Slide 24: AGR PIE and Safety Testing
Irradiated compacts are heated to high temperatures after irradiation to simulate accident conditions
  evaluates behavior during depressurized loss of forced cooling (D-LOFC) events
Fission gas release-to-birth ratios (R/B) monitored during irradiation
Fission product release measured from compacts (e.g., AGR-1 and AGR-2)
Locating and examining failed particles greatly improved understanding of fuel performance
Kernel and coating behavior characterized to support fuel performance models
Notes: Topics drawn from the 2023 AGR program overview (OSTI 2278790) https://www.osti.gov/biblio/2278790 . Specific safety test temperatures and failure fractions were not verified; pull numbers from that document or OSTI 1369357 if adding them.

## Slide 25: Interim Milestone: EPRI Topical Report
2002
AGR program
begins
May 2019
EPRI topical report
submitted to NRC
Aug 2020
NRC final safety
evaluation issued
Nov 2020
Approved report
published (-A)
EPRI-AR-1(NP) consolidates AGR-1 and AGR-2 results as a performance demonstration of UCO TRISO particles
NRC approval of the topical report is not qualification of the fuel; AGR-3/4 and AGR-5/6/7 provide further qualification data
Condition: applicants must evaluate discrepancies between their particles and the AGR particles (e.g., kernel size effects on stresses)
Notes: Submittal May 31, 2019 and SE letter August 11, 2020: EPRI transmittal letter https://www.nrc.gov/docs/ML2033/ML20336A053.pdf . Published -A version Nov 20, 2020 (EPRI TR 3002019978), package ML20336A052 https://www.nrc.gov/docs/ML2033/ML20336A052.html . Final SE ML20216A453 https://www.nrc.gov/docs/ML2021/ML20216A453.pdf . Condition 1 wording: NRC-CNSC TRISO Interim Report 2 https://www.nrc.gov/docs/ML2210/ML22101A297.pdf . Submitted report (AGR-1/AGR-2 basis): https://restservice.epri.com/publicdownload/000000003002015750/0/Product

## Slide 26: AGR Lessons for Qualification
About 18 years from program start (2002) to an approved topical report (2020), based only on AGR-1 and AGR-2
  an interim milestone, not fuel qualification; AGR-3/4 and AGR-5/6/7 were still required
A conventional, data-driven program, but with modern characterization, statistics, and modeling support
Qualification data transfer only within bounds
  the approval condition requires each applicant to justify that its particles match the tested population
Shows why fabrication specification is part of qualification: the data belong to a process, not just a material
Discussion: what parts of AGR could an AFQ approach shorten, and which could it not?
Notes: 18-year figure computed from 2002 program start and the August 2020 NRC SE on the AGR-1/AGR-2-based topical report. The topical report approval is not fuel qualification; qualification draws on the full program including AGR-3/4 and AGR-5/6/7. Remaining bullets are instructor synthesis.

## Slide 27: Metallic Fuel: NUREG/CR-7305
NRC-sponsored assessment of sodium-cooled fast-spectrum metallic fuel against the NUREG-2246 framework
Scope: U-10wt%Zr, up to 10 at% burnup
Documents the available experimental measurements, simulation capability, and historical knowledge and lessons learned
Connection to earlier lectures
  EBR-II and FFTF data form the legacy database
  the modeling gaps we discussed (redistribution, porosity, FCCI) are exactly what limits an evaluation model
Useful example of applying the framework to a fuel with a large but aging database
Notes: NUREG/CR-7305, "Metal Fuel Qualification: Fuel Assessment Using NRC NUREG-2246" (2023). Characterization of the modeling gaps as the limiting items is instructor framing; check the report conclusions before presenting.

## Slide 28: AFQ in Practice: GA-EMS FMR Fuel
GA-EMS is applying the AFQ methodology to Fast Modular Reactor (FMR) fuel
Target: qualify the new fuel in 5 years or less
Why AFQ is needed here
  target burnup is beyond the range of existing material property models (thermal conductivity, swelling)
  SiGA, a SiC-based cladding, is a new material for reactor applications
Approach pairs modeling and simulation with irradiation testing in a thermal reactor
  itself a non-prototypical condition for a fast reactor fuel
Notes: "Accelerated Fuel Qualification of Fast Modular Reactor Fuel in a Thermal Reactor: Modeling and Simulation Paired with Irradiation Testing," Nuclear Technology (2025), doi:10.1080/00295450.2025.2502283. Authors not verified. "SiC-based" description of SiGA is from general knowledge; verify.

## Slide 29: Structural materials code qualification

## Slide 30: Design Codes for Reactor Components
ASME Boiler and Pressure Vessel Code, Section III: rules for nuclear components
  Division 1: conventional (LWR-type) components
  Division 5: high temperature reactors
Division 5 applies where time-dependent (creep) behavior matters
  design allowables depend on both temperature and time
  creep and creep-fatigue damage must be evaluated
A material not listed in the code cannot simply be used in a code-stamped component
The regulator then endorses the code, with or without conditions
Notes: NRC endorsement of Division 5 is, I believe, through Regulatory Guide 1.87 Rev. 2, with conditions. Not verified; check the current revision.

## Slide 31: What Data Does a New Alloy Need?
Time-independent properties
  tensile, yield, physical properties over temperature
Time-dependent properties
  creep rupture and creep strain curves
  isochronous stress–strain curves
  creep-fatigue interaction
Weldments and product forms
  base metal behavior does not guarantee weld behavior
Thermal aging effects over design life
Environmental effects (coolant, impurities)
Multiple heats, to capture material variability
Notes: General list of Division 5-type data needs; instructor synthesis from general knowledge rather than a single cited source.

## Slide 32: Why It Takes So Long
Design lives of decades require extrapolating from much shorter tests
  long-term creep tests can run for years, and extrapolation must be justified
Data must be generated on multiple heats and product forms
Code committees must review and approve rules and allowables
Regulatory endorsement adds another step
Alloy 617 is the commonly cited example of a lengthy code qualification effort
Irradiation effects are handled with limited treatment in the code
  designers often must address irradiation effects separately
Notes: VERIFY: Alloy 617 Division 5 code case approval date (believed ~2020) and duration of the qualification effort. VERIFY: extent of irradiation-effects treatment in current Division 5 rules. Neither was verified.

## Slide 33: Connecting Fuel and Structural Qualification
Different processes, similar logic
  define the envelope, identify the controlling phenomena, generate data, build credible models
Both are bottlenecks for advanced reactor deployment
Both face the same tension
  accelerated and separate-effects data are faster
  the regulator and code bodies need confidence the data represent real service
Materials choices in design often reflect what is already qualified, not what is best

## Slide 34: Summary

## Slide 35: Summary
Qualification means high confidence that a material is made as specified and performs as the safety case claims, within a defined envelope
Traditional fuel qualification is empirical and sequential, historically 20+ years; the AGR TRISO program (AGR-1 through AGR-5/6/7) is the modern benchmark
NUREG-2246 provides a top-down framework: manufacturing parameters, performance envelope, evaluation models, data assessment
AFQ front-loads modeling and uses targeted separate-effects tests, but shifts the burden to model credibility
Lead test specimens allow operation to start before the full envelope is qualified
Structural alloys face a parallel, slow path through ASME Section III Division 5 and regulatory endorsement