## Slide 1: NE 763: Advanced Reactor Materials
Fall 2026
Dr. Benjamin Beeler

## Slide 2: Housekeeping
exam 2 grading completed and solutions posted to moodle
graded exams emailed out
avg of 92, thus, no curve
reminder to work on the presentations
exam 3 tentatively planned for first week of November (after the presentations)

## Slide 3: Last Time
Oxidizing conditions generated with fission:
  Excess fluorine generated due to fission, yielding oxidizing conditions
  Fission products take different forms (gaseous, precipitates, soluble salts)
  UF4/UF3 ratio is an indicator of redox potential
  Cover gas helps to remove fission products and control redox potential
Three principal corrosion processes:
  Reactions due to oxides on the metal; Reactions with dissolved impurities; Reactions with necessary constituents of the melt
  Rapid initial corrosion from impurities on surface or in salt; followed by Cr-diffusion-controlled corrosion
Different materials required for different systems, depending upon irradiation, temperature, salt exposure, etc.
Recent corrosion summary showed:
  purity of the salts is the primary factor impacting corrosion rates

## Slide 4: Need for molten salt data
The thermophysical properties of many of these salts are not well known for many of the fluoride salt systems of interest because of a lack of thermophysical property measurement data
If data are available for higher order systems, they are typically for only one (often the eutectic) or a handful of compositions of a particular system, providing little knowledge of how the thermophysical properties may change as functions of component concentrations and temperature
A primary reason for the lack of these thermophysical property data is the inherent difficulty in taking experimental measurements with fluoride salts, which tend to have high melting points, high corrosivity, and reactivity with oxygen and moisture
Because of these gaps, accurate thermal modeling of molten salt reactor designs is challenging, and safety evaluations may come with too high a degree of uncertainty

## Slide 5: Molten Salt Thermal Properties Database
Fundamental thermodynamic salt properties are pivotal in facilitating the development of multiscale and multiphysics reactor models for molten salt reactors
The MSTDB is a collection of thermal properties of molten salts relevant to the nuclear industry
Currently includes data for: Melting and boiling point, Density, Viscosity, Thermal conductivity, and Heat capacity
The current MSTDB-TP contains data for 811 different salt compositions
There is also a MSTDB-TC which includes phase diagrams

## Slide 6: Redlich-Kister expansion
The RK expansion can account for deviation from ideal mixing with the addition of an excess term
One way to increase the thermophysical understanding of these salt systems is by using estimation techniques
One method to quantify the pseudo-binary system interaction as it relates to salt density (and other properties) is use of a Redlich-Kister (RK) expansion
The choice to use an RK formalism for density estimation of molten salts has basis because excess molar volumes, which are directly related to density, have been commonly modeled using RK expansions

## Slide 7: Redlich-Kister expansion
The R-K approach shows improved predictions over assuming ideal mixing for both pseudo-binary and pseudo-ternary systems
Some systems can still present large errors, and need to be investigated through experiments or modeling to supplement the knowledge base
R-K models have also been extended to heat capacity and viscosity, and show similar improvements compared to ideal mixing
Density of NaF-LiFZrF4

## Slide 8: End of Molten Salts
Questions?

## Slide 9: Non-oxide ceramic fuels: Carbides and nitrides

## Slide 10: Why Carbides?
Possible fuel compositions with higher fissile atom density are non-oxide ceramics, for example, uranium–plutonium-mixed carbide or nitride
These fuels have higher thermal conductivity, high fissile heavy-atom density, and a high melting point compared to metallic fuel
The higher thermal conductivity of carbide fuel and high melting point makes carbide fuel suitable for operation at high power

## Slide 11: Why Carbides?
The more efficient heat transfer also allows for the possibility of large diameter fuel pins, with more fissile material per pin, and more power generation
High-specific-power operation permits fewer pins, compared to oxide, and a more compact core, which can reduce plant costs
Carbide fuel has a breeding ratio of at least 1.30, a doubling time of 15 years or less, and a burnup limit of more than 15 at.%
A large amount of development work on carbide and nitride fuels was performed from 1960 to 1970, and more than 5000 advanced fuel pins have been fabricated and irradiated
The practical difficulty of fabrication of carbide fuel hampered carbide development
The high-purity inert cover gas required for fuel fabrication was expensive and maintenance of C/M ratio was difficult

## Slide 12: Carbide Fuels: Reactor Applications
Sodium-cooled fast reactors (SFRs): (U,Pu)C demonstrated in India’s FBTR; newer PFBR uses MOX.
Gas-cooled fast reactors (GFRs): UC proposed for General Atomics EM² (SiC-clad fuel; conceptual design).
High-temperature gas reactors (HTGRs): UCO TRISO in X-energy Xe-100; licensing and fuel fabrication underway.
Nuclear thermal propulsion: (U,Zr,Nb)C under study for high-temperature hydrogen-cooled rocket reactors.
Carbide fuel cannot be used in LWR because of its incompatibility with the coolant
However, it can be safely used with liquid metal (Na or Pb) or gas (CO2 or He) coolants in Gen-IV reactors
Sources: IAEA (FBTR) | DOE (EM²) | DOE (Xe-100) | NASA (NTP)
1

## Slide 13: Fast Breeder Test Reactor (FBTR)
40 MWt (13.2 MWe) Na-cooled test reactor, Kalpakkam; critical October 1985
Rapsodie-based design (loop-type SFR); Pu-rich carbide fuel
Only reactor to run on a full mixed-carbide driver core
He-bonded pins, cold-worked SS316 clad
  Mark I: (U0.3Pu0.7)C; Mark II: (U0.45Pu0.55)C
Mark I: >2000 pins at 155 GWd/t; lead subassembly at 165 GWd/t (~16.5% FIMA)
  155 GWd/t limit: clad ductility, wrapper dilation, porosity exhaustion
  Only one pin failure, judged to be random
40 MWt since 2022
PFBR (500 MWe, critical April 2026) uses MOX

## Slide 14: US Interest in Carbide Fuels
Many laboratories in the world were engaged in studies on the development of carbide fuels based on uranium, plutonium, and thorium
After the oil crisis in 1974, a national advanced liquid-metal-cooled FBR fuels development program was initiated that built upon early years of carbide fuel development
Both carbide and nitride fuels offer a middle ground for LMFBR performance because of their higher thermal conductivity, fissile-atom density, and chemical compatibility with liquid sodium, and much higher melting point than metallic fuels

## Slide 15: Carbide Pin Designs
There are two concepts available for the carbide fuel pin depending upon the type of bond between the fuel pellet and the cladding material: He-bonded and Na-bonded carbide fuels
The average operating fuel temperature of the He-bonded pin is high because of low thermal conductivity of the He bond compared to the Na bond
This design requires a larger fuel–clad gap and an 85%TD pellet density to accommodate the swelling of the fuel
The fission gas release in a He-bonded pin will be higher compared to that from a sodium-bonded pin, due to the higher temperatures
Na-bonded carbide fuel pins also require a reduced smear density compared to oxide fuels to account for fuel swelling
The purity of the Na bond is very important, requiring strict tolerances on O content

## Slide 16: Fuel Density Definitions
Theoretical density (TD): density of a perfect, pore-free crystal; a fixed material property
  (U,Pu)N: 14.3 g/cm3; (U,Pu)C: 13.6 g/cm3
Pellet density: actual density of the fabricated pellet, as % TD
  Porosity = 100% − pellet %TD
Smear density (SD): fuel mass averaged over the entire clad interior, as % TD
  SD = (pellet %TD) × (rpellet / rclad,in)2
  Pores and gap both accommodate swelling
He-bonded: low pellet density, small gap
Na-bonded: high pellet density, large gap
  Both reach SD of ~70–80% TD
Theoretical density
Pore-free crystal;
material constant
Pellet density
Pores lower density;
quoted as % TD
Smear density
Pores + gap; fuel spread
over clad interior, % TD
Fuel
Pore / gap
Cladding
Example: German reference He-bonded carbide pin
84% TD pellet, 7.0 mm diameter, 7.4 mm clad ID
SD = 0.84 × (7.0/7.4)2 ≈ 0.75 → 75% TD

## Slide 17: Carbide Fuel Details
A hyperstoichiometric (C/M>1, carbon to metal ratio) fuel composition is chosen so that it contains some amount of sesquicarbide M2C3 phase (M=U+Pu), which accounts for the decrease in (C/M) ratio with burnup
Why would C/M decrease with burnup?
A low C/M ratio may result in the formation of actinide metal phases, which may form low-melting eutectics with the cladding and limit the life of the fuel pin
FCMI can potentially exist, depending upon the operating temperature of the fuel
O and N impurities play important roles, as they act as ‘carbon equivalent’, which affect the carbon potential of the fuel
Also have high Pu and low Pu designs, which impact properties and impurity sensitivity

## Slide 18: Carbide Fuel Details
Carbide fuels have higher swelling and lower fission gas release than oxide fuels
This is due to the lower fuel temperatures (higher thermal conductivity), and the microstructural evolution of fission gases
However, carbide fuels go to significantly higher burnups, leading to larger fission product inventories
Burnup limits are imposed by cladding stresses/damage due to fission gas pressure and FCMI

## Slide 19: Questions on carbide fuel overview?

## Slide 20: U(Pu)-C Phases
Uranium forms three compounds with carbon: UC, U2C3, and UC2, with only U2C3 being stoichiometric
UC is stable over a wide temperature and composition range
UC2 is stable in two high temperature phases
The Pu–C system has four compounds: Pu3C2, PuC1–x, Pu2C3, and PuC2
UC and PuC are face-centered cubic structures (NaCl-type)

## Slide 21: U/Pu-C Phase

## Slide 22: U/Pu2-C3
This structure is more complex than that of the mono- and dicarbides, and is often difficult to form
U2C3 is produced by a complex preparation procedure and decomposes into a mixture of mono- and dicarbides at high temperatures

## Slide 23: Phase Diagrams of Carbides
The differences in the UC/PuC diagrams are mainly due to (i) the presence of Pu3C2 compound, (ii) the low thermal stability of PuC compared to UC, and (iii) the high stability of Pu2C3 compared to U2C3

## Slide 24: Phase Properties
The brittleness of the monocarbides is due to alternate close-packed planes of metal and nonmetal atoms, restricting the slip and thereby hardening the crystal
Many fission products are not soluble in the monocarbide lattice due to the nature of the carbon bonding
The high density and low FP solubility of UC leads to higher swelling than UO2
The U2C3 phase has more open space in the structure, and generally has less swelling than UC
An increase in O and N impurities results in an increase of carbon activity and CO pressure of the fuel
O impurities are also known to contribute to the actinide redistribution in carbide fuels and fuel restructuring during burnup

## Slide 25: Key Properties
The thermophysical properties that are of importance and affect the fuel performance are solidus/liquidus temperature, thermal conductivity, coefficient of thermal expansion, elastic/fracture properties, creep, and hardness at ambient and at high temperatures
The solidus/liquidus temperatures along with thermal conductivity limit the fuel operating temperature in terms of linear heating rate
Thermal conductivity varies as a function of density, porosity (shape, size, and distribution), composition, presence of a second phase, grain size, etc.
Coefficient of thermal expansion is an important design parameter, the stresses generated in the fuel and by the fuel in the cladding are partly due to the difference in the CTE between the fuel and the cladding

## Slide 26: Key Properties
The elastic and fracture properties of the fuel are primarily responsible for the extent and severity of FCMI
Both thermal-induced and irradiation- induced creep of the fuel also determine the extent of FCMI
Mechanical and creep properties depend on composition, second phases, grain size, etc.
Pu lowers melting point, decreases thermal conductivity, increases expansion, and softens the fuel

## Slide 27: In-pile behavior
The in-pile fuel behavior depends to a large extent on the fuel operating temperature, which in turn depends on the type of pin or bond concept, namely, He-bonded fuel or Na-bonded fuel
A large number of mixed carbide fuels have been irradiated in the US, Europe, Russia, India, and Japan
The performance analysis of the mixed carbide fuel can be best understood based on their burnup period, the structural changes occurring during the burnup, and subsequently the swelling of the pin

## Slide 28: Burnup Stages
This is for He-bonded fuels
Stage A: At the BOL, the fuel undergoes cracking, which results in the movement of the fragmented fuel toward the cladding surface
The fuel–clad gap partly reduces but does not close
Fuel sees a dramatic increase in temperature due to cracking
Stage A lasts for a few days

## Slide 29: Burnup Stages
Stage B: Fuel undergoes unrestrained free swelling, crack healing, or resintering
Resintering/densification occurs for thermally unstable (high Pu high O) or low-density fuels, which causes an initial increase in gap size resulting in the rise in the fuel surface temperature
In stage B, free swelling occurs and crack healing starts, which results in the relocation of fuel fragments further from the center of the fuel to the periphery
Swelling causes fuel–clad gap closure, increase in heat transfer coefficient, and decrease in fuel surface temperature
Surface roughness of fuel and cladding limits complete gap closure
FCMI begins due to the swelling of the fuel
Stage B ends after a burnup of approximately 3 at.%

## Slide 30: Burnup Stages
Stage C
This stage starts after fuel–clad gap closure when a steady minimum surface temperature is reached, and it continues until the end of fuel life
For carbide fuel, this could be up to 15 at.%
At this stage, more homogeneous fuel–cladding interaction starts