## Slide 1: Nuclear Fuel Performance
NE-533
Spring 2023

## Slide 2: Notes on MOOSE final project
Final report
Has a discussion of all three parts in a more “complete” form
Includes presentation and analysis of results
Max of 10 pages
All final input/output files should be uploaded to moodle submission

## Slide 3: Last time
MOX Transients:
  Three main types of transient of interest in MOX SFRs: slow power transient (CRWA), blockage of a subassembly, unprotected loss of flow accident
  Fuel melting is one of the most critical concerns
Metallic fuel: U-Zr alloys
  Metal fuel can go to high burnup, good accident performance, inherent safety, easy to make
  Complex phase and composition environment, rapid, substantial swelling, followed by fission gas release, FCCI limits lifetime

## Slide 4: TRISO Fuel Performance

## Slide 5: High Temperature Gas Reactor TRISO Fuel
The HTGR fuel concept is based on TRISO fuel particles embedded in a graphite matrix
The core of a modular design (~500 MWth) contains approximately 1 billion TRISO particles
Coated particles have changed throughout the years, but have converged on the current TRISO particle concept

## Slide 6: TRISO Layers Purpose
Fuel kernel: fissile material, generates heat; typically UO2 or mixture of UO2 and UC (uranium oxycarbide : UCO); UC or UN are also fuel kernel materials
Buffer: Porous graphite with ~50% theoretical density; serves as a gas plenum to accommodate fission gases; removes stresses from fuel swelling; sacrificial layer for fission product damage
IPyC: pyrolytic carbon; load bearing layer against kernel internal pressure; protects fuel kernel during fabrication; retains most fission products
SiC: silicon carbide; main fission product barrier; load bearing layer
OPyC: pyrolytic carbon; protects the SiC during handling and compaction; further diffusion barrier for fission products; load bearing layer

## Slide 7: Phenomena in TRISO
Pressure build-up:
  Fission liberates oxygen which can bind to the carbon buffer and form CO
  Suppression of excess CO formation is especially critical for high burnup
  In the US, UCO fuel is used to allow for the conversion of UC2 into UO2 in the fuel kernel, controlling excess oxygen and limiting the CO production
Irradiation growth
  Fuel kernel will swell as a function of time, while the buffer layer will shrink
  PyC layers will initially shrink under irradiation, but will eventually reach a turnaround point where swelling will occur
  Radial swelling of PyC layers puts the SiC into compression
  Irradiation creep will eventually work to relieve stresses in the PyC layers

## Slide 8: Phenomena in TRISO
Kernel migration
  the movement of the kernel toward the TRISO coating, also known as the amoeba effect, may lead to a failure of the particle coating if the kernel reaches the iPyC layer
  The phenomenon is associated with carbon transport in the particle in the presence of a temperature gradient
  More likely to occur in oxide fuels due to the presence of free O, forming CO gas

## Slide 9: Phenomena in TRISO
Pressure vessel failure
  The inner pressure buildup from both fission gases and the CO increases with burnup and results in tensile stresses on the coating layers of the particle
  If these stresses exceed the tensile strength of the coating, it will burst into pieces
  Assuming that fabrication specifications are met, particle failure should not occur

## Slide 10: TRISO Pressure Vessel
The SiC represents the pressure vessel wall which will fail as soon as the stress induced in the SiC layer by the internal gas pressure exceeds the tensile strength of the SiC
Initially stresses in the SiC layer are compressive because of the attempted shrinkage of the two PyC layers, but as the gas pressure increases, they become tensile until failure occurs
While stresses in the OPyC vary little during the course of the irradiation, they decrease in the IPyC layer because of an increasing compressive component from increasing gas pressure

## Slide 11: Phenomena in TRISO
Fission product attack
  experiments show that noble metals can be transported to the SiC, where they can chemically interact
  Pd-Si compounds can form and lead to degradation of the SiC layer
  Ag has been observed to diffuse through intact SiC layers
  If the IPyC is cracked, CO formed can interact with SiC to for SiO gas, degrading the SiC layer
SiC thinning rates due to Pd corrosion

## Slide 12: Fuel Performance Codes
Primary FP codes in the US are PARFUME and BISON
  PARFUME is a mechanistic thermomechanical code that determines the failure probability of a population of fuel particles
  BISON utilized PARFUME as a basis to develop a fully 3-D mechanistic fuel performance model
The NRC has modified the FAST code to include FAST-TRISO
  1-D thermomechanics, material properties, failure modes
Failure modes that need to be captured: 1) Cracking of the IPyC layer; 2) Partial debonding of the IPyC from the SiC; 3) Pressure vessel failure of an aspherical particle; 4) Kernel/SiC interaction resulting from the Amoeba effect; 5) Thinning of the SiC layer by palladium attack of the SiC.

## Slide 13: Summary
Quick overview of TRISO fuel performance
The failure mechanisms and performance limits of reference HTGR fuels as a function of particle design parameters are relatively well established
Fuel fabrication and quality assurance is key to retention of fission products
A few fuel performance codes exist, but experimental data is limited for benchmarking
The Advanced Gas Reactor (AGR) program and experiments (AGR 1-7) are providing data for qualification