## Slide 1: NE 763: Advanced Reactor Materials
Fall 2025
Dr. Benjamin Beeler

## Slide 2: Exam Results

## Slide 3: Paper Presentation Assignment
A topic related to advanced reactor materials will be assigned and the student will present a presentation summarizing the topic area. Students will be evaluated on the technical content and the presentation/organization of the content.
Twenty minutes maximum (15 for talk, 5 for questions)
Conducted in class, slides uploaded day before presentations begin
Presentations on October 16 and 21

## Slide 4: Presentation topic assignments:
Alexandra Doherty: Cermet fuel concept and applications
Anthony Cowan: Corrosion in supercritical water-cooled reactors
Cecilia Harrison: SiC as a cladding material (non-TRISO applications)
Gwen White: Swelling of stainless steel under fast fluence
Josephine Hartmann: Corrosion of stainless steel in chloride salts
Kyle Holloway: Inert matrix actinide-bearing fuel concepts
Rashed Almasri: High temperature materials for gas reactor heat exchangers
Emily Quisenberry: Alternate geometries of metallic fuels (e.g., slotted, annular, etc.)
Justin Yarrington: Borosilicate waste glasses

## Slide 5: Last Time
Constituent redistribution in UZr
  thermodynamic and Soret diffusion effects
Different porosities in different phases
Thermal conductivity degrades with porosity, but increases with sodium infiltration
Fuel cladding mechanical and chemical interaction
FCMI limited by low smear density and large plenum
  swelling due to fission gas and solid fission products
FCCI is a complex thermodynamic and kinetic process
  low melting phases can be studied with diffusion couples

## Slide 6: Changes in Thermal Conductivity
U-Zr has a very high thermal conductivity compared to oxide fuels
However, developing porosity will degrade the thermal conductivity
Understanding the temperature also governs how our porosity will develop and how redistribution will vary axially
This is a coupled problem that is complex, but critical for prediction of fuel evolution

## Slide 7: Changes in Thermal Conductivity
Bond sodium plays an important role on the thermal behavior of the fuel during irradiation
At the point where the fuel reaches its maximum swelling the porosity in most of the fuel interconnects and gas is vented to the plenum
This allows the bond sodium to infiltrate the fuel body and increase the fuel’s overall thermal conductivity
Sodium infiltration is known because in PIE, the sodium level above the fuel elements, where the fuel has swelled out to the cladding, is always substantially lower than the total amount of preloaded sodium would indicate
Chemical analysis of irradiated fuel finds this “missing” sodium distributed throughout the fuel pin

## Slide 8: Changes in Thermal Conductivity
On average, approximately 15–20% of the porosity is filled with sodium
The overall thermal conductivity of the fuel drops continuously during the early free-swelling stage, due to porosity development, but then increases rather suddenly with gas release and sodium logging
Experiments at right had thermocouples in the center of the fuel

## Slide 9: Fuel-Cladding Interaction
Fuel-Cladding interactions are both mechanical and chemical in nature (FCMI and FCCI)
FCMI results from when the fuel swells, comes into contact with the cladding, and exerts an outward force on the cladding
Early element designs did not allow the fuel sufficient free swelling, this gas bubble pressure was transmitted directly to the cladding
Thus, all early designs suffered from cladding deformation and rupture at modest burnups
This was one of the primary reasons oxide fuels were pursued over metallic alloys
By the time the smear density solution had been implemented, metallic fuels had already been left behind

## Slide 10: Fuel-Cladding Mechanical Interaction
The cladding strain of low smear density, small plenum fuel rod designs is primarily creep strain due to FCMI (MK-I)
The cladding strain of high smear density, large plenum rods is mainly irradiation-induced cladding swelling (MK-II)
The creep strain can be accounted for by the plenum pressure stress alone, which confirms that FCMI is virtually nonexistent in suitably designed metallic fuel elements
Significant FCMI can be avoided to high burnup if the as-built fuel smeared density is kept to 75%, and a sufficient gas plenum is employed

## Slide 11: Fission-Induced Creep
Stress in the cladding due to fuel swelling will thus also depend on the effective creep rate of the fuel in-reactor
Measurable creep deformation of α-U during fissioning at temperatures where classical creep does not exist has been experimentally identified
These studies clearly established that at low temperature, the in-reactor creep rate of U is independent of temperature and linearly dependent on both stress and fission rate

## Slide 12: Fission Product Swelling
Post-irradiation examinations of high burnup fuel appear largely to support both partitioning into subgroups and assumptions of fission product behavior
A reason for partitioning these fission products is their different migration behavior in the fuel; such grouping allows an evaluation of this migration on the properties of the various radial phasal zones
Zr, Nb, and Mo are all in solution in the fuel phases
Alkali elements (Cs) are dissolved to some extent in the bond sodium
The noble metals (Pt) precipitate as compounds
The rare earths (Nd) precipitate as a separate compound or alloy
The majority of the alkaline (Sr) earths precipitate separately

## Slide 13: Fission Product Swelling
The accommodation of the nonsoluble fission products predictably results in a volume expansion as a function of burnup
As U and Pu are removed from the lattice as they fission, this results in a volume decrease that partially offsets the volume expansion due to fission products
Since Zr, Nb and Mo are soluble in the matrix, this compensates for some of the volume decrease due to the disappearance of U and Pu
The result of these contributions is an associated volume change of 0.2 vol.% per percent burnup

## Slide 14: Fission Product Swelling
The rare earths are found to collect in two separate phases in primarily large pores towards the periphery of the fuel and in gaps between the fuel and cladding
A chemical analysis of the bond sodium indicated that a major fraction of the alkali, and also some of the alkaline earth elements, can simply be added to the bond sodium volume

## Slide 15: Fission Product Swelling
The total volume of the nonsoluble fission products amounts to approximately 1.2% fuel volume increase per percent burnup

## Slide 16: Fuel-Cladding Chemical Interaction
FCCI is a complex multicomponent diffusion and thermodynamic problem
The characterization of fuel-cladding interdiffusion is exceedingly difficult because of the number of alloy components involved
Fuel element species, minor alloy additions (C, N, O) and fission products all play a role in FCCI
The potential problem of interdiffusion of fuel and cladding components is essentially twofold: (i) a weakening of the cladding’s mechanical properties; and (ii) the formation of relatively low melting point compositions in the fuel
Typically, diffusion couple experiments have been performed to try to evaluate these effects

## Slide 17: Fuel-Cladding Chemical Interaction
Experiments in the 1960s showed that the addition of Zr showed a decrease in diffusion rates and an increase minimum melting temperature
Additions of Pu accelerate the rate of attack and low possible melting points
This is one of the basis for which Zr was selected as the alloying element for “modern” metallic fuel

## Slide 18: Phase Diagrams for FCCI
To gain initial insight into the phases that may develop at the FC interface, one can look at available equilibrium phase diagrams, even though the irradiation process deviates from equilibrium
Phase diagrams can indicate the intermetallic phases present, the solid-solubility ranges in different phase regions, and the temperatures and compositions at which liquid phases develop
The intermetallic phases that are present in phase diagrams can form in the interaction zones during the interdiffusion process; wide ranges of solubility in terminal alloys can be an indication that interdiffusion rates may be high; and knowing the compositions of the low-melting phases is beneficial provides knowledge of potentially limiting conditions

## Slide 19: Phase Diagrams for FCCI
The U-Fe and Pu-Fe phase diagrams
Intermetallic UFe2 and U6Fe phases are present in the U–Fe phase diagram and PuFe2 and Pu6Fe phase are present in the Pu–Fe system
These are likely phases to form
These systems also undergo eutectic melting at temperatures as low as ~700K

## Slide 20: Phase Diagrams for FCCI
Addition of Zr towards U-Fe-Ze and U-Pu-Fe-Zr phase diagrams
Fe3Zr, Fe2Zr, FeZr2, and FeZr3 are intermetallic phases capable of forming in the FCCI zone
Continuous solid solutions have been reported between Pu6Fe and U6Fe and between PuFe2 and UFe2 2: (U,Pu)6Fe and (U, Pu)Fe2

## Slide 21: Diffusion Couples
Out-of-pile diffusion couple experiments are typically conducted to determine the interdiffusion behavior of the various constituents at a temperature of interest
Test have been performed with U–Fs, U–Pu–Fs, U–Zr, and U–Pu–Zr and different cladding alloys
Diffusion couple experiments have indicated that a eutectic phase can form in FCCI zones at temperatures near 700C, and this phase is similar to U–Fe6

## Slide 22: Protective Rind
Impurities in the fuel or cladding alloys have been suggested to play a role in determining the FCCI behavior
If enough impurities are present (e.g., C, O, or N), then Zr-rich layers that are stabilized by impurities can develop at the interface and impede the interdiffusion process
The extent of the formation would depend on the oxygen activity in the cladding
Work has been performed on U–Zr alloys to investigate the development of nitride layers with a N2 cover gas
This has been related to the rind and rind interactions with FCCI
The rind can form during a casting process due to the atmosphere and crucible/mold
It form on the exterior of the fuel slug, almost like a coating

## Slide 23: FCCI
The interaction zone formation in irradiated metallic fuel elements is localized
Typically, the largest interaction zones in fuel elements are created when a wedge-shaped crack forms in the fuel adjacent to the inner surface of the cladding and a large fission product deposit (primarily Nd, Ce, and La) develops

## Slide 24: FCCI
In many of the analyzed fuel elements, fuel–cladding interaction can be linked to the integrity of the Zr-rind
In the image, arrows indicate areas where rind is no longer intact
Both temperature and power variations along the length of a fuel element appear to impact the amount of fuel–cladding interaction that will occur
The maximum fuel–cladding interaction is observed in the combined high-temperature and high-power region of a fuel element

## Slide 25: FCCI
The burnup of a fuel pin is another parameter that impacts the size of the fuel–cladding interaction zone
Larger interaction zones are observed for higher burnup fuel elements
The larger inventories of fission products allow more lanthanides to diffuse down the temperature gradient, thereby increasing the inventory of fission products at the interface
For high burnup fuels, temperature effects also exacerbate FCCI due to thermal cond. degradation producing higher temperatures, and more rapid FP diffusion
Fuel elements at the hotter core positions can exhibit increased interdiffusion at the fuel–cladding interface over those at colder positions

## Slide 26: Summary
Radial redistribution of chemical species driven by thermodynamics and Soret diffusion
Include large plenum to accommodate fission gas release
Thermal conductivity degradation
  fission gas swelling/porosity, sodium infiltration
Fuel-cladding mechanical interaction
  fuel swelling, creep, internal pressure, etc.
Fuel-cladding chemical interaction
  phase diagrams and kinetics, low melting points, intermetallics, etc.

## Slide 27: FCCI
The burnup of a fuel pin is another parameter that impacts the size of the fuel–cladding interaction zone
Larger interaction zones are observed for higher burnup fuel elements
The larger inventories of fission products allow more lanthanides to diffuse down the temperature gradient, thereby increasing the inventory of fission products at the interface
For high burnup fuels, temperature effects also exacerbate FCCI due to thermal cond. degradation producing higher temperatures, and more rapid FP diffusion
Fuel elements at the hotter core positions can exhibit increased interdiffusion at the fuel–cladding interface over those at colder positions

## Slide 28: FCCI Compositions
Fe and Cr are the major constituents in HT-9 cladding and should show up as major constituents in the FCCI zones of irradiated HT-9-clad fuel elements
For D9-clad fuel elements, Fe, Ni, and Cr are major constituents that should be present in FCCI zones
There have been some irradiated fuel samples that were specifically destructively analyzed to observe FCCI
The lowest and highest determined temperatures at the fuel–cladding interface were 540 and 660 C, respectively
The thickest interaction zone measured was 170 mm, and the lanthanide fission products were the primary fuel constituents observed in the interaction layers

## Slide 29: FCCI Examinations

## Slide 30: FCCI Compositions
Element DP-16 was the only fuel element in which a sample was generated for analysis using SEM/EDS, in addition to the more typical OM and EPMA analyses usually performed on fuel elements
U-16Pu-23Zr and HT-9 cladding
X-ray analysis maps at the right
(b) U, (c) Pu, (d) Zr, (e) Fe, (f) Cr

## Slide 31: FCCI Compositions
X-ray map for fission products
EPMA analysis for key species
Fe diffuses into the fuel, Ce and Nd diffuse into the cladding, and Pd enriches in localized areas of the fuel near the fuel–cladding interface
The lanthanides penetrated the farthest into the cladding (40 mm) of any components originating in the fuel
(g) Ce, (h) Nd, (i) Ru, and (j) Pd

## Slide 32: FCCI Compositions
The DP-11 fuel element was irradiated to about 10 at.% burnup at elevated cladding temperatures (630–660 C), binary U-Zr
There is a 50-mm-wide zone of the cladding that is high in Cr and low in Fe and Ni
In the fuel, Fe has interdiffused around 250 mm
In the cladding band containing high Cr and low Fe and Ni, lanthanide concentrations are elevated

## Slide 33: FCCI
A variety of phases have been observed to form locally where swelled fuel has contacted the cladding
At the interface between the fuel and the cladding, the observed phases on both sides combine the cladding elements Fe, Ni, and Cr with the fuel components U, Zr, and Pu and the lanthanide fission products
In the cladding, the developed phases are enriched with cladding components, and they contain differing amounts of the primary fuel components and fission product components
Lanthanides penetrate farthest into the cladding, specifically Ce and Nd
Fe and Ni depletion zones are observed in all the fuel elements

## Slide 34: FCCI
In the fuel, some phases are observed that are enriched with the fuel constituents and contain Fe or Ni as the major nonfuel or components
Other phases are observed that primarily contain lanthanides
The interaction zone formation is localized
Temperature and power variations along the length of a fuel element appear to impact the amount of FCCI that occurs
Two different locations in DP-16

## Slide 35: Melting Experiments
One potentially significant impact that the presence of FCCI zones is the melting of phases inside the cladding
This will limit the allowable coolant temperature that can be used for the reactor, but it can become more important when considering transients and accidents
This illustrates the effect of the relatively low quantities of Fe required to cause melting on the uranium-rich side of the U–Fe phase diagram
In general, no liquid phase formation is observed below heating at 700C

## Slide 36: Metal fuel fabrication

## Slide 37: Metal Fuel Fabrication
Injection casting has been utilized for fuel slug fabrication
Remote fabrication has been performed inside a hot cell on recovered uranium
Fuel slugs for EBR II and FFTF were fabrication via injection casting

## Slide 38: Metal Fuel Fabrication
Starting materials are charged into the graphite crucible in the furnace
Silica molds with tops closed are set above the crucible
Crucible is coated with yttria
Molds coated with zirconia

## Slide 39: Metal Fuel Fabrication
Furnace closed and filled with Ar gas
Crucible is inductively heated to 1830K, and stirred electromagnetically
Ar gas removed, molds are lowered, then Ar gas returned
Pressure difference injects the melt into the molds

## Slide 40: Closing the Fuel Cycle
An important factor in selecting a fuel form for fast reactors is ease of fuel recycling, including reprocessing and fuel refabrication
Pyrometallurgical processing, called ‘melt refining,’ can be combined with refining techniques to recycle spent metallic fuel
This recycling process has been demonstrated for uranium alloy fuels in the 1960s, where fuel alloys were recycled as many as four times, and the fuel was returned to the reactor within 4–6 weeks of its removal from the reactor core

## Slide 41: Reprocessing
Pyroprocessing
For more than 50 years, pyrometallurgy has been studied as an alternative strategy in the reprocessing of used fuel
Pyrochemical processes rely on refining techniques at high temperature (500–900 C) depending on the molten salt eutectic used
Typically, chloride systems operate at lower temperature compared to fluoride systems, and are preferred in processing
These processes are mainly based on electrorefining or on extraction from the molten salt phase into liquid metal
Two processes-one for oxide fuel and one for metallic fuel-have been developed to near industrial scale

## Slide 42: IFR Pyroprocess
This process was developed in the US to be part of the IFR project, and can handle the treatment of transuranics
The fuel is recycled using an electrochemical process based on molten chloride salts and liquid metals
The molten salt medium for electrorefining is a solution of a certain amount of UCl3 dissolved in a LiCl–KCl eutectic

## Slide 43: IFR Pyroprocess
The fuel is electrochemically dissolved using a potential between the basket (loaded with used fuel) as anode and a stainless steel electrode in the salt as the cathode
Uranium and TRU are deposited on the cathodes
Once the fuel is dissolved and most of the uranium is deposited on the solid steel, this cathode is replaced by a liquid cadmium cathode, and the remaining TRUs can be co-deposited with the remaining uranium

## Slide 44: IFR Pyroprocess
The alkali, alkaline earth, rare earth, and halide FPs remain primarily dissolved in the salt phase
More than 90% of the noble metal FPs and fuel alloy material are retained in the chopped fuel cladding segments in the anode baskets
Can reduce the repository burden of radioactive waste by separating long-lived MA from spent light-water reactor fuel, burning MA in fast reactors, and decreasing the long-term radioactivity of nuclear waste

## Slide 45: Refabrication
Metal-fueled fast reactors facilitate the effective transmutation of MA because of the high-energy neutron spectrum
One of the measures to load MA into the reactor core is to add MA to the fuel alloy homogeneously
Can perform injection casting in the same manner as the fresh fuel, to form MA-bearing fuel alloys
These technologies are expected to reduce the fuel cycle cost even for small-scale fuel cycle plants because of the simplicity of the process and the compactness of the equipment
For example, in the injection casting process, composition adjustment, melting (alloying), and casting of the fuel slug can be done in a single injection-casting furnace

## Slide 46: Metallic fuel performance modeling

## Slide 47: Metallic Fuel Phenomena

## Slide 48: Constituent Redistribution Models
Constituent redistribution is driven by:
  temperature gradients in the fuel,
  solubility gradients in a phase and phase boundaries,
  additional chemical potentials applied by fuel– cladding gap and cladding
Results in three concentric zones, namely, a Zr-enriched central zone, a Zr-depleted and U-enriched intermediate zone, and a slightly Zr-enriched zone on the outer periphery
Migration quickly levels off early in life after a new distribution settles

## Slide 49: Constituent Redistribution Models
While ternary phase diagrams exist, their accuracy is suspect, and simplified pseudo-binary phase diagrams can be more easily implemented, and removes complexities associated with largely unknown phases
When applied to a fuel with different Pu content, the phase diagram must be modified accordingly

## Slide 50: Constituent Redistribution Models
Using the calculated phase fractions, the Fickian and Soret diffusion coefficient are determined
Artificial factors are used to set the diffusivity in two-phase regions and to scale diffusivities in each phase
The magnitudes of diffusivities in each phase are largely unknown, and effectively wholly unknown in two-phase regions
BISON Zr Diffusion Model

## Slide 51: Temperature Predictions
Constituent redistribution relies on accurate temperature profiles
Fuel temperature is affected by the thermal conductivity of the fuel, which in turn is changed by porosity evolution and sodium infiltration, in addition to changes in Zr concentration
BISON thermal conductivity models exist for the distinct phases/species, and account for degradation of thermal conductivity

## Slide 52: Porosity Predictions
BISON utilizes a simplified model for porosity
The mechanical force balance on an equilibrium bubble can be expressed by the Young-Laplace equation
Making assumptions for creep stress, bubble size, can calculate swelling due to fission gas
Finally, can determine porosity from the swelling
Solid fission products are a function of fission density

## Slide 53: Porosity Predictions
These porosity models don’t incorporate different phases, initial porosity, axial/radial swelling, etc.
These models have been updated slightly to improve code robustness, but still don’t incorporate these critical microstructural phenomena

## Slide 54: Mechanical Properties
Young’s Modulus
Poisson’s ratio
Creep
Cladding models for HT-9 creep and kth

## Slide 55: BISON Testing
BISON can handle binary and ternary fuel and compare reasonably well with EBR-II data
Discrepancies are due to inadequate knowledge of materials models, and underlying issues with material descriptions, and code robustness
Development is ongoing, and improvements to swelling models, for example, have been made

## Slide 56: Other Codes
LIFEMETAL
The code has evolved from the LIFE series of codes from ANL that perform steady-state and transient analyses for nuclear fuel
The original code was developed for UO2 and mixed oxide fuels for use in fast reactor systems
The code was developed in association with the IFR and has been extensively used for planning steady state and transient experiments at EBR-II

## Slide 57: Other Codes
ALFUS
JAEA code that is multiphysics in nature and focuses on the mechanical behavior of the fuel under irradiation
Both LIFE-METAL and ALFUS are capable of simulating metal fuel irradiation behavior to some extent
Both lack different swelling in different radial zone, coupling of redistribution, realistic predictions of FCCI

## Slide 58: Questions?