## Slide 1: NE 763: Advanced Reactor Materials
Fall 2025
Dr. Benjamin Beeler

## Slide 2: Last Time
Oxidizing conditions generated with fission:
  Excess fluorine generated due to fission, yielding oxidizing conditions
  Fission products take different forms (gaseous, precipitates, soluble salts)
  UF4/UF3 ratio is an indicator of redox potential
  Cover gas helps to remove fission products and control redox potential
Three principal corrosion processes:
  Reactions due to oxides on the metal; Reactions with dissolved impurities; Reactions with necessary constituents of the melt
  Rapid initial corrosion from impurities on surface or in salt; followed by Cr-diffusion-controlled corrosion
Different materials required for different systems, depending upon irradiation, temperature, salt exposure, etc.
Recent corrosion summary showed:
  purity of the salts is the primary factor impacting corrosion rates

## Slide 3: Need for molten salt data
The thermophysical properties of many of these salts are not well known for many of the fluoride salt systems of interest because of a lack of thermophysical property measurement data
If data are available for higher order systems, they are typically for only one (often the eutectic) or a handful of compositions of a particular system, providing little knowledge of how the thermophysical properties may change as functions of component concentrations and temperature
A primary reason for the lack of these thermophysical property data is the inherent difficulty in taking experimental measurements with fluoride salts, which tend to have high melting points, high corrosivity, and reactivity with oxygen and moisture
Because of these gaps, accurate thermal modeling of molten salt reactor designs is challenging, and safety evaluations may come with too high a degree of uncertainty

## Slide 4: Molten Salt Thermal Properties Database
Fundamental thermodynamic salt properties are pivotal in facilitating the development of multiscale and multiphysics reactor models for molten salt reactors
The MSTDB is a collection of thermal properties of molten salts relevant to the nuclear industry
Currently includes data for: Melting and boiling point, Density, Viscosity, Thermal conductivity, and Heat capacity
The current MSTDB-TP contains data for 811 different salt compositions
There is also a MSTDB-TC which includes phase diagrams

## Slide 5: Redlich-Kister expansion
The RK expansion can account for deviation from ideal mixing with the addition of an excess term
One way to increase the thermophysical understanding of these salt systems is by using estimation techniques
One method to quantify the pseudo-binary system interaction as it relates to salt density (and other properties) is use of a Redlich-Kister (RK) expansion
The choice to use an RK formalism for density estimation of molten salts has basis because excess molar volumes, which are directly related to density, have been commonly modeled using RK expansions

## Slide 6: Redlich-Kister expansion
The R-K approach shows improved predictions over assuming ideal mixing for both pseudo-binary and pseudo-ternary systems
Some systems can still present large errors, and need to be investigated through experiments or modeling to supplement the knowledge base
R-K models have also been extended to heat capacity and viscosity, and show similar improvements compared to ideal mixing
Density of NaF-LiFZrF4

## Slide 7: End of Molten Salts
Questions?

## Slide 8: Non-oxide ceramic fuels: Carbides and nitrides

## Slide 9: Why Carbides?
Possible fuel compositions with higher fissile atom density are non-oxide ceramics, for example, uranium–plutonium-mixed carbide or nitride
These fuels have higher thermal conductivity, high fissile heavy-atom density, and a high melting point compared to metallic fuel
The higher thermal conductivity of carbide fuel and high melting point makes carbide fuel suitable for operation at high power

## Slide 10: Why Carbides?
The more efficient heat transfer also allows for the possibility of large diameter fuel pins, with more fissile material per pin, and more power generation
High-specific-power operation permits fewer pins, compared to oxide, and a more compact core, which can reduce plant costs
A large amount of development work on carbide and nitride fuels was performed from 1960 to 1970, and more than 5000 advanced fuel pins have been fabricated and irradiated
The practical difficulty of fabrication of carbide fuel hampered carbide development
The high-purity inert cover gas required for fuel fabrication was expensive and maintenance of C/M ratio was difficult

## Slide 11: Carbide Reactor
The Indian FBR program started with the introduction of plutonium-rich mixed uranium–plutonium carbide as the driver fuel for a small loop-type fast breeder test reactor
The reactor became critical in the year 1985, is still in service, and it is the only reactor operating on a full core of carbide fuel
A larger reactor is being constructed in India based on this design
Carbide fuel cannot be used in LWR because of its incompatibility with the coolant
However, it can be safely used with liquid metal (Na or Pb) or gas (CO2 or He) coolants in Gen-IV reactors
Carbide fuel has a breeding ratio of at least 1.30, a doubling time of 15 years or less, and a burnup limit of more than 15 at.%

## Slide 12: US Interest in Carbide Fuels
Many laboratories in the world were engaged in studies on the development of carbide fuels based on uranium and plutonium and thorium
After the oil crisis in 1974, a national advanced liquid-metal-cooled FBR fuels development program was initiated that built upon early years of carbide fuel development
Both carbide and nitride fuels offer a middle ground for LMFBR performance because of their higher thermal conductivity, fissile-atom density, and chemical compatibility with liquid sodium, and much higher melting point than metallic fuels

## Slide 13: Carbide Pin Designs
There are two concepts available for the carbide fuel pin depending upon the type of bond between the fuel pellet and the cladding material: He-bonded and Na-bonded carbide fuels
The average operating fuel temperature of the He-bonded pin is high because of low thermal conductivity of the He bond compared to the Na bond
This design requires a larger fuel–clad gap and 85% smear density to accommodate the swelling of the fuel
The fission gas release in a He-bonded pin will be higher compared to that from a sodium-bonded pin, due to the higher temperatures
Na-bonded carbide fuel pins also require a reduced smear density compared to oxide fuels to account for fuel swelling
The purity of the Na bond is very important, requiring strict tolerances on O content

## Slide 14: Carbide Fuel Details
A hyperstoichiometric (C/M>1, carbon to metal ratio) fuel composition is chosen so that it contains some amount of sesquicarbide M2C3 phase (M=U+Pu), which accounts for the decrease in (C/M) ratio with burnup
A low C/M ratio may result in the formation of actinide metal phases, which may form low-melting eutectics with the cladding and limit the life of the fuel pin
FCMI can potentially exist, depending upon the operating temperature of the fuel
O and N impurities play important roles, as they act as ‘carbon equivalent’, which affect the carbon potential of the fuel
Also have high Pu and low Pu designs, which impact properties and impurity sensitivity

## Slide 15: Carbide Fuel Details
Carbide fuels have higher swelling and lower fission gas release than oxide fuels
This is due to the lower fuel temperatures (higher thermal conductivity), and the microstructural evolution of fission gases
However, carbide fuels go to significantly higher burnups, leading to larger fission product inventories
Burnup limits are imposed by cladding stresses/damage due to fission gas pressure and FCMI

## Slide 16: Questions on carbide fuel overview?

## Slide 17: U(Pu)-C Phases
Uranium forms three compounds with carbon: UC, U2C3, and UC2, with only U2C3 being stoichiometric
UC is stable over a wide temperature and composition range
UC2 is stable in two high temperature phases
The Pu–C system has four compounds: Pu3C2, PuC1–x, Pu2C3, and PuC2
UC and PuC are face-centered cubic structures (NaCl-type)

## Slide 18: U/Pu-C Phase

## Slide 19: U/Pu2-C3
This structure is more complex than that of the mono- and dicarbides, and is often difficult to form
U2C3 is produced by a complex preparation procedure and decomposes into a mixture of mono- and dicarbides at high temperatures

## Slide 20: Phase Diagrams of Carbides
The differences in the UC/PuC diagrams are mainly due to (i) the presence of Pu3C2 compound, (ii) the low thermal stability of PuC compared to UC, and (iii) the high stability of Pu2C3 compared to U2C3

## Slide 21: Phase Properties
The brittleness of the monocarbides is due to alternate close-packed planes of metal and nonmetal atoms, restricting the slip and thereby hardening the crystal
Many fission products are not soluble in the monocarbide lattice due to the nature of the carbon bonding
The high density and low FP solubility of UC leads to higher swelling than UO2
The U2C3 phase has more open space in the structure, and generally has less swelling than UC
An increase in O and N impurities results in an increase of carbon activity and CO pressure of the fuel
O impurities are also known to contribute to the actinide redistribution in carbide fuels and fuel restructuring during burnup

## Slide 22: Key Properties
The thermophysical properties that are of importance and affect the fuel performance are solidus/liquidus temperature, thermal conductivity, coefficient of thermal expansion, elastic/fracture properties, creep, and hardness at ambient and at high temperatures
The solidus/liquidus temperatures along with thermal conductivity limit the fuel operating temperature in terms of linear heating rate
Thermal conductivity varies as a function of density, porosity (shape, size, and distribution), composition, presence of a second phase, grain size, etc.
Coefficient of thermal expansion is an important design parameter, the stresses generated in the fuel and by the fuel in the cladding are partly due to the difference in the CTE between the fuel and the cladding

## Slide 23: Key Properties
The elastic and fracture properties of the fuel are primarily responsible for the extent and severity of FCMI
Both thermal-induced and irradiation- induced creep of the fuel also determine the extent of FCMI
Mechanical and creep properties depend on composition, second phases, grain size, etc.
Pu lowers melting point, decreases thermal conductivity, increases expansion, and softens the fuel

## Slide 24: In-pile behavior
The in-pile fuel behavior depends to a large extent on the fuel operating temperature, which in turn depends on the type of pin or bond concept, namely, He-bonded fuel or Na-bonded fuel
A large number of mixed carbide fuels have been irradiated in the US, Europe, Russia, India, and Japan
The performance analysis of the mixed carbide fuel can be best understood based on their burnup period, the structural changes occurring during the burnup, and subsequently the swelling of the pin

## Slide 25: Burnup Stages
This is for He-bonded fuels
Stage A: At the BOL, the fuel undergoes cracking, which results in the movement of the fragmented fuel toward the cladding surface
The fuel–clad gap partly reduces but does not close
Fuel sees a dramatic increase in temperature due to cracking
Stage A lasts for a few days

## Slide 26: Burnup Stages
Stage B: Fuel undergoes unrestrained free swelling, crack healing, or resintering
Resintering/densification occurs for thermally unstable (high Pu high O) or low-density fuels, which causes an initial increase in gap size resulting in the rise in the fuel surface temperature
In stage B, free swelling occurs and crack healing starts, which results in the relocation of fuel fragments further from the center of the fuel to the periphery
Swelling causes fuel–clad gap closure, increase in heat transfer coefficient, and decrease in fuel surface temperature
Surface roughness of fuel and cladding limits complete gap closure
FCMI begins due to the swelling of the fuel
Stage B ends after a burnup of approximately 3 at.%

## Slide 27: Burnup Stages
Stage C
This stage starts after fuel–clad gap closure when a steady minimum surface temperature is reached, and it continues until the end of fuel life
For carbide fuel, this could be up to 15 at.%
At this stage, more homogeneous fuel–cladding interaction starts

## Slide 28: Evolution with Burnup
Carbide fuel containing 70% and 55% PuC was used as the driver fuel for FBTR
PIE at burnups of 2.5, 5, 10, and 15.5 at.% shows the evolution of the pin
After 10 at.% burnup, the gaps had closed at the center of the fuel column
Circumferential cracks due to thermal stresses formed, and a discrete zone free from any porosity is observed near the outer region at high BU

## Slide 29: Fission Gas Release
FGR in carbide fuel pins is lower than oxide fuel pins, mainly due to lower temperatures
Release rates from carbide are <1% at temperatures below 900 C but rise to about 5%–10% with temperature rising to 1200 C
Above 1200 C, gas release is associated with bubble growth and interlinkage at grain boundaries, as in oxide fuels
Low density fuel releases more FG than high density, due to additional porosity
Off-stoichiometry also promotes porosity, and thus increases FGR

## Slide 30: Fuel Restructuring
The cross section can be divided into four structural zones, becomes well defined when the fuel sees a burnup of 1.3 at.%.
Zone 1 is the porous fuel at the center having high temperature and helps in the release of fission gases
Zone 3 contributes to high microscopic swelling
Zone-IV is the coolest zone of the fuel cross section, which is next to the fuel cladding
Zone 2 is an intermediate zone that only exists at very high heating rate (>100 kW/m)

## Slide 31: Fuel Restructuring
Zone 1 has large bubbles, interconnected porosity
Zone 2 exhibits grain growth parallel to the temperature gradient, similar to columnar grains in MOX fuel
Zone 3 has coaxial grain growth and developed porosity
Zone 4 typically has a stable grain size and near as-fabricated porosity
Zone 2 does not always form, expected to form at higher temperatures
At low LHR (<50 kW/m) no restructuring is observed

## Slide 32: Fuel Creep
The source of stresses in the fuel under irradiation is the pressure generated by fission gases produced within the fuel
After the fuel–clad gap closure, free swelling is restrained, and a back stress is generated by the cladding on the fuel
Unlike close-packed metals, deformation of carbide requires much higher stresses because of the strong covalent bonding existing between the metal atom and the carbon atom
Two types of creep deformation are operative in the fuel: temperature-dependent thermal creep and irradiation creep
Thermal creep has been shown to start at 1000C and dominate over radiation-induced creep
The steady-state creep curve has been determined and is a function of stress, temperature, composition, grain size, and impurity content in the fuel

## Slide 33: Fuel Creep
Steady-state creep data of UC1-x and MC1+x at a stress of 20 MPa
Substantial creep only exists for a limited part of the fuel, and thus most of the fuel acts as a brittle material
Irradiation-induced creep is independent of temperature, but increases with fluence
Additional porosity or second phases will change this data
No data on creep of high-Pu mixed carbide or Pu-C fuel

## Slide 34: Carbide FCCI
FCCI in fuel pins containing carbide fuel consists of clad carburization, slight reaction with FPs, and formation of intermetallic compounds
Carbides generally present fewer compatibility problems than MOX fuels
Chemical Reactions with FPs
Very little available oxygen leads to FP-C interactions, and we have an expected decrease in C/M ratio with burnup
Significant FP-cladding interactions are generally not seen
Some Te intergranular attack, some reaction with iodine
Generally not a concern

## Slide 35: Carbide FCCI
Low melting phases
Hypostoichiometric carbide fuels can contain U/Pu metal as a second phase which can form intermetallic compounds with the cladding
Experimental compatibility tests of (U,Pu)C with cladding have shown intermetallic compounds such as (U,Pu)Fe2 or (U,Pu)Ni5 in the fuel and cladding interface
At typical fuel surface temperatures (~1000K), reaction rates should be slow to create intermetallics
However, if sufficient hypostoichiometry is present, can react to form intermetallics

## Slide 36: Cladding Carburization
Carbide fuels are designed to be hyperstoichiometric, which results in a two-phase UC/U2C3 microstructure
The presence of excess carbon prevents the formation of intermetallic phases, but carburizes the cladding
The decarburization of fuel and the carburization of cladding are governed by the dissolution of carbon atoms from the fuel and then diffusion into cladding
Cr forms very stable carbides, and carburization often takes the form of Cr23C6 precipitation

## Slide 37: Cladding Carburization
Cr23C6 precipitation starts at the grain boundaries, and then can proceed along preferred crystallographic planes
The carburization proceeds deeper into the material
The grain boundary carbides can lead to intragranular failure of the steel after only a moderate burnup
Austenitic stainless steels are very susceptible to carburization and are deemed too brittle if carbon content reaches 0.6 wt.%

## Slide 38: Cladding Carburization
Carbon activity and partial pressure of CO are important parameters responsible for clad carburization
In sodium-bonded fuel, carbon transfer from the fuel to the clad takes place by dissolution of carbon in sodium liquid
In He-bonded fuel pins, carbon transfer takes place through CO
Out-of-pile testing with Na-bonded fuel showed carburization above 1000 K, with hardening of the SS316 cladding up to 100 mm
The depth of carburization in Na-bonded fuel was greater than in the He-bonded pins

## Slide 39: Cladding Carburization
Cladding temperature plays a critical role in carburization
The temperature gradient in the fuel causes carbon to migrate to colder zones in the fuel, increasing the C/M ratio at the pellet surface
Carburization depth shows a strong dependence on cladding temperature
Carbon penetration seems to follow a diffusion process with a constant surface concentration

## Slide 40: Na Bonded Pin Performance
For the sodium-bonded fuel pin, the smear density is lower than that of He-bonded fuel
This allows for the manufacture of a denser fuel with less initial porosity
In the beginning (stage A), the fresh fuel fractures, reducing thermoelastic stresses and drastically changing temperature gradient of the fuel
There is no abrupt change in fuel temperature in this concept
The lower temperature of the sodium-bonded pin keeps the swelling rate of the fuel low
The decrease in thermal conductivity with burnup is compensated by a slow decrease in linear heating
FCMI can be avoided till end of life by proper selection of initial fuel–clad gap
Na bond acts like a medium for transfer of carbon from the fuel to clad, causing clad carburization

## Slide 41: He Bonded Pin Performance
He bonding is the most preferred bonding concept of carbide fuel, due to cost and the potential for Na bond deterioration at high burnup
The in-pile performance of the He-bonded pin depends to a large extent on the porosity of the as-fabricated fuel
The initial temperature rise is much higher at the beginning of life because of the lower thermal conductivity of the He bond compared to Na bond
The lower thermal conductivity of the He bond requires the reduction of the fuel–clad gap compared to the Na-bonded fuel
The fuel density for He bonded fuel is lower and has a fabrication porosity of about 15%
The gap closure in the early burnup period results in lowering of the fuel temperature, and free swelling changes into restrained swelling under the contact pressure developed at the clad–fuel interface

## Slide 42: Pin Failure
The mechanical properties of the fuel and clad (creep, fracture toughness) largely predict the fuel behavior after gap closure
Cladding breaches due to FCMI or FCCI can be due to loss of ductility of the clad, carburization of the clad, or fuel swelling
Clad carburization makes the clad surface hard and brittle and cracks form and propagate easily
It has been observed that the He-bonded pin can be operated safely up to 15 at.% burnup (peak burnup 20 at.%).

## Slide 43: Carbide Fabrication
Fabrication of carbide fuel on commercial scale is a difficult task and needs additional care because of its pyrophoricity, high radio toxicity, and the concern for criticality restricts the batch size
Carbide powders formed during carbothermic reduction of oxides are prone to oxidation and hydrolysis
This requires high-purity inert-gas cover in the fabrication line consisting of glove boxes

## Slide 44: Fabrication Techniques
Melting casting
In this method, UO2 or U metal chips with graphite are arc-melted and made into the form of a button
Melting casting route results in large-grained materials compared to that obtained by powder metallurgical methods
The melting casting method is, however, uneconomical due to the high cost of metal fabrication
Metal hydriding– dehydriding
This method is followed for small-scale production of high-purity carbides, where the metal hydride reacts with graphite
Actinide carbides MC and M2C3 can be prepared from a mixture of hydride and graphite
For UC, the reaction between uranium metal and a hydrocarbon gas (methane) is carried out with careful control of the hydrocarbon flow

## Slide 45: Carbothermic Reduction
Uranium monocarbide is mainly produced by carbothermic reduction of UO2 and carbon following the reaction
A mixture of UO2 and carbon is blended together and the mixture is compacted at 300–600 MPa along with an organic binder
The pellets are heated in a vacuum induction furnace and ground to a powder for compaction

## Slide 46: Carbothermic Reduction
Uranium–plutonium-mixed carbide is also prepared by carbothermic reduction of UO2–PuO2
The physical state and homogeneity of the mixture influences the reaction rate and the quality of the final product
The reaction is complicated by the uneven distribution of plutonium in the two carbide phases and the formation of CO2 and CO, especially in hyperstoichiometric feedstock
Pu can volatilize and evaporate, which needs to be controlled via increased CO partial pressure
Carbothermic reduction temperature also depends on the Pu content of the material

## Slide 47: Pressing
The conventional powder metallurgy route of carbide fuel fabrication has certain disadvantages, including pick up of O/N impurities from the cover gas and risks of pyrophoricity
Direct pressing takes the product of carbothermic reduction and presses them into a low density pellet, which can be sintered into the final product
This reduces O pickup, reduces dust and impurities, and reduces time/cost
There is an additional route that involves wet processing of nitrate-based fuels in a sol-gel technique

## Slide 48: As-fabricated microstructures
Carbide pellets are susceptible to surface defects, such as chips and cracks
As in all sintered materials, residual porosity will be present
Varying degrees of the M2C3 phase will be present and are observable via characterization
Mixed carbide fuel with (a) 70%PuC and (b) 20%PuC showing bright/white areas of sesquicarbide phase