## Slide 1: Modeling Reactivity Insertion Experiments of TRISO Particles in NSRR using BISON
Presentation by Robert Gentile

## Slide 2: Introduction
TRISO fuels being considered for wide range of advanced reactors
Under RIA, kernel may experience rapid expansion & melting
Work focuses on modeling TRISO behavior using BISON
Two failure mechanisms considered

## Slide 3: Experimental Data
Data and calculations published by Umeda et. al.
Validation calculation falls in correct range

## Slide 4: Experimental Data

## Slide 5: BISON and Material Models
Finite element code based on MOOSE
Some irradiation models not included in simulations
Primary material properties
  Specific heat
  Thermal expansion
  Thermal conductivity
  Density
  Elastic modulus
Thermal Conductivity
  UO2 capped at 2670 K
Specific Heat
  UO2 capped at 2670 K
Coefficient of Thermal Expansion
  UO2 set to correlation form MATPRO

## Slide 6: BISON and Material Models

## Slide 7: BISON and Material Models

## Slide 8: BISON and Material Models

## Slide 9: Model Description
Single TRISO particle surrounded by graphite shell
Interface debonding not permitted
3D mesh used
Simulation run at 10s initial condition, stopped 1s after initiation
0.5ms timesteps used during transient

## Slide 10: Results

## Slide 11: Results

## Slide 12: Results

## Slide 13: Results

## Slide 14: Summary and Future Work
Simulated set of TRISO particle transient irradiation experiments from NSRR
Obtained reasonable agreement in max temperature calculations and experimental SiC fracture probability
Fuel melting predicted at same energy deposition as onset of SiC fracture
Future Work and Improvements:
  Simulating longer pulses and determining stresses in other relevant matrix materials
  Capturing effects of burnup and fast neutron flux on kernel & layers
  Acquiring material property selections from ABAQUS simulations