## Slide 1: NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Last Time
Key thermophysical properties includes thermal conductivity, CTE, creep, etc., and vary strongly based upon composition
Two primary phases: UC and U2C3
Three stages in burnup that affect centerline temperature
Fuel restructures into typically three zones with variable porosity
Carburization of cladding is the key FCCI phenomenon
Control of C/M ratio via initial hyperstoichiometry prevents low melting metal phases forming
Carbothermic reduction is primary fabrication route

## Slide 3: Nitride Fuels
Nitride fuel has been proposed as an advanced fuel for fast reactors and developed since the 1960s
Nitride fuel is a solid solution of uranium mononitride (UN) and plutonium mononitride (PuN), in which the Pu/(U+Pu) molar ratio ranges from 0.15 to 0.25

## Slide 4: Summary