NE 763 Exam 1

Point values indicated expected depth of response.

- What are the individual layers in a TRISO particle? What purpose does each layer have? (10 pts)

- What are the trade-offs between carbide and oxide fuel kernels? (12 pts)

- Discuss fission product chemistry in the fuel kernel. (8 pts)

- How does the nature of irradiation damage accumulation change with irradiation temperature in SiC? How does this impact swelling? (18 pts)

- How does thermal conductivity change in SiC with irradiation? What are the primary phonon scatterers? (10 pts)

- How does graphite dimensionally change under irradiation? Why does this behavior happen? (18 pts)

- List and explain three types of failure mechanisms for TRISO particles. (9 pts)

- Provide one example of an advanced TRISO concept and explain why it is of interest. (5 pts)

- What are the concerns for intermediate heat exchanger materials in a He environment? Discuss corrosion of these materials. (10 pts)