Exam 2: NE533: Nuclear Fuel Performance

Show all work. Label question number in your response. Pay attention to units. Point values correspond to expected depth of response.

- (10 pts) Consider a fuel rod with a pellet radius of 0.55 cm that is experiencing a linear heat rate of 350 W/cm.

  - What is the maximum stress experienced by the pellet? kf = 0.05 W/cm-K, E = 200 GPa, ν = 0.35, and α = 10x10-6 1/K?

  - Given σfracture= 150 MPa, how far do cracks extend into the fuel?

- (10 pts) Consider the stress state in a zircaloy-clad fuel rod pressurized to 15 MPa with an average radius of 0.55 cm and a cladding thickness of 0.05 cm.

  - Calculate all three components of the stress using the thin-walled cylinder approximation.

  - Calculate all three components of the stress at the inside wall assuming a thick-walled cylinder.

- (16 pts) Calculate the change in the gap thickness due to thermal expansion. Do not perform iterations. Rf = 0.52 cm. tgap = 0.005 cm, TCO = 550 K, tclad = 0.08 cm, kfuel = 0.04 W/cm-K, kgap = 0.003 W/cm-K, kclad = 0.15 W/cm-K, LHR = 175 W/cm, c = 10x10-6 1/K, f = 14x10-6 1/K, Tref(fuel=clad) = 300 K.

- (10 pts) What are the hoop and radial stresses at the inner radius of the cladding due to thermal expansion? DT=50 K; ac=15x10-6; E=100 GPa; n=0.34; tc=0.06 cm; Ri=0.55cm.

- (6 pts) Determine the densification. Fission rate = 6x1013 fiss/cm3-s, 0=0.015, BD=5 MWD/kgU, (UO2) =10.97 g/cc, t=100 days.

- (5 pts) Describe both elasticity and plasticity.

- (8 pts) Define strain hardening. What causes strain hardening?

- (3 pts) What three things must all fuel performance codes be able to do?

- (3 pts) Provide an example of a 0-D defect. Provide an example of a 3-D defect.

- (5 pts) How do grains form in the sintering process of fuel?

- (8 pts) Describe the concept of microstructure-based (mechanistic) fuel performance modeling and why it is beneficial.

- (8 pts) What is meant by microstructure? Given an example of a processing technique and the impact it has on the microstructure and related properties.

- (4 pts) Does diffusion occur more quickly inside the grains, or on the grain boundaries? Why?

- (4 pts) What is a driving force for grain growth? What can impede grain growth?