## Slide 1: Lecture 7: Analytical solution of the fuel temperature profile
January 25, 2017
Michael R Tonks
Mechanical and Nuclear Engineering
Some content taken Professor Motta’s book, chapter 9

## Slide 2: Today we will begin our discussion of heat transport in the fuel
Module 1: Fuel basics
Module 2: Heat transport
  Intro to heat transport and the heat equation
  Analytical solution of the heat equation
  Numerical solution of the heat equation
  1D solution of the heat equation using Matlab
  2D solution of the heat equation using Matlab
  Coolant temperature change, power generation, and melting
Module 3: Mechanical behavior
Module 4: Materials issues in the fuel
Module 5: Materials issues in the cladding
Module 6: Accidents, used fuel, and fuel cycle

## Slide 3: In order to solve for the temperature profile in the fuel and cladding, we make assumptions
Assumption 1: We only care about the steady state solution
Assumption 2: The behavior is axisymmetric
Assumption 3: T is constant in z
Assumption 4: The thermal conductivity k is independent of T
Q
T0
Ts
  TCO TCI
Tcool

## Slide 4: We will start by solving for the temperature profile in the fuel
Consider the radius r = 0 in the center and r = Rf on the outer edge
Use the boundary conditions: T’(0) = 0, T(Rf) = Ts
Solve for the temperature T(r)

## Slide 5: The linear heat rate is the heat rate delivered per unit length of fuel
LHR = πRf2Qav (W/cm), where Qav is the radially averaged heat generation rate
If we substitue LHR into our temperature equations, we get

## Slide 6: Next, we need to determine the heat transport through the gap
Derive an expression to solve for Ts - TIC
Fuel
clad
qfuel = qgap
Ts TIC
We can define the gap conductance
So,
We assume a linear temperature profile across the gap

## Slide 7: The thermal conductivity of the gap depends on the gas that is filling it
The gas can is filled with He at the beginning of life, but begins to fill with Xe due to fission gas release.
A = 16 for He and 0.7 for Xe
The fraction of Xe in the gas mixture, y, increases with time
The thermal conductivity of the mixture is determined with
Then, compute the conductance

## Slide 8: Now we find the temperature change in the cladding
The expression for TIC – TOC is
Fuel
clad
qfc = qclad
TIC TOC

## Slide 9: The last step is to compute the temperature change through the coolant
Heat conduction through the coolant is due to convection
hcool is the convective heat transfer coefficient

## Slide 10: So, to summarize the analytical temperature equations:
Note, tC = δc
Fuel:
Gap:
Cladding:
Coolant:
Inc terms of Q
In terms of LHR

## Slide 11: Fuel and Cladding Thermal Properties

## Slide 12: To solve for the temperature profile across the radius, you first solve for the transition temperatures
You first solve for the transition temperatures.
Start from the coolant and work inward
Then, assume a linear profile everywhere except in in the fuel
Finally, solve for the temperature profile throughout the fuel
Q
T0
Ts
  TCO TCI
Tcool

## Slide 13: Example: Calculate the temperature profile for a fuel rod using the following data:
Tcool=580 K; LHR = 200 W/cm; hcool =2.5 W/cm2- K
Fuel pellet radius RF =0.5 cm, Cladding thickness C= 0.06 cm; Gap width gap= 30 m
First, we calculate TCO = LHR/(2 π Rf hcool) + Tcool TCO = 200/(2 π*0.5*2.5) + 580 = 25.5 + 580 = 605.5 K;
Then, TCI = LHR C/(2 π Rf kc) + TCO, where kc = 0.17 W/cm-K (from table) TCI = 200*0.06/(2 π*0.5*0.17) + 605.5 = 22.5 + 605.5 = 628.0 K ;
Next, Ts = LHR /(2 π Rf hgap) + TCI, where kHe = 16-e6 Tci0.79 = 0.0026 W/cm-K hgap = kHe/δgap = 0.0026/30e-4 = 0.87 W/cm2-K Ts = 200/(2 π*0.5*0.87) + 628.0 = 73.5 + 628.0 = 701.5 K ;
Finally, T0 = LHR/(2 π k) + Ts, where k = 0.03 W/cm-K (from table) T0 = 200/(4 π*0.03) + 701.5 = 530.5 + 701.5 = 1232.0 K ;

## Slide 14: We finish, by calculating the temperature profile throughout the fuel

## Slide 15: In class problem: Calculate the fuel centerline temperature if 30% of the gas in the gap is Xe
Tcool=580 K; LHR = 200 W/cm; hcool =2.5 W/cm2- K
Fuel pellet radius RF =0.5 cm, Cladding thickness C= 0.06 cm; Gap width gap= 30 m
TOC = 605.5 K; TIC = 628.0 K; T0 – TIC = 530.5 K
kHe = 0.0026 W/cm-K, kXe = 0.7e-6 TCI0.79,
kXe = 0.7e-6 6280.79 = 1.36e-4 W/cm-K
kgap = 0.0026(1-0.3)*(1.36e-4)0.3 = 0.001 W/cm-K
hgap = 0.001/30e-4 = 0.3386 W/cm2-K
Ts = 200/(2π0.5*0.3386) + 628.0 = 188.0 + 628.0 = 816.0 K
T0 = 816.0 + 530.5 = 1346.5 K

## Slide 16: Even 30% Xe in the gap has a large impact on the fuel centerline temperature

## Slide 17: The heat generation rate varies axially, so the LHR does as well
Consider a fuel rod of length 2Z0,
Where
  LHR0 is the centerline linear heat rate (z = Z0)
  where Zex is the extrapolation distance
  γ ≈ 1.3
z
z = 0
z = Z0

## Slide 18: The coolant temperature actually varies with axial position along the rod
Integrating from the core entry (z = 0) to height z:
The axial power profile results in axial variation of LHR

## Slide 19: Example: We will calculate the LHR and Tcool with axial variation
mdot = 0.25 kg/s-rod; Z0 = 150 cm; LHR0 = 150 W/cm; CPW = 4200 J/kg-K; Tin = 570 K
Plugging these values into the equations gives

## Slide 20: Summary
We can derive analytical expressions for the temperature profile within a fuel rod by making four assumptions
  Steady state solution
  Temperature is axisymmetric
  T is constant in z
  The thermal conductivity is independent of temperature
The temperature profile in the fuel is parabolic.
We assume the temperature profiles in the gap, cladding, and coolant are linear