Exam 4: NE533: Nuclear Fuel Performance

Show all work. Label question number in your response. Pay attention to units. Point values correspond to expected depth of response.

- (18 pts) A ZIRLO cladding tube is in reactor at 625 K for 500 days. The initial wall thickness is 600 m.

- Estimate the oxide thickness after this time?

- Assuming the hydrogen pickup fraction is 14%, what is the weight ppm of hydrogen in the cladding? Assume PBR = 1.56, Zr = 6.5 g/cc, ZrO2 = 5.68 g/cc.

- (2 pts) What is the rate-limiting step in the aqueous corrosion of Zr cladding?

- (8 pts) Where do hydrides form in the cladding? Why? What impacts do hydrides have?

- (12 pts) What is a RIA? What is a typical RIA in a PWR or BWR. Describe what happens during a RIA.

- (12 pts) What is a LOCA? Describe the impacts of a LOCA. How is it different than a RIA?

- (4 pts) How does burnup impact the type of failure and the failure probability during an accident?

- (6 pts) What are the four pathways to make the fuel/cladding system more accident tolerant?

- (6 pts) List one near-term ATF concept and why it is of interest.

- (6 pts) What happens to zirconium cladding when it is exposed to high temperature steam?

- (6 pts) List three examples of limiting phenomena governing LWR operation.

- (6 pts) What fuel performance and safety impacts does CRUD have?

- (6 pts) List two water chemistry controls that have been implemented in LWRs, including why they were implemented.

- (8 pts) List and describe two key microstructural phenomena that are unique to MOX fuels.