NE 763 Exam 3

Please provide your responses to the following questions. Point values indicated the expected depth of response.

- What are the types and benefits of molten salt reactors? (6 pts)

Three types: solid fueled molten salt cooled; flowing salt fueled and salt cooled; static salt fueled and flowing salt cooled. Also, can be thermal or fast. High heat capacities, high thermal conductivity, atmospheric pressures, large margin to boiling, negative reactivity coefficient, flexibility of composition, reprocessing can proceed directly, etc.

- What role do the different components of molten salt fuels serve? (6 pts)

Fuel salts typically consist of a fissile species (e.g., UF4), and multiple solvent species. The solvents serve multiple purposes, namely, lowering the melting point, lowering the viscosity, and serving as an oxygen getter to prevent oxidation of the fissile species.

- What role does the cover/sparge gas serve in MSRE type reactors? (6 pts)

Primary control of impurities and redox conditions. Allows for tailoring the fluorine concentration, can assist in removal of fission gases, fission product precipitates, and corrosion products. Critical to control corrosion rates, dissolution, and deposition.

- What does the UF4/UF3 ratio represent, and why do we care about it? (6 pts)

The UF4/UF3 ratio is a proxy for the redox potential, which is effectively a measure of how much excess fluorine is present within the system. A higher UF4/UF3 ratio indicates more excess fluorine and will lead to excessive oxidation of the cladding. An overly low UF4/UF3 ratio will result in the formation of UC compounds with graphite.

- Discuss corrosion of the cladding in a molten salt environment. How does this impact materials selection. (16 pts)

Corrosion occurs through interactions with three types of species: oxides, impurities in the salt, and necessary constituents of the salt. Oxide layers do not inhibit corrosion but can actually accelerate corrosion via the presence of intermediate oxide phases that can more readily be converted to fluorides than the metallic species. Impurities can further accelerate corrosion through the formation of intermediate fluoride compounds (e.g., FeF2), which can then be converted into CrF2. Additional fluorine present will increase the redox potential, which can then lead to reactions of UF4 with Cr metal to generate CrF2. For typical cladding materials, Cr is the most common alloying element that participates in the corrosion process because the formation energy of CrF2 is lower than any other cladding constituent (Fe, Ni, etc.). Cr corrosion has been observed to be rate limited by the diffusion of Cr to the surface of the structural materials. Because of the preference for Cr dissolution into the salt, materials low in Cr (low-Cr Ni-alloys) are the primary candidates for salt-facing components. Also, graphite is of interest in the core of thermal salt reactors due to the low formation energy of CF4 compounds.

- Why are we interested in carbide and nitride fuels? (6 pts)

These fuel types represent a ‘best of both worlds’ area of fuel properties, with high fissile density, high thermal conductivity, and high melting points. This allows for high burnup fuels operating at higher powers. UC and UN are being considered for a number of advanced reactors, including HTGRs, Pb-cooled reactors, and space reactors.

- What are the two types of pin designs for C and N fuels? Discuss design and operational ramifications of the designs. (12pts)

Na-bonded and He-bonded. He-bonded designs are the standard choice with a low pressure He gas filling the cladding tube. He has a low thermal conductivity, and thus these fuels operate at higher temperatures. He-bonded pins must have either lower smear densities or a reduced theoretical density to allow for additional swelling incurred at higher temperatures.  He-bonded pins have relatively high fission gas release due to the high temperatures. Na-bonded pins can have high theoretical densities and smaller gaps due to the high thermal conductivity of Na, which leads to lower temperatures, and subsequently less swelling and gas release. C transport through the Na accelerates carburization of the cladding compared to He-bonded pins. Potential issues of using Na as bond due to pyrophoricity are mitigated through the use of He.

- What are the three stages of temperature evolution in C and N fuels? (8 pts)

A) Initial temperature ramp-up, leads to thermal cracks which further reduce the effective thermal conductivity and cause an increase in the temperature. B) Densification and unrestrained free swelling proceed, which initially increases the gap and then proceeds to close the gap, leading to a steady decrease in fuel temperature. C) Closure of gap, pseudo steady-state temperature, restrained swelling and FCMI occurs.

- How do carbides and nitrides restructure as a function of burnup? (10 pts)

Typically restructure into 3 zones. Central high temperature zone is highly porous, releases fission gases. Intermediate zone consists of equiaxed grain growth. High fission gas swelling in region 2, but temperatures not sufficiently high to allow for large bubble interconnection and release. Outer zone is the coolest zone, small fission gas bubbles, no fission gas release, minimal swelling contribution, as-fabricated microstructure. All three zones form for both carbides and nitrides. In carbides, a fourth zone can develop which is similar to the columnar grain growth region in MOX fuels if the linear power is sufficiently high. At very low powers, no restructuring will occur.

- Discuss FCCI for carbide fuels. (10 pts)

Fission products typically will only form carbide phases, metallic precipitates, or gas bubbles in the fuel, and thus are of limited concern. If C/M ratio is too low, low melting point intermetallics may form at fuel/cladding interface. Thus, carbides are made with excess C, which then contributes to carburization, which is the primary FCCI concern. Carbon is transported to the cladding and can form Cr23C6 precipitates. Precipitates form first on grain boundaries and can then propagate along crystallographic planes intragranularly. Carburization leads to embrittlement of the cladding because carbides impede dislocation motion. Carburization is worse in Na-bonded pins.

- What is the primary cause of failure (and burnup limits) in UC and UN fuels? How is it mitigated? (6 pts)

Fuel cladding mechanical interaction (FCMI). This is because of the higher swelling of UC/UN compared to oxide fuels and the lower creep rates due to slower diffusivities. Carburization/nitriding embrittles the cladding, exacerbating the stresses from FCMI. FCMI can be mitigated through a lower smear density or a more porous fuel.

- How do the C/M and N/M ratios change with burnup? Why is this important? (8 pts)

C/M ratio decreases with burnup, as fission products react with C. This potentially allows for the formation of intermetallic precipitates which have low melting points. Thus, carbides are usually fabricated as hyperstoichiometric. Result of hyperstoichiometry is carburization of the cladding. N/M ratio increases slightly with burnup, as fewer fission products can form stable nitride phases. This can lead to the formation of U2N3 phases and potential nitriding of the cladding.