## Slide 1: NE 763: Advanced Reactor Materials
Fall 2025
Dr. Benjamin Beeler

## Slide 2: advanced cladding

## Slide 3: The need for advanced cladding
Austenitic stainless steels are widely used as structural components in nuclear service
At high dose, the microstructure develops a high concentration of voids, leading to dramatic swelling
Void swelling in 304SS
Swelling of cladding in FFTF and BN-600

## Slide 4: The need for advanced cladding
High fluence can also provide significant radiation hardening, coupled with severe losses in ductility
In addition to high fluence, high temperature contributes to void swelling
SS significantly weakens with increasing temperature
Thus, their applicability is limited in advanced reactor systems where high dose and high temperature are present

## Slide 5: Fast Reactor Conditions
The structural components experience a different environment in advanced fast reactors than those in commercial LWRs
Key phenomena include void swelling, irradiation growth, irradiation hardening, irradiation creep, and helium embrittlement

## Slide 6: Ferritic and Ferritic-Martensitic Steels
The advanced ferritic and ferritic–martensitic steels of current interest have evolved from creep-resistant ferritic steels
Subsequent developments through different levels of Cr and Mo have led to the current ferritic and ferritic–martensitic steels: 9–12% Cr–Mo steels
F-M steels have advantageous mechanical properties, are relatively cheap, and control of their microstructure can be performed with heat treatments
F-M steels generally have worse high T mechanical properties than austenitic steels, especially creep life and irradiation creep resistance

## Slide 7: Crystal and Microstructures
alpha-Fe: ferrite, bcc
gamma-Fe: austenite, fcc
delta-Fe: high temperature ferrite, bcc
martensite: C-rich bct
pearlite: lamellar combination of ferrite and cementite (Fe3C)
also upper and lower bainite: don’t worry about it
alpha’: Cr rich ferrite (mainly induced via thermal aging)
martensite
ferrite
ferrite-martensite

## Slide 8: Ferritic-Martensitic Steels
The ability to retain ferrite is dependent upon the alloying elements and the heat treatments
In addition to Cr and Mo, the amount of Si, V, and C affect the phase boundaries
Accordingly, the 9-12% Cr/Mo family of steels can either be martensitic (9Cr–1MoVNb (T91)), ferritic (12Cr–1MoVW (HT9)) or ferritic–martensitic (9Cr–2Mo–V–Nb (EM12)) steel
TTT diagram of austenite
Pseudo-binary phase diagram with Cr equivalent

## Slide 9: Composition Effects
The development of 9Cr-Mo steels was initially focused on oxidation resistance and creep strength
The optimized initial alloy composition considered was 9Cr, 2Mo, 1W, 0.5Si, with C, B, V, Nb, and Ta in small amounts
A reduction in Cr content lowers the oxidation resistance
Higher Cr content has two effects, 1) it increases the hardenability leading to the formation of martensite, and 2) promotes the formation of d-ferrite, reducing the toughness
If the W+Mo concentration is kept <3%, creep strength will reduce, while higher amount promotes the formation of δ-ferrite and brittle Fe2Mo Laves phase

## Slide 10: Composition Optimization
The addition or replacement of Mo with W and B increases the stability of M23C6
Lower Ni content introduces δ-ferrite, while its increase reduces creep strength
Lower Si reduces oxidation resistance, while higher Si content leads to agglomeration of carbides
The composition of all other elements can be optimized, based on structure–property correlation studies

## Slide 11: Composition Optimization
The development of high creep-rupture strength steels is based on optimizing the composition, δ-ferrite content, increasing the stability of the martensite, dislocation structure, and maximizing the solid solution and precipitation hardening
Based upon this property tailoring, a large number of alloys have been developed over the last 75 years
Reduced activation ferritic-martensitic (RAFM) steels steels have been developed in order to make concentrations of high activation residual elements lower

## Slide 12: Microstructure
The microstructure of the steels consists of a) martensite laths containing dislocations; b) coarse M23C6 particles located at prior austenite and ferrite grain boundaries; c) finer carbide precipitates found within the laths and at the lath/subgrain boundaries
M2X precipitates rich in Cr also form
HT-9 initial microstructures

## Slide 13: Microstructure
In reactor, this microstructure will change, with the M2X precipitates being replaced by MX intermetallic and Laves phases due to long exposure to high temperature
There are three types of processes with respect to evolution of secondary phases: irradiation-induced precipitation, irradiation-enhanced transformations, and the irradiation modified phases
The evolution of these phases depends on the composition and structure of the steel and the irradiation parameters like the temperature and fluence
Fe2Mo Laves intermetallic phase around the M23C6

## Slide 14: Radiation Damage
Dislocation loops are the primary defect species observed
Loops are typically larger and with a lower number density as the irradiation temperature is increased
Loop size and density are increased as a function of dose, with loop density potentially saturating at 10 dpa
Voids can also form above 400C
Radiation-induced segregation can occur in these steels, but has been significantly less studied than in austenitic steels
General consensus that Cr is depleted at interfaces, and Ni, Si , and P are enriched at sinks
RIS appears to be dependent on both irradiation dose and temperature

## Slide 15: Phase Precipitation
Thermal processing will lead to precipitation, which affects the mechanical properties
Most of the carbon forms in M23C6 precipitates, which increase strength and reduce ductility
RIS leading to Cr depletion increases the matrix Cr composition and can lead to alpha’ formation, which embrittles the material
Chi, G, and sigma phases are enriched in Si and Ni and can nucleate at interfaces

## Slide 16: Precipitate Hardening
Precipitation hardening relies on changes in solid solubility with temperature to produce fine particles of an impurity phase which impedes the movement of dislocations
Since dislocations are often the dominant carriers of plasticity, this serves to harden the material

## Slide 17: Irradiation Hardening
Microstructure changes lead to irradiation hardening of the steel
High amounts of carbon in 12% Cr steels leads to a large amount of precipitation, up to twice as much as 9% Cr steels
This high carbon content is needed to use steels as martensite
Both the steels have mainly M23C6 carbides with a small fraction of monocarbides
This high concentration of precipitates can eventually lead to brittle failure
The critical stress is inversely proportional to the crack length, crack length is equal to the diameter of the carbide precipitate, thus fracture stress also decreases with increasing precipitate size

## Slide 18: Irradiation Creep Resistance
Irradiation creep resistance needs a good combination of thermal creep behavior and long-term microstructural stability at high temperature
In order to fabricate creep resistant steels, you design to have a number of microstructural features that are present
  Introduce high dislocation density to increase the strength of the basic lattice
  Strengthen the host lattice by solid solution strengtheners or defects
  Stabilize the boundaries created by phase transformations by precipitating carbides along the boundaries
  Arrest dislocation glide and climb by selection of crystal structure, solid solution, interfaces, dislocation interactions
  Resist sliding of grain boundaries by introducing special types of boundaries and anchoring the boundaries with precipitates

## Slide 19: Irradiation Creep Resistance
Ensure long-term stability of the microstructure, especially against recovery and coarsening of the fine second phase particles
In the case of 9–12 Cr steels, the martensitic lath structure decorated with only MX which should be stable over long-term service life is the most desired structure
MX can be stabilized over M23C6 by reducing the carbon content, but we need high amounts of C to have appropriate high temperature behavior
undesirable
desirable

## Slide 20: Irradiation Creep Resistance
So careful tailoring of alloying elements has led to improvement of the creep strength
Thermal creep behavior provides a starting point, which can then be refined by studying creep under irradiation
The irradiation creep depends on the stress level, the temperature, and the dose
Thermal Creep
Irradiation Creep

## Slide 21: Irradiation Creep Resistance
The excess point defects precipitate into either interstitial or vacancy loops, but not randomly
The interaction between point defects and stress leads to the precipitation of interstitial loops parallel to the applied stress, while vacancy loops form in planes perpendicular to the stress: stress-induced preferential nucleation (SIPN)
Under applied stress, the vacancies migrate preferentially to grain boundaries perpendicular to the applied stress, while the interstitials toward boundaries parallel to the stress: stress-induced preferential absorption (SIPA)
SIPN
SIPA

## Slide 22: Creep Evolution
The radiation-induced defects also evolve from isolated point defect to loops and voids, which have different types of influence on irradiation creep
Irradiation creep occurs simultaneously with swelling and swelling can influence irradiation creep
At very small dose levels, swelling enhances creep rates; beyond a certain dose level the creep component reduces; at high dose levels creep disappears, while swelling continues

## Slide 23: Irradiation Embrittlement
Ferritic steels have a large number of monocarbides which aid in creep resistance
The lath boundaries are decorated with Cr rich M23C6 precipitates which increase the thermal stability
Embrittlement is caused by 1) segregation of elements to lath boundaries which make the grain boundaries decohesive, and 2) evolution of carbides and intermetallic phases
For removable components such as cladding, which are subjected to high temperature and pressure with a residence time of a few years, creep is the issue which decides their design and performance
For permanent support structures increase in hardening and loss in fracture toughness on irradiation are major issues

## Slide 24: Irradiation Embrittlement
The increase in the ductile to brittle transition temperature, DBTT, is known to be related to irradiation hardening, which is generally observed to saturate with fluence
Evidence for a possible maximum in DBTT was observed for the 12Cr steel irradiated in the range of 35–100 dpa in the FFTF
High fluence and/or high temperature are required before a maximum is observed
Thus, these properties are a balance between the point defect production and irradiation-induced precipitation
The precipitation during irradiation hardens the steel and irradiation accelerated recovery and aging soften the steel
The high temperature recovery produces an observable saturation in hardening above ~720K

## Slide 25: DBTT Changes

## Slide 26: DBTT
BCC materials can undergo significant increase in the DBTT at low T for even 1 dpa
The minimum operating temperature to avoid embrittlement F/M steels is ~500 K
Extensive evaluation of the embrittlement behavior of the ferritic steels for different compositions has been performed
Compositions around 9Cr show the least change in the DBTT, and addition of phosphorous, copper, vanadium, aluminum, and silicon increase the DBTT
The 12Cr steels, like HT9, show a larger shift in DBTT as compared to modified 9Cr–1Mo steel, balancing between swelling resistant 12Cr steels and 9Cr steel which is less prone to embrittlement than 12Cr steels

## Slide 27: Features affecting Embrittlement
There are a number of microstructural features that can impact the embrittlement of F/M steels
Prior austenite grain size (PAGS)
The size of martensitic lath (which is sensitive to austenitization temperature)
Tempering/annealing, which can increase carbide precipitate size
The generation of helium through (n,alpha) reaction

## Slide 28: Void Swelling Resistance
Ferritic steels were experimentally observed to exhibit superior radiation resistance compared to austenitic steels, which is largely based on their low swelling behavior
The 9Cr–1Mo steel, modified 9Cr–1Mo (Grade 91), 9Cr–2Mo, and 12Cr–1MoVW (HT9) have low swelling rates at doses as high as 200 dpa
The threshold dose for swelling in ferritic steels is as high as nearly 200 dpa, compared to 80 dpa for the present generation austenitic stainless steel
HT9 shows 1% swelling at 693 K for 200 dpa