## Slide 1: NE 591: Advanced Reactor Materials
Fall 2021
Dr. Benjamin Beeler

## Slide 2: Last Time
Thermal conductivity degradation
  fission gas swelling/porosity, sodium infiltration
Fuel-cladding mechanical interaction
  fuel swelling, creep, internal pressure, etc.
Fuel-cladding chemical interaction
  phase diagrams and kinetics, low melting points, intermetallics, etc.

## Slide 3: FCCI
The burnup of a fuel pin is another parameter that impacts the size of the fuel–cladding interaction zone
Larger interaction zones are observed for higher burnup fuel elements
The larger inventories of fission products allow more lanthanides to diffuse down the temperature gradient, thereby increasing the inventory of fission products at the interface
For high burnup fuels, temperature effects also exacerbate FCCI due to thermal cond. degradation producing higher temperatures, and more rapid FP diffusion
Fuel elements at the hotter core positions can exhibit increased interdiffusion at the fuel–cladding interface over those at colder positions

## Slide 4: Fuel-Cladding Chemical Interaction

## Slide 5: Metal Fuel Fabrication
Injection casting has been utilized for fuel slug fabrication
Remote fabrication has been performed inside a hot cell on recovered uranium
Fuel slugs for EBR II and FFTF were fabrication via injection casting

## Slide 6: Metal Fuel Fabrication
Starting materials are charged into the graphite crucible in the furnace
Silica molds with tops closed are set above the crucible
Crucible is coated with yttria
Molds coated with zirconia

## Slide 7: Metal Fuel Fabrication
Furnace closed and filled with Ar gas
Crucible is inductively heated to 1830K, and stirred electromagnetically
Ar gas removed, molds are lowered, then Ar gas returned
Pressure difference injects the melt into the molds

## Slide 8: Reprocessing
Pyroprocessing
In the electrometallurgical
process, irradiated metal fuel is anodically dissolved
While uranium is deposited on the solid cathode, plutonium is collected in the liquid cadmium cathode with uranium, minor actinides (MA: Np, Am, Cm), and part of the lanthanide fission products
This inherently low-decontamination aspect brings about a proliferation- resistant feature to the electrometallurgical process

## Slide 9: Reprocessing
Pyroprocessing
Can reduce the repository burden of radioactive waste by separating long-lived MA from spent light-water reactor fuel, burning MA in fast reactors, and decreasing the long-term radioactivity of nuclear waste
Metal-fueled fast reactors facilitate the effective transmutation of MA because of the high-energy neutron spectrum
One of the measures to load MA into the reactor core is to add MA to the fuel alloy homogeneously

## Slide 10: Refabrication
Injection casting
These technologies are expected to reduce the fuel cycle cost even for small-scale fuel cycle plants because of the simplicity of the process and the compactness of the equipment
For example, in the injection casting process, composition adjustment, melting (alloying), and casting of the fuel slug can be done in a single injection-casting furnace

## Slide 11: SFR Cladding
HT9 is the current cladding material of choice for SFRs
HT9 is a nonswelling martensitic stainless steel
The rate of cladding strain has increased for the initially 85% fuel smeared density elements
12.5% BU

## Slide 12: Metal Fuel
Introduction
Fabrication
Constituent Redistribution
Swelling and Fission Gas Release
FCMI
FCCI
Fission Product Behavior
Factors Controlling Fuel Lifetime

## Slide 13: Mixed oxide fuel

## Slide 14: Mixed Oxide (MOX) Fuel
Introduction
Fuel Restructuring
Constituent Redistribution
Geometrical Evolution
Evolution of O/M ratio
Migration of Fission Products
Fission Gas Release
Life Limiting Phenomena

## Slide 15: MOX Introduction
Despite some disadvantages, such as its low U density, poor thermal conductivity, and its chemical reaction with sodium, MOX fuel (U,Pu)O2 is the fuel that has been used most in fast reactors
In order to avoid the dramatic swelling of metallic fuels, MOX fuels were explored in fast reactors
Behavior was observed to be satisfactory and was relatively widely implemented in SFRs

## Slide 16: Geometry
The fuel pin 2–3m long, 5–10mm diameter, clad in a steel tube 0.4–0.6mm thick closed in both ends by welded plugs

## Slide 17: Sodium coolant

## Slide 19: pyroprocessing

## Slide 23: Questions?